## Slide 1: DPS in NYS
Richard Hamilton
Advance Testing Company

## Slide 2: Testing to Date
16 paving days on Route 30A in Glen, NY
  8 miles long
  9 days 19mm <0.3
  7 days 9.5mm <0.3
1 paving day on Route 97 in Lordsville, NY
  9.5 mm <0.3
Zipper pattern with 3 ft and 9 ft offsets
Additional pass 2.5 ft where joint matching

## Slide 3: Puck Correlations w/RDM 1.0
Chart: Route 97 9.5 mm Pucks vs Dielectric
| 5.9260799999999998 | 5.8557133300000004 | 5.0134466700000004 | 5.0732566700000001 | 5.8225666699999996 | 5.7000799999999998 | 5.0849033300000004 | 5.0799933299999998 | 5.2958100000000004 | 5.33765 | 5.5559433299999998 | 5.5608500000000003 | 5.54345 | 5.2888933299999996 | 5.3312766700000003 | 5.5746200000000004 | 4.9647166699999996 | 5.5626866699999997
 | 151.3 | 150.7 | 133.4 | 134 | 149.1 | 149 | 136.7 | 136 | 138.9 | 138.6 | 146.6 | 144.4 | 143.9 | 141.3 | 141.8 | 145.2 | 132.7 | 144.8

## Slide 4: Data Analysis
Chart: 30A NB 9.5 mm Density, pcf (100 ft. average)

## Slide 5: Data Analysis
Chart: 30A SB 9.5 mm Density, pcf (100 ft. average)

## Slide 6: QA Procedures
Sensor leveling
HDPE Scans
Swerve testing

## Slide 7: Data Analysis
Chart: Density, pcf

## Slide 8: Core Prediction
Chart: Core Density vs RDM Prediction
| 1
Core 1 Density | 145.08 | 146.6
RDM 1 Ave. | 146.6
Core 2 Density | 146.2
RDM 2 Ave. | 145.7
Core 3 Density | 142.1
RDM 3 Ave. | 143