## Slide 1: MnDOT Data Collection and Analysis
Kyle Hoegh
Mercedes Maupin
Shongtao Dai

## Slide 2: MnDOT Analysis: 2021 Collection Season
Hired 2 contractors to collect according to data specification
  Mathy: Pay by the section with a DPS cart they own (needed to borrow our puck kit and GPS equipment)
  Ulland: Pay be the project with minimum acceptable coverage using rental DPS (needed to borrow our GPS equipment initially, and at times throughout the season
4 Projects (TH21 – 13 days, TH 60 (2 projects – 27 days, TH 30 – 6 days)
  Last year: 6 Projects with puck fabrication (251, 2, 30, 95, 25, MnROAD)
46 production days with Core Accuracy Checks
  Last year: 30 unique production days
> 300 pucks fabricated and tested
  Last year: 78 pucks fabricated and tested
> 600 dielectric tests
  Last year: 234 dielectric tests

## Slide 3: Data Consistency Check
On-Site Result: Swerve
https://youtu.be/A3j870wC2dA?t=285

## Slide 4: Data Consistency Check
On-Site Result: Swerve
https://youtu.be/A3j870wC2dA?t=422

## Slide 5: Data Consistency Check
On-Site Result: Swerve
https://youtu.be/A3j870wC2dA?t=459
Pass Forward
Pass Back

## Slide 6: Data Consistency Check
On-Site Result: Swerve
https://youtu.be/A3j870wC2dA?t=486
Pass Forward
Pass Back

## Slide 7: Data Consistency Check
On-Site Result: Line Test
https://youtu.be/A3j870wC2dA?t=192

## Slide 8: Data Consistency Check
On-Site Result: Line Test
https://youtu.be/BdLn62fxHRc?t=21

## Slide 9: Data Consistency Check
On-Site Result: Line Test
https://youtu.be/BdLn62fxHRc?t=163

## Slide 10: Data Consistency Check
On-Site Result: Line Test
https://youtu.be/BdLn62fxHRc?t=295
Right Sensor
Center Sensor
Right Sensor

## Slide 11: Data Consistency Check
On-Site Result: Line Test
https://youtu.be/BdLn62fxHRc?t=295
Density:
Density:

## Slide 12: Data Consistency Check
Season Results: Continued last year’s trend of highly consistent sensors!
  Last Year: Little to no bias between sensors on average
    171:
      0.014 avg
      93% within 0.08
      78% within 0.05
    173:
      -0.006 avg
      96% within 0.08
      90% within 0.05
    181:
      -0.007 avg
      94% within 0.08
      81% within 0.05
  This year only required consistency check every 4000 ft. or 4 hours whatever comes first.

## Slide 13: Dielectric to Density: Core Accuracy Check
2020: TH2 Example
Puck conversions continue to be very stable day to day
  Small day to day variation if no significant changes in mix
  Able to detect large mix changes
mndot.gov
2021: TH 60 Example (>100 pucks)

## Slide 14: 2020 Dielectric to Density: Core Accuracy Check
Mostly reasonable agreement

## Slide 15: 2020 Dielectric to Density: Core Accuracy Check
Some biased but good relationship e vs %Gmm

## Slide 16: 2020 Dielectric to Density: Core Accuracy Check
Some poor relationship

## Slide 17: 2021 Dielectric to Density: Core Accuracy Check
2021 Results: Continued last year’s trend of mostly good agreement:
  Click excel document here to go through details of the 2021 results

## Slide 18: 2021 Dielectric to Density: Bias Investigation
2021 Results: Still some worrisome days with bias between field and pucks
  Contacted GSSI with issue: Initial investigation has no “smoking gun” (shown here in next few slides)
  More detailed investigation with UNH contract
  Proposed technical working group meetings to attack challenges and get feedback on potential solutions

## Slide 19: 2021 Dielectric to Density: Bias Investigation
Plot of showing bias spanning a set of 18 paving days (dataset) from TH60 exhibiting the bias
  Nomalize cores and pucks to max density dielectric (calculated using mix model) and plotting confirms bias between cores and pucks.
Finding root cause of this bias is the goal of the investigation

## Slide 20: 2021 Dielectric to Density: Bias Investigation
A sub-sample from 9 paving days was chosen. The sub-sample consists of 3 different observed scenarios:
  Good Agreement between cores and pucks (6-22, 6-29, 7-16)
  Core and puck calibrations appeared to be linearly offset (6-15, 6-18, 6-21)
  Core calibration shows no linear trend (6-17, 6-25, 6-30)

## Slide 21: Initial evaluation of sources of bias
Need for calibration puck in lab
  RDM 2.0 kit has this
Bias between surface reflection dielectric (field) and velocity dielectric (lab)
  Use magnetic susceptibility meter
Moisture presence
  Use moisture gauge?
Use of Puck thickness that is consistently too high or low
  Thickness Gage shows no significant thickness error in Gyratory readout
  Some variability in high voids

## Slide 22: Potential Sources of Error or Bias: Magnetic Susceptibility
Granite with Magnetic Susceptibility of 0.02 and dielectric of 5.5
Dielectric calculated by travel time = 5.5* (1.02) = 5.6
Dielectric calculated by surface reflection = 5.4

## Slide 23: Potential Sources of Error or Bias: Magnetic Susceptibility
Material bias needs to be evaluated in two ways
  Magnetic susceptibility measurements need to be performed. A potential tool for this is the KT-10 magnetic susceptibility meter.
    Interestingly, the Gmm Dielectric of the TH60 pucks translates to an aggregate dielectric of over 7.0 using the mixing model. This high dielectric suggests that the aggregate may either be limestone or a granite with heavy metals, such as iron, which may provide some magnetic susceptibility.
    Magnetic susceptibility measurements on a sample of the TH60 pucks performed at UNH on 11/4/21 indicate no significant magnetic susceptibility.
    UNH has possession of pucks for additional testing

## Slide 24: Initial evaluation of sources of bias
Need for calibration puck in lab
  RDM 2.0 kit has this
Bias between surface reflection dielectric (field) and velocity dielectric (lab)
  Use magnetic susceptibility meter
Moisture presence
  Use moisture gauge?
Use of Puck thickness that is consistently too high or low
  Thickness Gage shows no significant thickness error in Gyratory readout
  Some variability in high voids
DPS Moisture Test with Gann Meter and FLIR MR160 Meter

## Slide 25: Initial evaluation of sources of bias
On 3 days there are calculated Percent voids less then -5%. This scenario corresponds to an anomalously high reflection amplitude that is often related to excessive moisture on the surface.

## Slide 26: Initial evaluation of sources of bias
Need for calibration puck in lab
  RDM 2.0 kit has this
Bias between surface reflection dielectric (field) and velocity dielectric (lab)
  Use magnetic susceptibility meter
Moisture presence
  Use moisture gauge?
Use of Puck thickness that is consistently too high or low
  Thickness Gage shows no significant thickness error in Gyratory readout
  Some variability in high voids

## Slide 27: Potential Sources of Error or Bias: Puck Thickness Sensitivity
Precise puck thickness equipment shows generally good agreement with gyratory readouts
  Saved one puck per day: 46 pucks
  Compared gyratory reading to puck thickness measurement

## Slide 28: Initial evaluation of sources of bias
Effect of Temperature
  Sensor internal
  Pavement surface
  Puck temperature
  Heating history of the antenna from one day to the next
    Potential impact up to 0.1 difference in dielectric
    If antenna temperature calibration has changed since factory cal, this difference could be greater than 0.1
Using the approximation that a 1% change in amplitude translates to about a 1.2% change in voids, it is observed(left size) that the vast majority of the core measurements have a normalized amplitude that is 0.995 or greater. This means that any temperature correction applied to the measurements would modify the calculated % voids by about 0.6 or less.

## Slide 29: Initial evaluation of sources of bias
Effect of Temperature
  Sensor internal
  Pavement surface
  Puck temperature
  Increase in dielectric per change in temperature approximately 0.1 dielectric per 100 degrees Fahrenheit
  Not significant enough to explain difference.

## Slide 30: Initial evaluation of sources of bias
Effect of Temperature
  Sensor internal
  Pavement surface
  Puck temperature
  Increase in dielectric per change in temperature approximately 0.08 dielectric per 100 degrees Fahrenheit
  Not significant enough to explain difference.

## Slide 31: Initial evaluation of sources of bias
Effect of Sensor Height: Highly variable if deviated from height at metal plate calibration
  Can be a change of over 0.1 dielectric for a 0.2 in. change in height.

## Slide 32: Initial evaluation of sources of bias
Effect of Sensor Height
SN 303
SN 303
Comparisons between %Void differences and Metal plate calibration height (left) and height change between the metal plate and core measurements (right) reveal no suspicious trends.

## Slide 33: Initial evaluation of sources of bias
Effect of Surface Texture: Potential Segregation?
To calculate the data plotted, only the distance-based core file data were used.
The standard deviation of the surface reflection amplitude from each scan is divided by the standard deviation of the direct coupling amplitudes. The averages from all the cores are plotted. Values greater than 1 imply surface texture/lateral variability in dielectrics. There are two anomalous days – day 1 and day 3.

## Slide 34: Initial evaluation of sources of bias
Effect of Metal Calibration
  The calibration from Day 4 was used to process the data because the data from it had the lowest %Void difference. After reprocessing, the average %Voids difference decreased in all the other datasets. The decrease in %Void difference was substantial in Day 2 data. The decrease in %Void difference was not sufficient to entirely remove bias, but the median bias is decreased from 1.9% to 1.3%.
  Doesn’t explain shift.

## Slide 35: Evaluation will continue with UNH and others. . .
Will look at other effects in addition to statistical analysis on data:
  Mix tested right out of truck for pucks, maybe sample behind paver?

## Slide 36: Density Assessment – Finalized Defect Detection and “PWL (really percent conformance) Released
Email from GSSI last week (11/3):
The reason for this email is to provide you information about this update and some of its new features (reports) that can be very helpful to you.
Export Defects – This will export files (both .csv and .kml files) of user-defined defects only. This allows the user to have data of defects only and not have to scroll/filter/view/and whatever else you do through tons of data to find and process the defects
PWL Reports – This will export files for PWL information. Valid values are user-entered into the system, and reports are exports to show PWL information.

## Slide 37: Density Assessment – Defect Detection
Typical analysis file by file
  Example with 2 sensors straddling the joint 0.75 ft. away and 2.25 ft from joint
  Good information just tough to navigate while on-site

## Slide 38: Density Assessment – Defect Detection
Geospatial view

## Slide 39: Density Assessment – “PWL” (Actually Percent Conformance)
Ability to define mat and joint acceptable density levels (min and max) and calculate percent conformance in user defined segments.
  MnDOT has been using other post processing tools like matlab and more recently VETA to make these types of calculations
  This is a simpler tool that can be run on-site and doesn’t require outside expertise (will show simple excel template to visualize it).

## Slide 40: Density Assessment – “PWL” (Actually Percent Conformance)
Joint/Mat % conforming
Project Information:
Ex: 052221 TH21-HMA-L1-12L-CL
Lane Extents

## Slide 41: Density Assessment – “PWL” (Actually Percent Conformance)
Example Data Organization/Analysis
using simple excel templates: TH21

## Slide 42: Thank you again!
Kyle Hoegh
kyle.hoegh@state.mn.us
507-398-2669

## Slide 43: Geospatial Filtering
Further Analysis needs
  Filter geospatially by offset?