## Slide 1: TPF-5 (443) Dps user group meeting November 10, 2021
Notes: Welcome and intro

## Slide 2: 2021 Ohio DOT DPS updates
Craig E. Landefeld, P.E.
ODOT Office of Pavement Engineering

## Slide 3: 2021 – 1 step forward - 2 steps back
COVID Issues
Staffing Issues
Contractor Issues

## Slide 4: 2021 Collection Procedures
Air/Metal Calibration Daily
AM/PM Line Test
Swerve collection pattern
Acceptance Core Collection
Lab Gyratory Samples
Long Joint Collection
  Single
  Straddle

## Slide 5: COS-US36 Project details
7mi. Rural 4–Lane Divided
1.5in -12.5mm Int.
1.5in -12.5mm Surface
Hot joint on shoulders
Cold joint at lane line
447 Joint Density Spec
Contractor Gyratories???

## Slide 6: Repeat Line Tests
Chart: COS-36 Line Test Data
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11
Machine 1 | -0.05 | 0.04 | 0.08 | 0.04 | 0.02 | 0.03 | 0.03 | 0.05 | 0 | 0.08 | 0.07 | -0.03 | -0.01 | 0.07 | 0.07 | 0.1 | 0.04 | -0.06 | 0.04 | 0 | 0.02 | 0.01 | 0.07 | 0.11 | 0.09 | 0.13 | 0.07 | -0.01 | 0.04 | 0.08
Machine 2 | 0.05 | -0.01 | 0 | 0.01 | 0.07 | 0.11 | 0.13 | -0.25 | 0.05 | 0.02 | -0.19 | 0.04 | -0.02 | 0.01 | -0.05 | -0.05 | -0.08 | -0.16 | -0.03 | -0.05 | -0.14 | 0.03 | -0.02 | 0.02 | 0.02 | 0.06 | 0.05 | -0.41 | 0.02 | -0.03
Upper Limit | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08
Lower Limit | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08
Notes: The tolerance we discussed in the past was 0.08. I think the default on the RDM may be 0.1

## Slide 7: COS-36 Core Calibrations
Chart: COS-36 Machine 1 Time
| 5.641 | 5.65 | 5.5960000000000001 | 5.5990000000000002 | 5.7039999999999997 | 5.7009999999999996 | 5.64 | 5.6390000000000002 | 5.6740000000000004 | 5.6689999999999996 | 5.6630000000000003 | 5.6639999999999997 | 5.7119999999999997 | 5.7089999999999996 | 5.657 | 5.6580000000000004 | 5.5919999999999996 | 5.593 | 5.4619999999999997 | 5.649 | 5.4889999999999999 | 5.5830000000000002 | 5.4210000000000003 | 5.7590000000000003 | 5.4829999999999997 | 5.6950000000000003 | 5.6230000000000002
Machine 1 Time | 94.3 | 94.3 | 94.3 | 94.3 | 95.4 | 95.4 | 94.4 | 94.4 | 95.5 | 95.5 | 94.4 | 94.4 | 95.2 | 95.2 | 93.5 | 93.5 | 93 | 93 | 94 | 95.1 | 95 | 93.3 | 93.3 | 95.1 | 94.4 | 95.7 | 93.7
Chart: COS-36 Machine 2 Time
| 5.556 | 5.774 | 5.6840000000000002 | 5.6909999999999998 | 5.5890000000000004 | 5.5140000000000002 | 5.6310000000000002 | 5.4930000000000003 | 5.593 | 5.6159999999999997 | 5.742 | 5.7190000000000003 | 5.4690000000000003 | 5.649 | 5.6509999999999998 | 5.4349999999999996 | 5.7930000000000001 | 5.6740000000000004 | 5.6630000000000003 | 5.6159999999999997 | 5.6139999999999999 | 5.5519999999999996 | 5.62 | 5.577 | 5.548 | 5.5439999999999996 | 5.5860000000000003 | 5.0209999999999999 | 5.7610000000000001 | 5.56 | 5.7009999999999996 | 5.6719999999999997 | 5.5149999999999997 | 5.6849999999999996 | 5.59 | 5.7270000000000003 | 5.4980000000000002 | 5.4080000000000004 | 5.766 | 5.5030000000000001 | 5.6760000000000002 | 5.5460000000000003
Machine 2 Time | 95.3 | 96.8 | 95.4 | 95.3 | 95.2 | 94 | 95.1 | 93.1 | 93.3 | 94.1 | 95.2 | 95.7 | 93.2 | 96.7 | 95.4 | 92.8 | 96 | 95.3 | 95.3 | 94.8 | 94.1 | 95.5 | 95.2 | 95.2 | 93.5 | 93 | 94.5 | 94.5 | 96 | 94 | 95.2 | 95.1 | 95.4 | 95.7 | 95 | 94.7 | 93.3 | 93.3 | 95.1 | 94.4 | 95.7 | 93.7

## Slide 8: COS-36 Core Calibrations
Chart: COS-36 Machine 1 Distance
Chart: COS-36 Machine 2 Distance
| 5.6989999999999998 | 5.5810000000000004 | 5.5789999999999997 | 5.4710000000000001 | 5.7149999999999999 | 5.5860000000000003 | 5.5519999999999996 | 5.57 | 5.6310000000000002 | 5.516 | 5.6890000000000001
Machine 2 Distance | 94.9 | 94.3 | 94.3 | 94.4 | 95.5 | 95.2 | 95.2 | 93.5 | 93 | 95.4 | 95.7

## Slide 9: COS-36 Longitudinal joint scans
Chart: Average Dielectric on Longitudinal Joint Straddle Sensors
| 180 - 188 | 192 - 200 | 216 - 224 | 278 - 288 | 288 - 298
M1 203 | 5.9847 | 5.8024 | 5.7244 | 5.6496 | 5.574
M1 209 | 5.6835 | 5.6349 | 5.6203 | 5.4937 | 5.5835
M2 182 | 5.5913 | 5.5557 | 5.5354 | 5.4741 | 5.4806
M2 183 | 5.6347 | 5.6596 | 5.628 | 5.4464 | 5.4456
Chart: Average Dielectric on Longitudinal Joint Single vs Straddle vs Joint Core
| 180 - 188 | 192 - 200 | 216 - 224 | 278 - 288
M1 Single | 5.347 | 5.3453 | 5.3423 | 5.4217
M2 Single | 5.2241 | 5.3783 | 5.4615 | 5.4037
M1 Straddle | 5.8341 | 5.7187 | 5.6724 | 5.5716
M2 Straddle | 5.613 | 5.6077 | 5.5837 | 5.4602
M1 Joint Core | 5.5705 | 5.8575
M2 Joint Core | 5.59 | 5.818
Notes: - Two different runs on the joint
  - Single sensor on the joint
  - Straddling the joint with two sensors
    - Took average of two sensors for comparison on left

## Slide 10: FAI-664 project details
5mi. Rural 2-lane
1.0in
1.25in. Surface Course
Control Section
  Type 1 Surface, PG 70-22M, 20% RAP
High RAP
  Balanced Mix Design
  Type 1 Surface, PG 70-22 w. recycling agent, 55-60% RAP
Notes: The control section is planned to start production tomorrow morning around 10 AM (they still need to finish some intermediate mix). This mix is a Type 1 Surface with PG 70-22M with 20% RAP being produced out of the Shelly Co.’s Lancaster plant. Should be the northbound lane.
The high RAP/Balanced Mix Design mix is planned to start Friday, weather permitting, and end Saturday. This mix is also a Type 1 Surface but the final grade is to grade out as a PG 70-22 and include a recycling agent. The mix will have 55-60% RAP in it. There is a minimum of a 120 CT Index and a max of 12.5 mm on the Hamburg after 10,000 cycles (see attached plans, sheet 5 for more info).

## Slide 11: Repeat Line Tests
Chart: FAI-664 Line Test Data
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 1 | 2 | 3 | 4 | 5 | 6 | 7
Machine 1 | 0.048 | 0.137 | -0.043 | -0.001 | 0.005 | 0.136
Machine 2 | -0.087 | -0.036 | 0.007 | 0.018 | 0.17 | -0.061 | 0.008 | -0.015 | -0.004 | -0.069 | -0.097 | -0.262 | 0.066 | -0.092 | -0.102 | -0.04 | -0.062 | -0.079 | -0.092 | 0.005 | -0.084
Upper Limit | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08 | 0.08
Lower Limit | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08 | -0.08
Notes: The tolerance we discussed in the past was 0.08. I think the default on the RDM may be 0.1

## Slide 12: FAI-664 Core Calibrations Control section
Chart: Dielectric
| 4.7160000000000002 | 5.05 | 5.1589999999999998 | 4.7830000000000004 | 4.9349999999999996 | 5.3330000000000002 | 5.1689999999999996 | 5.0880000000000001 | 4.7990000000000004 | 5.319 | 5.4139999999999997 | 5.1669999999999998 | 5.3449999999999998 | 5.2249999999999996
Control Time | 92.7731 | 93.192 | 93.6101 | 94.0017 | 94.2383 | 95.0479 | 95.267 | 94.1082 | 91.8051 | 95.96 | 96.5015 | 94.8771 | 96.793 | 96.1266
Chart: Density (%)
| 0.91 | 0.92 | 0.93 | 0.94 | 0.95 | 0.96 | 0.97 | 0.98
 | 0.00050283 | 0.006023 | 0.072943 | 0.3319 | 0.42918 | 0.14817 | 0.010745 | 0.00033886
 | 0.00054656 | 0.0065696 | 0.079513 | 0.41141 | 0.84059 | 0.98876 | 0.99951 | 0.99985
Notes: The calibration curve was taken in TIME mode
Used Unit 2 for these next two slides as that was the unit that was operated for both mixes

## Slide 13: FAI-664 Core Calibrations high rap section
Chart: Dielectric
| 5.4779999999999998 | 5.8840000000000003 | 5.508 | 5.1749999999999998 | 6.0449999999999999 | 5.6820000000000004 | 5.399 | 5.2160000000000002 | 5.9909999999999997 | 6.1289999999999996 | 6.0090000000000003 | 5.9630000000000001 | 5.9359999999999999 | 5.9470000000000001 | 5.8970000000000002
HR Time | 91.0722 | 94.8438 | 90.5727 | 86.8706 | 96.2034 | 94.4206 | 89.3511 | 89.9718 | 93.8785 | 95.4947 | 95.3004 | 95.423 | 94.3196 | 95.3004 | 92.5215
Chart: Density
| 0.87 | 0.88 | 0.89 | 0.9 | 0.91 | 0.92 | 0.93 | 0.94 | 0.95 | 0.96 | 0.97 | 0.98
 | 0.0037436 | 0.014922 | 0.041754 | 0.10656 | 0.19009 | 0.22724 | 0.19562 | 0.13134 | 0.064581 | 0.017725 | 0.0036043 | 0.00076612
 | 0.0054847 | 0.020407 | 0.06216 | 0.16872 | 0.35881 | 0.58605 | 0.78167 | 0.91301 | 0.97759 | 0.99532 | 0.99892 | 0.99969
Notes: The calibration curve was taken in TIME mode
Notice the scales on the frequency graph, the high rap is more variable (standard dev of control was about 0.12, high rap about 0.21)

## Slide 14: Machine Comparisons
Chart: 2020 MAD-70 Dielectrics
| 5.3660470493211303 | 5.455563553905117 | 5.5450800584891038 | 5.6345965630730905 | 5.7241130676570773 | 5.813629572241064 | 5.9031460768250508 | 5.9926625814090375 | 6.0821790859930243 | 6.171695590577011 | 6.2612120951609977 | 6.3507285997449845 | 6.4402451043289712 | 6.529761608912958 | 6.6192781134969447 | 6.7087946180809315 | 6.7983111226649182 | 6.887827627248905 | 6.9773441318328917 | 7.0668606364168784 | 7.1563771410008652
1 | 0.014853 | 0.034924 | 0.075052 | 0.1474 | 0.26459 | 0.43406 | 0.65078 | 0.89174 | 1.1167 | 1.2782 | 1.337 | 1.2782 | 1.1167 | 0.89174 | 0.65078 | 0.43406 | 0.26459 | 0.1474 | 0.075052 | 0.034924 | 0.014853
2 | 0.014804 | 0.034809 | 0.074804 | 0.14692 | 0.26372 | 0.43263 | 0.64864 | 0.8888 | 1.1131 | 1.2739 | 1.3326 | 1.2739 | 1.1131 | 0.8888 | 0.64864 | 0.43263 | 0.26372 | 0.14692 | 0.074804 | 0.034809 | 0.014804
Chart: 2021 COS-36 Dielectrics
| 4.6185313402580697 | 4.6925202730867852 | 4.7665092059155008 | 4.8404981387442163 | 4.9144870715729319 | 4.9884760044016474 | 5.0624649372303629 | 5.1364538700590785 | 5.210442802887794 | 5.2844317357165096 | 5.3584206685452251 | 5.4324096013739407 | 5.5063985342026562 | 5.5803874670313718 | 5.6543763998600873 | 5.7283653326888029 | 5.8023542655175184 | 5.876343198346234 | 5.9503321311749495 | 6.0243210640036651 | 6.0983099968323806
1 | 0.01797 | 0.042253 | 0.090802 | 0.17834 | 0.32012 | 0.52515 | 0.78736 | 1.0789 | 1.3511 | 1.5464 | 1.6176 | 1.5464 | 1.3511 | 1.0789 | 0.78736 | 0.52515 | 0.32012 | 0.17834 | 0.090802 | 0.042253 | 0.01797
2 | 0.017503 | 0.041157 | 0.088445 | 0.17371 | 0.31181 | 0.51152 | 0.76692 | 1.0509 | 1.316 | 1.5063 | 1.5756 | 1.5063 | 1.316 | 1.0509 | 0.76692 | 0.51152 | 0.31181 | 0.17371 | 0.088445 | 0.041157 | 0.017503
COS-36 | M1 | M2
Mean | 5.36 | 5.33
Std Dev | 0.247 | 0.253
MAD-70 | M1 | M2
Mean | 6.26 | 6.11
Std Dev | 0.298 | 0.299
FAI-664 | M1 | M2
Mean | 5.05 | 5.03
Std Dev | 0.121 | 0.124
Chart: 2021 FAI-664 Dielectrics
| 4.6818838061467138 | 4.7181898213123965 | 4.7544958364780792 | 4.7908018516437618 | 4.8271078668094445 | 4.8634138819751271 | 4.8997198971408098 | 4.9360259123064925 | 4.9723319274721751 | 5.0086379426378578 | 5.0449439578035404 | 5.0812499729692231 | 5.1175559881349058 | 5.1538620033005884 | 5.1901680184662711 | 5.2264740336319537 | 5.2627800487976364 | 5.299086063963319 | 5.3353920791290017 | 5.3716980942946844 | 5.408004109460367
1 | 0.036621 | 0.086109 | 0.18505 | 0.36344 | 0.65237 | 1.0702 | 1.6046 | 2.1987 | 2.7535 | 3.1514 | 3.2965 | 3.1514 | 2.7535 | 2.1987 | 1.6046 | 1.0702 | 0.65237 | 0.36344 | 0.18505 | 0.086109 | 0.036621
2 | 0.035874 | 0.084354 | 0.18128 | 0.35603 | 0.63908 | 1.0484 | 1.5719 | 2.1539 | 2.6974 | 3.0872 | 3.2293 | 3.0872 | 2.6974 | 2.1539 | 1.5719 | 1.0484 | 0.63908 | 0.35603 | 0.18128 | 0.084354 | 0.035874
Notes: Now the question becomes what are good comparison methods??

## Slide 15: Things to consider???
Causes of sensor variability?
Causes of poor core calibrations?
How do we define “comparison”
Is the effect of joint enrichment an issue?
Could we use this as a tool to assess Void Reducing Asphalt Membrane (VRAM)?
Notes: Copy from April presentation

## Slide 16: What’s next ???
Machine Comparisons
– Precision & Bias
- QC/QA Procedure & Comparison Tolerances
2. Gyratory Procedures
    - Work with Producers
3. Collection Procedures (Swerve? Long. Joints?)
    - Swerve / Linear
    - Longitudinal Joints
4. VETA Analysis
    - 2022 Projects
5. Specs for Pilot/Shadow Projects
Notes: Copy from April presentation

## Slide 17: Questions
?
Last updated 12/9/2021