## Slide 1
Barry Paye, PE
Chief Materials & Pavement Engineer
Wisconsin DOT
WisDOT Cold In-Place Recycling Pavement Rehabilitation

## Slide 2
Introduction to Cold In-Place Recycling (CIR)
Types of CIR Equipment
Benefit of CIR
Pavement distresses addressed by CIR
Overview of WisDOT CIR Projects
CIR Projects Short Term Performance Data
Public Relations
Presentation Outline

## Slide 3
CIR uses mechanical process to produce RAP from the existing pavement, add a stabilizing agent, relay & compact into a stabilized base.
Typical CIR process treatment depth - 3 to 4”
Cold In-Place Recycling (CIR)

## Slide 4
Multi – Unit CIR Train
Types of CIR Equipment
Milling
Crushing/Sizing
Pug mill
AC Tank
Pick Up Machine/Paver
Working Direction

## Slide 5
Types of CIR Equipment
Single-Unit CIR Train
Cutting chamber
AC Tank
Water

## Slide 6: Benefit of CIR
Cost Savings
  Potential cost savings compared to equivalent
  mill/overlay rehabilitation methods.
Engineering
  Addresses actual distress rather than symptoms.
  Cracks eliminated/reduced – CIR act as crack relief layer.

## Slide 7: Benefit of CIR
Construction Time
  CIR layer can be opened to traffic within a couple of
  hours.
  Minimal Traffic disruption and user delay.
Environmental Benefit
  Using in-place materials minimizes hauling cost & use
  of virgin material.
Notes: .

## Slide 8
Ruts < ½ in 
> ½ in ?1
Crack Fatigue ?1
Longitudinal 
Transverse 
Reflective 
Block 
Potholes (surface only) 
Poor Ride 
Poor Drainage no
Structural Deficiency ?2
Base/subgrade Failure no
Questions?
Provided not base, subbase or subgrade related.
In conjunction with
Overlay to increase
structural capacity
Distresses addressed by CIR
Pavement Distresses addressed by CIR

## Slide 9: CIR Projects Map (Since 2012)
Construction Year | Project Length (Lane-Mile)
2012 | 26
2014 | 24
2015 | 50
2016 | 58
Total | 158

## Slide 10: STH 27(Sparta – Black River Falls)
CIR Construction – 2016
Design AADT 11,000, 15.2% Truck
ESALs 20 years – 1,598,700
4” CIR Layer + 2.5” HMA Overlay
Project Length = 8.402 miles

## Slide 11: STH 27 - Placing/Compaction
CIR
Non-CIR
Finished CIR Layer

## Slide 12: STH 48 (Grantsburg – Frederic)
Pavement History – Before CIR
Last Resurfaced 3”- 4” inch 1994
Various Maintenance activities
CIR Construction – 2012
      Design AADT 1,100, 5.2% Truck
      ESALs-20 years – 131,400
4” CIR + 2” HMA Overlay
Project Length = 12.56 Miles

## Slide 13: STH 48 (Grantsburg – Frederic)
After 3 Years
After construction

## Slide 14: STH 48 (Grantsburg – Frederic) Performance Data Four years in service
Chart: Survey Location (mile)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
2015 | 24.18 | 281.72 | 85.39 | 0 | 541.77 | 47.01 | 17.52 | 12.4 | 0 | 0 | 0 | 0
2016 | 0 | 388.13 | 84.3 | 0 | 544.03 | 47.31 | 17.77 | 10.29 | 0 | 0 | 0 | 0
CIR
Non-CIR
CIR
Chart: Survey Location (mile)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
2015 | 22.93 | 21.71 | 67.58 | 12.53 | 302.42 | 5.07 | 7.61 | 0 | 7.94 | 88.03 | 115.32 | 0
2016 | 21.96 | 21.79 | 82.04 | 11.19 | 271.21 | 14.39 | 7.06 | 0 | 0 | 85.33 | 92.86 | 0
Transverse Cracking
CIR
Non-CIR
CIR
Longitudinal Cracking
Chart: Survey Location (mile)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
2015 | 63.175 | 73.275 | 64.55 | 65.225 | 61.4 | 73.325 | 74.825 | 67.275 | 72.85 | 76.25 | 78.85 | 61.55
2016 | 63.275 | 75.075 | 70.725 | 64.8 | 65.675 | 72.275 | 75.275 | 66.375 | 72.6 | 73.725 | 78.175 | 60.7
Roughness
CIR
Non-CIR
CIR
Chart: Survey Location (mile)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
2015 | 0.098687 | 0.099933 | 0.083975 | 0.073543 | 0.071843 | 0.0717 | 0.068763 | 0.080067 | 0.080288 | 0.08307 | 0.06947 | 0.092993
2016 | 0.09266 | 0.094692 | 0.068797 | 0.059685 | 0.08738 | 0.081295 | 0.071265 | 0.067268 | 0.074205 | 0.077308 | 0.07584 | 0.10151
CIR
Non-CIR
CIR

## Slide 15: STH 64 (Gilman-Medford)
CIR Construction – 2014
Design AADT 10,800, 17.5% Truck
ESALs = 1,708,200
4” CIR + 2” HMA Overlay
Initial Project Plan 13.3 miles (appr. 30% CIR
completed)

## Slide 16
STH 64 (Gilman - Medford )
Before CIR
Finished CIR Layer
CIR – Both Lanes
EB Lane CIR
WB Lane Mill&Overlay
EB Lane CIR
WB Lane Mill&Overlay
Mill & Overlay – Both Lanes
CIR Operation
2016
2016
2016
2016

## Slide 17: STH 64 (Gilman – Medford) Performance Data two year in service
Chart: Average Rut Depth
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13
2015 | 0.060952 | 0.062957 | 0.070335 | 0.063512 | 0.075695 | 0.054087 | 0.056953 | 0.055718 | 0.057758 | 0.06276 | 0.057875 | 0.06371 | 0.057855
2016 | 0.065905 | 0.072645 | 0.071468 | 0.07218 | 0.076677 | 0.05712 | 0.060452 | 0.052903 | 0.061517 | 0.063218 | 0.061595 | 0.06846 | 0.057605
Chart: Survey Location (mile)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13
2015 | 63.38 | 70.79 | 12.34 | 0 | 127.47 | 42.39 | 0 | 0 | 0 | 0 | 11.3243 | 0 | 0
2016 | 76.9 | 64.19 | 19.68 | 9.84 | 256.73 | 95.04 | 6.86 | 22.2 | 0 | 0 | 0 | 0 | 0
Transverse Cracking
CIR
Non-CIR
CIR
Non-CIR
Roughness
Chart: Survey Location (mile)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13
2015 | 35.025 | 36.275 | 32.225 | 36.7 | 40.7 | 39.825 | 33.125 | 31.825 | 47.675 | 40.825 | 34.975 | 38.175 | 30.45
2016 | 36.725 | 38.8 | 33.275 | 37.225 | 45.225 | 45.75 | 39.35 | 35.825 | 50.575 | 42.4 | 36.725 | 41.8 | 32.65
Non-CIR
CIR

## Slide 18: Summary of CIR Projects IRI and Rut Depth Values
Chart: Average IRI Value (inch/mile) 2016 Survey
| STH 95 (Const_2015) | CTH H (Const_2015) | STH 48 (Const_2015) | STH 64 (Const_2014) | STH 48 (Const_2012)
 | 40.2875 | 36.9104 | 49.1313 | 40.83 | 69.8896
Chart: Average Rut Depth (inches) 2016 Survey
| STH 95 (Const_2015) | CTH H (Const_2015) | STH 48 (Const_2015) | STH 64 (Const_2014) | STH 48 (Const_2012)
 | 0.056943 | 0.061825 | 0.066501 | 0.062479 | 0.079326

## Slide 19: Design Criteria & Considerations
Distressed Layer & Distress Types
Traffic Volume
Historical Information
Geometric Considerations
Roadway, Subgrade & Drainage
Layer Coefficient - 0.30-0.35
Mix Design Considerations
Curing Time

## Slide 20: WisDOT Experience
17% Let savings vs 4” mill & overlay
10x reduction in cracking compared to mill & overlay
Minimal disturbance to traveling public

## Slide 21: Public Benefits

## Slide 22: Public Benefits

## Slide 23: Public Benefits

## Slide 24: Questions/Contact
Barry Paye, PE
Materials Management Section
Phone: 608-246-7945
Email: Barry.paye@dot.wi.gov