## Slide 1: INTELLIGENT COMPACTION NRRA Conference May 23-24, 2017
Presenter: Joseph Holland (Caltrans Research)
Prepared by: Ebi Fini, P.E (Caltrans Contruction)

## Slide 2: Caltrans Asphalt Concrete Specification Section 39 Standard Specification
HMA construction:
Method Compaction- Compaction of hot mix asphalt with thickness <0.15’ (46 mm). Density is not measured.
Density Requirement - Compaction of hot mix asphalt with thickness ≥0.15’ (46 mm). Density is measured.
.

## Slide 3: Section 39-2.01C(15)(b) Method Compaction
39-2.01C(15)(b) Method Compaction
Use method compaction for any of the following conditions:
1. HMA pavement thickness shown is less than 0.15 foot
2. Replace asphalt concrete surfacing
3. Leveling courses
4. Areas the Engineer determines conventional compaction and compaction measurement methods are impeded
HMA compaction coverage is the number of passes needed to cover the paving width. A pass is 1 roller's movement parallel to the paving in either direction. Overlapping passes are part of the coverage being made and are not a subsequent coverage. Do not start a coverage until completing the prior coverage.
Method compaction must consist of performing:
1. Breakdown compaction of each layer with 3 coverages using a vibratory roller. The speed of the vibratory roller in miles per hour must not exceed the vibrations per minute divided by 1,000. If the HMA layer thickness is less than 0.08 foot, turn the vibrator off.
2. Intermediate compaction of each layer of HMA with 3 coverages using a pneumatic-tired roller* at a speed not to exceed 5 mph.
Finish compaction of HMA with 1 coverage using a steel-tired roller.
* RHMA use steel roller for intermediate compaction.

## Slide 4
Hot Mix Asphalt Intelligent Compaction Target Values Method Compaction |  |  | 
IC Requirements | HMA Type A Unmodified Asphalt Binder | HMA Type A PG-M Asphalt Binder | RHMA-G
Breakdown Compaction Minimum Surface Temperature °F 1st PASS | 250 | 240 | 285
Compaction Number of Breakdown passes | 3 | 3 | 3
Intermediate Compaction Minimum Surface Temperature °F Last Pass | 190 | 180 | 250
Intermediate Compaction Number of Passes | 3 | 3 | 3
Hot Mix Asphalt Open Graded Friction Course (OGFC) Intelligent Compaction Target Values Method Compaction |  |  | 
IC Requirements | OGFC Unmodified Asphalt Binder | OGFC PG-M Asphalt Binder | OGFC RHMA-O RHMA-HB
Breakdown Compaction Minimum Surface Temperature °F 1st PASS | 240 | 240 | 280
Complete Compaction Minimum Surface Temperature °F Last Pass | 200 | 180 | 250
Minimum Number of Passes | 2 | 2 | 2
Section 39 of CT Standard Specifications

## Slide 5
Warm Mix Asphalt Intelligent Compaction Target Values Method Compaction |  |  | 
IC Requirements | HMA Type A Unmodified Asphalt Binder | HMA Type A PG-M Asphalt Binder | RHMA-G
Breakdown Compaction Minimum Surface Temperature °F 1st PASS | 240 | 230 | 260
Breakdown Compaction Number of Passes | 3 | 3 | 3
Intermediate Compaction Minimum Surface Temperature °F Last Pass | 190 | 170 | 230
Intermediate Compaction Number of Passes | 3 | 3 | 3
Warm Mix Asphalt Open Graded Friction Course (OGFC) Intelligent Compaction Target Values Method Compaction |  |  | 
IC Requirements | OGFC Unmodified Asphalt Binder | OGFC PG-M Asphalt Binder | OGFC RHMA-O RHMA-HB
Breakdown Compaction Minimum Surface Temperature °F 1st PASS | 230 | 230 | 270
Complete Compaction Minimum Surface Temperature °F Last Pass | 190 | 170 | 240
Minimum Number of Passes | 2 | 2 | 2
Section 39 of CT Standard Specifications

## Slide 7: Premature Pavement Failure
Courtesy of Mark Woolaver, VAOT
Chart: 
| Material Failure | Workmanship
 | 21 | 79

## Slide 8: Why Intelligent Compaction (IC)?
Shortcomings in Conventional Compaction
Limited
Feedback
Over-
Compaction
Under-
Compaction
Leads to
Distresses

## Slide 9: Why Intelligent Compaction?
Shortcomings in Conventional Acceptance
Limited Number
of Locations
After Compaction
is Complete

## Slide 10
100 % Coverage
1 / 1,000,000
Courtesy of Caterpillar
(IC)

## Slide 11: Instrumented Rolling Train
HMA Rolling Train
Courtesy of Rebecca Embacher, MnDOT
Stabilized / Un-stabilized Full Depth Reclamation (FDR)

## Slide 12: IC Retrofit
Printer
Control Box
GNSS Receiver
Temperature
Sensor
Temperature
Sensor
Courtesy of Trimble
Accelerometer

## Slide 13: An Example IC System
Accelerometer
GPS Receiver
HCQ GPS Navigator
Temperature Sensors
Control Panel

## Slide 15: IC Data Flow
IC data
Point Tests and GPS data
Vendor’s software

## Slide 16: Veta Software
Developed by FHWA
Veta is a map-based tool for viewing and analyzing geospatial data.
Used to generate various IC reports

## Slide 17: Many Systems …One Software

## Slide 18: Why Using Veta
Critical for standardization
Included in Specs
  Caltrans
  AASHTO
  FHWA
  many States IC specs
Public domain -- Free

## Slide 19: Veta Software

## Slide 20: Benefits of IC
Reliable monitoring of compaction activities
    No. of Passes
    Coverage
    Temperature
    Stiffness
Improve compaction… better performance
Improve efficiency… cost savings
Increase information… better QC/QA
Consistency & Uniformity

## Slide 21: Implementation of Intelligent Compaction in California

## Slide 22: CALTRANS INTELLIGENT COMPACTION
Used as part of Contractor QC program
Not used as Acceptance
Used in Pilot Projects at this time
Cost of IC is about 3% to 5% of the bid item

## Slide 23: Caltrans IC Specs
Cold In Place Recycling
HMA

## Slide 24: IC Specs Administration
Contractor is responsible for data collection, analysis, report preparation, and data upload
  14 Construction forms
  3 IC CIR construction reports
    Mapping existing pavement
    Test Strip
    Compaction Quality Control report
  2 IC HMA construction reports
    Test Strip HMA≥0.15’
    Compaction Quality Control report
  Information (Data) submittals
    Data uploading to DOT servers

## Slide 25: CT IC Target Values
Intelligent Compaction Target Value: Compaction target values established at test strip (>0.15’) or specified that are used by roller operator to monitor compaction and in data analysis to generate compaction quality control report.
  No. of Passes
  Breakdown Compaction Temperature
  Intermediate Compaction temperature
  Intelligent Compaction Measurement Value (Pseudo Stiffness)

## Slide 26: Case Study

## Slide 27: Section 39- Hot Mix Asphalt
Intelligent Compaction Target Values Method Compaction

## Slide 28: IC Quality Compaction Summary

## Slide 29: Veta Viewer

## Slide 30: Coverage

## Slide 31: Pass Counts

## Slide 32: 1st Pass Breakdown Temp.

## Slide 33: 1st Pass Breakdown Temp.

## Slide 34: Last Pass Intermediate Compaction

## Slide 35: Exploring Possible Density QA with Ground Penetrating Radar (Ken Maser (Infrasense)

## Slide 36
GPR Dielectric Map

## Slide 37: Caltrans Intelligent Compaction Webpage www.dot.ca.gov/hq/construc/IC

## Slide 38: For More Info on IC
http://www.dot.ca.gov/hq/construc/ic/
Ebi.fini@dot.ca.gov
Website
Email
(916) 227-5396
Phone

## Slide 39
Contact Ebi Fini 916-227-5396 ebi.fini@dot.ca.gov
IC@dot.ca.gov