## Slide 1: Integration of Traffic Speed Deflectometer (TSD) and Ground Penetrating Radar (GPR) for Network-Level Roadway Structure Evaluation
by
Ken Maser, Adam Carmichael,
Infrasense, Inc
Pete Schmalzer,
Nichols Consulting Engineers
Bill Shaw,
Idaho Transportation Department
NRRA 2017 Conference
May 24, 2017

## Slide 2: Background
PMS assessments are based on surface distress
  Continuous distress survey systems are available
Remaining life depends on roadway structure
Continuous roadway structure data has been harder to get
  FWD testing requires closures, too much time, limited coverage
TSD and GPR combined can now provide continuous roadway structure data
  ~200 miles per day/no closures

## Slide 3: Objectives of Idaho Pilot Project
Use TSD deflection data with GPR layer thickness data to calculate properties of the roadway structure continuously across the network
  Subgrade Modulus
  Effective Structural Number
  Remaining Life
Offer the data on a geospatial database platform usable to a wide audience
Demonstrate the use of the data at both network and project levels
Notes: Mention level of detail useful at the project level

## Slide 4: Pilot Project Scope – Idaho District 6
735 miles of roadway:
168 miles Interstate
567 miles primary roads

## Slide 5: Data Collection
TSD continuous at 10m intervals
  Provides deflection slope at various offsets from load
FWD at 100 ft. intervals in selected 2-mile regions for calibration/verification
Ground Penetrating Radar (GPR)
  1 GHz Horn Antenna, continuous at 1 foot intervals
Selective coring for layer structure clarification
Notes: Mention GPS and coordination

## Slide 6: Traffic Speed Deflectometer (TSD)

## Slide 7: Ground Penetrating Radar (GPR)
DMI
1 GHz Horn Antenna
1 GHz Horn Antennas
GPS

## Slide 8: GPR Data Analysis
Top of Pavement
Bottom of AC
Bottom of Base
Increasing Milepost
Depth
Bottom of CRABS
8" Diam.
Core

## Slide 9: TSD Data Analysis Procedure
Calculate subgrade modulus (Mr) directly from deflection slope of outer sensors
Compute deflections by integrating deflection slopes
Compute pavement modulus, Ep from deflections and layer thickness
Calculate SNeff from Ep and thickness for each point

## Slide 10: TSD vs. FWD – Maximum Deflection (D0)
Chart: Station (m)

## Slide 11: TSD vs. FWD – Subgrade Modulus (MR)
Chart: Station (m)

## Slide 12: Sample Analysis Result (SNeff)
SNeff
SNeff=3

## Slide 13: Remaining Life and Segmentation
Calculate remaining life at each point
  given SNeff at each test point, compute ESALs
  using traffic projections convert ESALS to life
Segment the pavement based on remaining life
Targeted 1-6 mile segment length, based on typical rehab project length.

## Slide 14: Segmentation and Remaining Life (SH 28)
Chart: Milepost

## Slide 15: Pavement Substructure GeoDatabase
Data is recorded in a series of tables
Data is displayed spatially using ArcGIS
Database is accessible through iPLAN
http://iplan.maps.arcgis.com/apps/webappviewer/index.html?id=36433c5e330e48378bca126af4920549

## Slide 16: Segmented Remaining Life (years) in iPLAN

## Slide 17: Segmented Remaining Life (years)
Notes: Big picture condition of network – basis for priorities and budgeting. Data is available at a level of detail that supports project level decisionmaking

## Slide 18: Example Segment Analysis – SH28
SNeff
Mr
Remaining Life

## Slide 19: Example Segment Analysis – SH28
SNeff
Mr

## Slide 20: Example Segment Analysis – SH28
Mr

## Slide 21: I-15 Southbound Segment Analysis
Remaining Life
SNeff
Mr

## Slide 22: Current Effort – Use of Structure Data in Pavement Management
Incorporate roadway structure parameters into PMS database (TAMS)
Combine structure parameters with surface distress in decision rules
Evaluate changes in resource allocation and rehabilitation plans
Notes: We have now shown how roadway structure can be used to project pavement life and rehab needs on a network level. These were two small corridors, but the approach can be extrapolated, and this is being done in a current project. ----Current effort will lead to what-if scenarios. Does the info make a difference

## Slide 23: Summary
Combination of TSD and GPR has been demonstrated for determining network-level roadway structure data
Process has been applied to 735 miles of roadway
Resulting data is available via a statewide geodatabase
Results demonstrate potential impact on rehab design
Current work will complete remaining 340 miles of roads in the district and will investigate impact of results on pavement management