## Slide 1: Workshop #3 - Unbonded Concrete Overlays
Brett Trautman, P.E.
Construction & Materials Div.
Missouri DOT
NRRA Pavement Conference
Albertville, MN
May 23, 2017

## Slide 2: Overlay Types
Unbonded Concrete Overlays over Concrete Pavement
Unbonded Concrete Overlays over Asphalt Pavement
Bonded Concrete Overlays over Asphalt Pavement (BCOA)
Bonded Concrete Overlays over Concrete Pavement (BCOC)

## Slide 3: Early Beginnings
Missouri unbonded overlays date back to 1930s
21 projects from 1932 to 1970
First project on US 40 in Callaway County circa 1932

## Slide 4: Early Beginnings
Over 12 miles paved on US 40 in Callaway and Montgomery Counties
Projects scattered all over the state

## Slide 5: 1981 Survey
Seven of 21 projects unsurfaced as of 1981
Overlay thickness from 4“ - 6“
Half doweled / half undoweled
Interlayer
Waterbound select material (1“ - 8“)
Cutback
Not sure

## Slide 6: Current PCC Overlay Generation
~ 20 conventional unbonded concrete overlay projects constructed since 1986 (all but 2 since 2000)
Primarily Interstate
Nearly all JPCP
Most ~ 8 inches thick
Placed over PCCP or composite pavement

## Slide 7: Current PCC Overlay Generation
Six ‘big block’ projects since 2006
Six ‘ultrathin’ (BCOA) projects since 1999
All have fibers
Four bonded PCC overlay (BCOC) projects since 1990
No fibers used

## Slide 9: Approximately 5% of Missouri Interstate centerline miles have an unbonded concrete overlay.

## Slide 10: Unbonded Concrete Overlays ‘Conventional’
I-55 in Pemiscot County
I-44 in Greene-Webster Counties
Missouri Experience

## Slide 11: I-55 in Pemiscot County
First new generation
Constructed in 1986
Approximately 7.8 miles in SB lanes
9“ JRCP, 61.5’ joint spacing - Doweled
Milled existing AC overlay
No tied shoulders
Original PCC ~ 8“

## Slide 12: I-55 in Pemiscot County

## Slide 13: I-55 in Pemiscot County
Overall Performance in 2004
  Ave. IRI = 110 (in/mile)
  Ave. Condition = 19.4 (out of 20)
Diamond ground in 2006
  Ave. IRI ~ 75 (in/mile)
Some full depth patching exists

## Slide 14: I-44 in Greene-Webster Counties
First 8“ unbonded JPCP in Missouri
Constructed in 2000
Approximately 5.7 miles in WB lanes
15’ joint spacing - Doweled
Placed 1“ bondbreaker
Tied shoulders
Pavement diamond ground at time of construction

## Slide 15: I-44 in Greene-Webster Counties

## Slide 16: I-44 in Greene-Webster Counties
Ave. IRI after construction diamond grinding = 36.8 (in/mile)
Recent Performance
Ave. IRI = 38 (in/mile)
Ave. Condition = 19.9 (out of 20)
Very few patches
Grooved for skid resistance in 2010

## Slide 17: Lessons Learned

## Slide 18: Concrete Overlay Issues
Unbonded Concrete Overlay design thickness – Increase from 8” to 9” for high volume overlays is warranted

## Slide 21: Thickness vs. % Cracking
Chart: Cracking
Chart: Percent of Slabs Cracked Within QC Lot
| 5.6818181818181865E-2 | 0.10227272727272729 | 2.2727272727272759E-2 | 0 | 2.5000000000000012E-2 | 5.0847457627118703E-2 | 4.5045045045045064E-2 | 0.13513513513513525 | 0 | 2.6923076923076949E-2 | 2.9411764705882353E-2 | 0.20408163265306123 | 0.26881720430107531 | 0 | 9.6491228070175433E-2 | 0.29896907216494878 | 0.21985815602836889 | 0.19753086419753094 | 1.5639374425023E-2 | 0.15315315315315314 | 3.1674208144796406E-2 | 0.23026315789473692
 | 7.89 | 7.95 | 8.372 | 7.8 | 8.028 | 8.322 | 8.196 | 8.1 | 8.282 | 8.322 | 7.814 | 7.8825 | 7.9 | 8.24 | 7.88 | 7.54 | 7.86 | 7.54 | 8.02 | 7.8

## Slide 22: Concrete Overlay Issues
Unbonded Concrete Overlay Interlayer – Stick with geotextile

## Slide 25: Concrete Overlay Issues
Widened slabs – Probably not a good idea

## Slide 26
2’ widening

## Slide 27: What experience have you had?

## Slide 28: Unbonded Concrete Overlays ‘Big Block’
Route D in Cass County
- South of Kansas City
2) US 61 in Jefferson County
Missouri Experience

## Slide 29: Route D in Cass County
9300 AADT (5 % trucks)
8-in PCC, 30-ft joints w/ 1-in dowels
Only 22 years old
  Severely deteriorated by D-cracking
  Estimated 25% of area required full depth repair prior to conventional HMA overlay

## Slide 30: Route D in Cass County
5-inch minimum thickness
6-foot square panels
No steel
No fibers
Interlayer/Separation Layer Option
  Bituminous Layer
  Geotextile Fabric (selected – first in country - 2008)

## Slide 31
Existing Pavement Condition

## Slide 32
Pre-overlay repairs
Consist of bituminous, cementitious, or other materials meeting approval.

## Slide 33
Fabric Placement

## Slide 34
Securing Fabric

## Slide 35
Placing and Finishing Surface

## Slide 36: November 2015 Survey
First thorough visual distress survey
9768 panels total (3.47 centerline miles)
69 panels cracked or spalled for 0.7% failure rate
Most failures located near northern transition (@ Rte 150)

## Slide 37: Route D in Cass County
November 2015

## Slide 38: US 61 in Jefferson County
Composite pavement section south of St. Louis required rehab.
Originally scoped for 3 ¾ HMA overlay, but changed to 5-inch UBOL or ‘big block’
Constructed in 2009
6.5’ by 6.5’ joint spacing

## Slide 39: US 61 ‘Big Block’
Primarily placed directly on existing composite pavement
Inlays constructed at transition areas near bridges and RR approaches and along side wide, new concrete entrances
220+ entrances in 12.7 miles!!!!

## Slide 41
Utilized Longitudinal Joint Device Forming

## Slide 42
Joint Formation

## Slide 43: February 2016 Survey
First visual distress survey
31,840 panels total (~ 10 centerline miles)
333 panels cracked, spalled or patched for 1.06% failure rate
2/3 of failures located in northernmost mile

## Slide 44
Chart: No. of Distressed Panels on US 61
| 1 | 201 | 401 | 601 | 801 | 1001 | 1201 | 1401 | 1601 | 1801 | 2001 | 2201 | 2401 | 2601 | 2801 | 3001 | 3201 | 3401 | 3601 | 3801 | 4001 | 4201 | 4401 | 4601 | 4801 | 5001 | 5201 | 5401 | 5601 | 5801 | 6001 | 6201 | 6401 | 6601 | 6801 | 7001 | 7201 | 7401 | 7601 | 7801
# of Distressed Panels | 46 | 0 | 0 | 137 | 29 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 10 | 9 | 0 | 0 | 2 | 0 | 0 | 37 | 0 | 0 | 6 | 0 | 0 | 0 | 0 | 0 | 0 | 6 | 2 | 0 | 2 | 47 | 0

## Slide 45: US 61 in Jefferson County
February 2016

## Slide 46: US 61 in Jefferson County
February 2016

## Slide 47: US 61 in Jefferson County
February 2016

## Slide 48: What experience have you had?

## Slide 49: Thank You!!
Brett.Trautman@modot.mo.gov
573-751-1036