## Slide 1: Longitudinal Joint Seal Development & Implementation
NRRA Pavement Conference
Jim Trepanier
Aggregate, HMA & Metals Unit Chief
Illinois Dept. of Transportation

## Slide 2: HMA Quiz
What is the leading HMA distress driving pavement rehabilitation in Illinois?
  Loss of Friction
  Wheel Path Rutting
  Raveling
  Premature Cracking
  Raveling & Cracking at the Centerline Joint

## Slide 3: Deteriorated Joint

## Slide 14: Answer
What is the leading HMA distress driving pavement rehabilitation?
  Loss of Friction
  Wheel Path Rutting
  Raveling
  Premature Cracking
  Raveling & Cracking at the Centerline Joint

## Slide 15: Why the Poor Performance?

## Slide 16: Effect of In-Place Voids on Life Washington State DOT Study
Chart: In-situ Air Voids, %
| 7 | 8 | 9 | 10 | 11
Remaining Service Life, Years | 100 | 98 | 94 | 83 | 64
93% 92% 91% 90% 89%
Compaction Level
Notes: This Washington study is often referenced. It highlights the relationship between in-place pavement air voids and pavement service life.
With longitudinal joint densities typically at 90% or less it is easy to explain those opening photos of premature joint failures. At ninety percent compaction (10-percent air voids) we can expect joint performance to be: joint performance = mat performance – 1/5.
When joint density drops to 89% then joint performance can expect to be: joint performance = mat performance – 1/3. For a 15 year expected mat performance, giving up 1/5th means the joints fail 3 yrs earlier than mat (giving up 1/3rd means the joints fail 5 yrs earlier).

## Slide 17: Effect of In-Place Voids on Life Washington State DOT Study
Chart: In-situ Air Voids, %
| 7 | 8 | 9 | 10 | 11
Remaining Service Life, Years | 100 | 98 | 94 | 83 | 64
93% 92% 91% 90% 89%
Compaction Level
Notes: This Washington study is often referenced. It highlights the relationship between in-place pavement air voids and pavement service life.
With longitudinal joint densities typically at 90% or less it is easy to explain those opening photos of premature joint failures. At ninety percent compaction (10-percent air voids) we can expect joint performance to be: joint performance = mat performance – 1/5.
When joint density drops to 89% then joint performance can expect to be: joint performance = mat performance – 1/3. For a 15 year expected mat performance, giving up 1/5th means the joints fail 3 yrs earlier than mat (giving up 1/3rd means the joints fail 5 yrs earlier).

## Slide 18: Deteriorated Joint
How many years?

## Slide 19: How many years?

## Slide 20
Maintenance - Disruptive and Dangerous

## Slide 21: Efforts to Minimize Permeability along Longitudinal Joints
2001/2002 Longitudinal Joint Sealants
  IDOT worked w/ 2 companies to Develop a Longitudinal Joint Sealant (LJS)
  LJS is a Band of Asphalt Binder that Seals a lift of HMA from the Bottom Up.
  Here is How it Works:

## Slide 22: Joint Sealant Concept
Band melts up into the joint thus:
  Increasing density
  Decreasing permeability
  Increasing joint life
Unconfined
18 inches
Joint Sealant

## Slide 23: Asphalt Materials/Hendy Quickseam

## Slide 24: Longitudinal Joint Seal

## Slide 25: Longitudinal Joint Seal 12 Yrs Later

## Slide 26: Longitudinal Joint Seal 12 Yrs Later
No LJS
LJS

## Slide 27
Shear Tears

## Slide 28: Heavy Duty Pressure Distributor for Applying LJS

## Slide 29: Heavy Duty Pressure Distributor for Applying LJS

## Slide 30: Five Minutes After Placement

## Slide 31: Paving over LJS

## Slide 33: Licensed Subcontractor ≈ 11 Trucks

## Slide 34: LJS Spec Features
No Density Measurements within 1 foot from Joint
  Cannot use Production Gmm
  Gmm substantially reduced due to dramatic increase in asphalt binder
LJS can be applied:
  Push Cart
  Drag Box
  Roll out Tape
  Heavy Duty Pressure Distributor

## Slide 35: LJS Material Spec
Test | Test Requirement | Test Method
Dynamic shear @ 88°C (unaged), G*/sin δ, kPa | 1.00 min. | AASHTO T 315
Creep stiffness @ -18°C (unaged), Stiffness (S), MPa m-value | 300 max. 0.300 min. | AASHTO T 313
Ash, % | 1.0 - 4.0 | AASHTO T 111
Elastic Recovery, 100 mm elongation, cut immediately, 25°C, % | 65min. | ASTM D 6084 (Procedure A)
Separation of Polymer, Difference in °C of the softening point (ring and ball) | 3 max. | ITP Separation of Polymer from Asphalt Binder”

## Slide 36: LJS Spec Application Rates

## Slide 37: Longitudinal Joint Spec
Implementation Goals:
  2016 – 2 Projects per District
  2017 – 50% of Projects per District
  2018 – Full Implementation

## Slide 38: 2016 - LJS Projects
Total of 20-plus projects statewide
Average awarded cost $2.17 / lineal ft
Observations:
  Some minimal sporadic flushed spots < 25 feet in 10 plus miles (not a hindrance & shows migration is occurring)
  Shear tear will occur if required tack not in place
  Pressure Distributor Operators getting better
  Mix will pull up over unbonded scabs

## Slide 40: Cost Comparison
Inlay: $8.00 / lineal ft
  Includes: traffic control, mobilization, milling, priming, paving, pavement marking

## Slide 41: Cost Comparison
Microsurfacing: $4.81 / lineal ft
  Includes: crack seal, traffic control, pavement marking/removal

## Slide 42: Cost Comparison
Route and Seal: $2.00 / lineal ft
  Includes: crack seal, traffic control

## Slide 43: Cost Comparison
Longitudinal Joint Seal: $2.00 lineal ft

## Slide 44: LJS - Life Cycle Cost Analysis Two Lane Road
Chart: Additional Service Life (Years)
Breakeven LJS Unit Price | 6.51 | 6.84 | 7.64 | 8.83 | 10.26
Ave. Awarded LJS Unit Price | 2.17 | 2.17
Cost per lineal foot

## Slide 45: Also Works as a Tack Coat

## Slide 46: Thank You