## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Evaluation of the Benefits From Structural Fibers in Thin Concrete Pavements
Manik Barman
Assistant Professor, UMD
+ 46 Associate Members

## Slide 2
Manik Barman
Manik Barman, Assistant Professor (PI)
Bryce Hansen, Former Graduate Student
Jared, Munch, Graduate Student
Uma Arepalli, Post Doctoral Associate
Research Team

## Slide 3
Thanks to TAP Members and other Experts
Tim Anderson, MnDOT Kaye Bieniek, Minnesota LRRB Tom Burnham, MnDOT (TL) John Donahue, Missouri DOT Christine Dulian, MnDOT Debra Fick, MnDOT Bernard Izevbekhai, MnDOT | James Krstulovich, Illinois DOT Clifford, McDonald Maria Masten, MnDOT Luke Pinkerton, Helix Steel Dulce Rufino, California DOT Julie Vandenbossche, University of Pittsburgh Matthew Zeller, CPAM

## Slide 4
Thin Concrete Pavement/ Overlay
Over agg. base
Over asphalt
Over composite
Thin conc. Pavement
Thin conc. Overlays
Over concrete
Thickness: 3 to 6 inches
(bonded/unbonded)

## Slide 5
Thin Concrete Pavement Distresses
Joint faulting
Slab migration
Cracks
Notes: Introduction of thin concrete overlays. Importance of bonding and load transfer.

## Slide 6
Use of Fibers
Observed benefits:
1. Reduce cracking/ hold cracks tight
2. Increase load transfer efficiency
- reduce faulting
3. Reduce slab migration
4. Reduce slab thickness
5. Increase slab size (?)
Verities of Fibers; Many States
Notes: Introduction of thin concrete overlays. Importance of bonding and load transfer.

## Slide 7
Commonly used Structural Fibers
State | Number of Projects | Projects using Steel fibers |  | Projects using Synthetic fibers |  | Synthetic Fiber Dosage Distribution (%) | 
 |  | % | Dosage lb/yd3 | % | Dosage lb/yd3 | 3 lb/yd3 | Other lb/yd3
Georgia | 6 | 0 | N/A | 100 | 3 | 100 | 0
Illinois | 19 | 6 | 80 | 94 | 3, 4, 7.5 | 11 | 89
Kansas | 8 | 0 | N/A | 100 | 3 | 88 | 12
Minnesota | 11 | 0 | N/A | 100 | 3, 6.5, 25 | 36 | 64
South Carolina | 3 | 0 | N/A | 100 | 3 | 100 | 0
Virginia | 3 | 28 | 50, 75 | 72 | 3, 20, 25, 0.9 | 17 | 83
Total | 50 | 6 | N/A | 94 | -- | 51 | 49

## Slide 8
Examples of Performance Benefits
With FRC (King & Roesler, 2014).
With PCC (King & Roesler, 2014).
Illinois
Fibers helped to reduce slab
migration
Pavement performing well over the
design life, with heavy truck traffic

## Slide 9
Burnham, 2015
Minnesota
Examples of Performance Benefits
Still performing after 20 years of interstate traffic
Notes: Generally, LTE will be low at low temperature because of a wider crack width. We can observe this kind of trend in Cells 94 and 95. We do not see this trend in Cell 95, which had structural fiber. It appeared that structural fiber helped in transferring load in low temperature. So, we can say structural fiber contributed in Cell 95. It may be noted that as much as 25 lb/cy fiber was added in the concrete.

## Slide 10
South Carolina
Fibers holding shattered slab
pieces
Examples of Performance Benefits

## Slide 11
Missouri
Fibers did not reduce panel cracking but did reduce crack widths and joint degradation. No faulting was observed on this project and may be related to the use of fibers.
-- John Donahue
September, 2015
Examples of Performance Benefits

## Slide 12
General Performance Summary
State | Performance summary
Illinois | Reduced slab migration, joint separation, faulting and increased ride quality
Kansas | Less faulting, spalling and panel cracks
Minnesota | Increased LTE in old cells; no strong conclusions on 2014 cells, NRRA sections?
Missouri | Restricted faulting, reduced crack width and joint degradation
South Carolina | Increased service life
Virginia | Fibers exhibited good resiliency in minimizing cracking and crack width

## Slide 13
Now The Big Question is:
      How do we select fibers and dosages?
      How do we quantify fibers’ benefits and appropriately incorporate in the structural design?
      Use -
      Laboratory test results
      Use field performance and distress data
      Use test results on instrumented test sections, e.g. MnROAD
      Numerical Modeling

## Slide 14
Laboratory Study

## Slide 15
FRC: Fresh Conc. Properties
Typical volume fraction: 0.25% to 1.5%
Slump: 1 to 4 in. lower compared to PCC
Fiber balling: When aspect ratio >100
Vf > 1%
Steel
Typical volume fraction: 0.25% to 1.5%
Slump: Usually drops
Fiber balling: When aspect ratio >100
Vf > 1%
Synthetic

## Slide 16
Steel FRC: Hardened Conc. Properties
Comp. strength: 0% to 25% increase
Flexural strength: 0 to 50%
Direct tensile strength: 40% more compared to PCC
Chart: Vol. fraction
| 0 | 2.5000000000000001E-3 | 5.0000000000000001E-3 | 7.4999999999999997E-3 | 0.01
Compressive Strength | 6007 | 6702 | 7272 | 7462 | 6640
After Mahadik & Kamane, 2014
Chart: Vol. fraction
| 0 | 2.5000000000000001E-3 | 5.0000000000000001E-3 | 7.4999999999999997E-3 | 0.01
Flexural Strength | 670 | 857 | 931 | 960 | 899

## Slide 17
Syn. FRC: Hardened Conc. Properties
Comp strength: Little improvement; ductile failure of cylinders
Flexural strength: No improvement
Toughness/ Residual strength: Significant improvement
Load transfer efficiency (LTE): Significant improvement
Chart: Reinforcement Index (Vf*AR)
| 52.5 | 35 | 17.5 | 17.5 | 35 | 52.5 | 22.5 | 45 | 67.5 | 16.5 | 33 | 49.5 | 15 | 30 | 45 | 24.125 | 48.25 | 72.375 | 50 | 75 | 25 | 0 | 18.5 | 37 | 55.5 | 23.5 | 47 | 70.5
Synthetic | 6760 | 7060 | 6740 | 7080 | 6840 | 7100 | 6670 | 6860 | 6830 | 6610 | 6380 | 6770 | 6920 | 7790 | 7260 | 6660 | 6670 | 6740 | 6690 | 6290 | 7170 | 6960 | 6960 | 6230 | 6410 | 6570 | 6940 | 6850
Chart: Reinforcement Index (Vf *AR)
| 52.5 | 35 | 17.5 | 17.5 | 35 | 52.5 | 22.5 | 45 | 67.5 | 16.5 | 33 | 49.5 | 15 | 30 | 45 | 24.125 | 48.25 | 72.375 | 50 | 75 | 25 | 18.5 | 37 | 55.5 | 23.5 | 47 | 70.5 | 0
Synthetic | 720 | 780 | 760 | 760 | 690 | 730 | 790 | 770 | 780 | 700 | 720 | 710 | 680 | 750 | 790 | 740 | 750 | 750 | 710 | 690 | 780 | 780 | 690 | 680 | 710 | 750 | 760 | 720
Most Popular

## Slide 18
Post Crack Performance
Chart: Volume Fraction (%)
| 0.25 | 0.5 | 0.75
S.S.1 | 75.0556 | 158.3583 | 274.7778
S.S.2 | 53.6694 | 175.2229 | 319.1972
S.S.3 | 23.575 | 167.0389 | 325.8562
S.S.4 | 92.1333 | 225.9306 | 349.5833
S.T.5 | 116.8604 | 207.9528 | 326.625
S.C.6 | 116.1944 | 242.8542 | 330.5556
S.E.7 | 123.25 | 266.5813 | 318.6028
S.E.8 | 100.4813 | 150.2778 | 267.5833
S.E.9 | 133.3444 | 291.925 | 370.9722
S.T.11 | 85.825 | 163.8417 | 276.0417
Chart: Displacment (mil)
a
b
RSR= b/a*100

## Slide 19
Post Crack Performance
Chart: Volume Fraction (%)
| 0.25 | 0.5 | 0.75
S.S.1 | 10.3933 | 20.575 | 35.6133
S.S.2 | 6.7767 | 24.165 | 45.8667
S.S.3 | 2.9375 | 21.4233 | 41.325
S.S.4 | 12.4367 | 29.275 | 46.1333
S.T.5 | 14.8625 | 29.4267 | 47.3867
S.C.6 | 16.8067 | 31.675 | 41.1333
S.E.7 | 15.8333 | 33.95 | 43.3067
S.E.8 | 14.175 | 20.6433 | 36.4
S.E.9 | 17.3767 | 41.3567 | 50.6167
S.T.11 | 12.8 | 20.1 | 34.3
Chart: Volume Fraction (%)
| 0.75 | 0.5 | 0.25 | 0.25 | 0.5 | 0.75 | 0.25 | 0.5 | 0.75 | 0.25 | 0.5 | 0.75 | 0.25 | 0.5 | 0.75 | 0.25 | 0.5 | 0.75 | 0.5 | 0.75 | 0.25 | 0 | 0.25 | 0.5 | 0.75 | 0.25 | 0.5 | 0.75
Synthetic | 43.3067 | 33.95 | 15.8333 | 17.3767 | 41.3567 | 50.6167 | 2.9375 | 21.4233 | 41.325 | 14.175 | 20.6433 | 36.4 | 16.8067 | 31.675 | 41.1333 | 12.4367 | 29.275 | 46.1333 | 24.165 | 45.8667 | 6.7767 | 0 | 14.8625 | 29.4267 | 47.3867 | 10.3933 | 20.575 | 35.6133

## Slide 20
Post Crack Performance
Chart: Volume Fraction (%)
| 0.25 | 0.5 | 0.75 | 0.25 | 0.5 | 0.75 | 0.5 | 0.75 | 0.25 | 0.25 | 0.5 | 0.75
Straight | 2.9375 | 21.4233 | 41.325 | 12.4367 | 29.275 | 46.1333 | 24.165 | 45.8667 | 6.7767 | 10.3933 | 20.575 | 35.6133
End Crimped (steel) | 29.2667 | 67.02 | 54.6
Embossed | 43.3067 | 33.95 | 15.8333 | 17.3767 | 41.3567 | 50.6167 | 14.175 | 20.6433 | 36.4
Twisted | 14.8625 | 29.4267 | 47.3867
Continously crimped | 16.8067 | 31.675 | 41.1333
~ 50% more

## Slide 21
Joint Performance/ LTE

## Slide 22
Joint Performance/ LTE

## Slide 23
Joint Performance/ LTE
Chart: Time (s)
Chart: 
Chart: 
Deflections
Plain concrete
CW = 16 mils
CW = 47 mils
CW = 126 mils

## Slide 24
Joint Performance/ LTE
Chart: Load (kip)
Chart: Load (kip)
Chart: Differential Displacement (mil)
No Fibers
0.25% Vf
0.50% Vf

## Slide 25
Joint Performance/ LTE: Beam vs Slab
Chart: Crack width (mm)
| 0.43180000000000002 | 0.50800000000000001 | 0.68579999999999997 | 0.93979999999999986 | 1.1429999999999998 | 1.2192000000000001 | 1.3461999999999998 | 1.778 | 1.9811999999999999 | 2.1590000000000003 | 2.4384000000000001 | 2.9971999999999999 | 3.5813999999999995 | 4.5973999999999995 | 5.5880000000000001 | 7.8993999999999991 | 9.7281999999999993
Beam 1 | 81.5 | 79.5 | 76.5 | 73.5 | 66.5 | 59.5 | 47.5 | 50 | 50.5 | 49 | 49 | 46.5 | 39 | 36 | 20 | 16.5 | 11
Beam 2 | 85.5 | 81.5 | 80 | 78 | 73.5 | 66 | 67 | 56 | 60 | 63 | 60.5 | 55 | 55.5 | 44.5 | 46 | 35 | 29.5 | 17.5 | 16 | 9
Beam 3 | 81.5 | 76.5 | 77 | 68 | 66.5 | 63.5 | 63 | 61 | 55 | 55.5 | 46 | 44.5 | 36 | 26 | 19.5 | 10.5 | 9.5
Beam 4 | 83 | 82 | 80.5 | 80.5 | 77 | 70 | 73 | 73 | 62 | 62 | 54 | 53 | 48.5 | 51.5 | 40.5 | 36.5 | 19 | 16.5 | 8
Beam 5 | 79 | 87 | 80 | 69 | 63.5 | 60 | 54.5 | 44.5 | 42 | 28 | 24.5 | 17.5 | 8 | 6
Slab | 95.1156 | 91.7645 | 83.2951 | 77.9682 | 74.3913 | 69.3064 | 60.4645 | 56.0258 | 53.9412 | 45.4339 | 41.2182 | 26.6721 | 24.868 | 20.3109 | 18.3062 | 16.1102 | 15.3399 | 16.0283 | 12.2817
Barman and Vandenbossche, 2014
R2 > 0.8

## Slide 26
Joint Performance/ LTE vs Crack Width
Chart: Crack Width (mil)
| 11.166666666666694 | 12.833333333333327 | 16.666666666666607 | 26.666666666666544 | 36.999999999999773 | 43.333333333333151 | 46.666666666666707 | 47.500000000000021 | 47.833333333333172 | 58.333333333333421 | 58.500000000000142 | 58.666666666666721 | 59.499999999999886 | 74.833333333333456 | 76.333333333333513
Plain Concrete 1 | 86.2247 | 78.6882 | 87.4223 | 76.6208 | 47.2271 | 40.1727 | 33.2389 | 64.6375 | 42.5906 | 55.5433 | 39.0002 | 31.5836 | 22.6077 | 30.6037 | 35.6619 | 16.1064
Plain Concrete 2 | 35.6619 | 16.1064 | 10.3986 | 16.365 | 15.5319 | 10.1204
S.S.4 | 81.5277 | 87.8107 | 83.3382 | 88.7641 | 78.1961 | 69.6229 | 69.9902 | 87.2809 | 62.7492 | 63.4669 | 86.7663 | 63.966 | 57.1672 | 55.3111 | 71.2192 | 51.4988 | 65.2366 | 43.7493 | 45.5251 | 51.0145 | 41.2096 | 34.9715 | 31.4702 | 37.1775 | 28.3738
S.T.5 | 81.5277 | 78.8077 | 82.2308 | 78.4298 | 77.8012 | 75.6349 | 75.053 | 69.9902 | 72.7455 | 73.6487 | 70.105 | 70.5666 | 64.8669 | 62.7492 | 68.6467 | 57.791 | 53.8587 | 51.4988 | 39.9203 | 45.5251 | 42.9891 | 32.8648 | 34.9715 | 27.1854 | 28.3738 | 24.0027 | 19.6023
S.C.6 | 75.463 | 75.9584 | 68.9616 | 65.3429 | 58.8752 | 54.342 | 44.0895 | 38.0232 | 21.7241 | 20.3438 | 82.1666 | 83.1333 | 84.5493 | 79.9095 | 74.8224 | 67.6496 | 58.3688 | 35.3488 | 26.4508 | 19.7895 | 80.571 | 77.9256 | 77.1303 | 77.6132 | 73.9631 | 72.6239 | 69.1208 | 62.5946 | 49.0119 | 30.0139 | 19.2757
S.E.9 | 85.1846 | 85.1393 | 89.9185 | 77.7965 | 83.1142 | 87.1077 | 72.3251 | 81.3338 | 86.4396 | 66.2829 | 85.6512 | 75.5366 | 86.0141 | 62.4 | 58.4084 | 56.6987 | 75.6888 | 46.301 | 49.5866 | 35.501 | 24.943 | 36.8737 | 28.5226 | 29.0567 | 25.8704 | 16.914
S.T.11 1 | 80.0574 | 75.2177 | 77.3052 | 79.9368 | 80.6984 | 79.8291 | 79.664 | 77.3937 | 78.8438 | 78.1894 | 73.5468 | 76.2569 | 74.8646 | 72.1335
S.T.11 2 | 76.2569 | 74.8646 | 72.1335 | 70.3669 | 66.4274 | 58.7272 | 68.9188 | 53.6786 | 42.3556 | 23.0835 | 42.1163 | 26.5124 | 17.3564 | 26.0262
S.T.11 fiber was used MnROAD NRRA sections
Chart: Crack Width (mil)
| 3.8333333333334294 | 5.1666666666666154 | 9.3333333333330462 | 28.833333333333488 | 32.666666666666622 | 34.999999999999993 | 50.666666666666714 | 52.666666666666345 | 60.166666666666629 | 67.333333333333314 | 74.999999999999886 | 92.333333333333229 | 101.16666666666626 | 103.16666666666679 | 124.33333333333326 | 154.50000000000023 | 165.83333333333306 | 166.49999999999994
S.S.4.5 | 8.08 | 9.625 | 11.38 | 11.14 | 14.64 | 13.375 | 12.77 | 15.76 | 16.64 | 14.235 | 17.3 | 19.745 | 19.2 | 16.565 | 23.93 | 21.3 | 24.73 | 28.08
S.T.5.5 | 9.845 | 12.33 | 10.77 | 12.83 | 13.095 | 11.435 | 13.805 | 12.105 | 13.205 | 14.145 | 13.245 | 14.795 | 14.105 | 13.29 | 15.755 | 14.085 | 15.55 | 15.155 | 17.79 | 17.35 | 19.055 | 19.835 | 20.37 | 22.695 | 22.095 | 22.36 | 25.245
S.C.6.5 | 10.94 | 9.96 | 10.615 | 11.12 | 11.99 | 11.615 | 12.305 | 11.62 | 12.275 | 11.605 | 12.865 | 11.77 | 13.175 | 13.715 | 12.09 | 13.125 | 12.28 | 14.815 | 12.42 | 14.75 | 13.31 | 16.025 | 16.48 | 15.55 | 19.66 | 20.415 | 21.45 | 20.665 | 20.12 | 23.335 | 22.15
S.E.9.5 | 11.15 | 9.495 | 12.12 | 11.125 | 13.25 | 13.135 | 11.79 | 13.395 | 13.175 | 12.5 | 13.66 | 13.995 | 14.045 | 14.92 | 13.26 | 15.19 | 15.275 | 14.99 | 17.365 | 16.685 | 19.115 | 20.32 | 24.135 | 25.54 | 20.295 | 24.38
S.T.11.5 | 10.005 | 10.805 | 11.055 | 11.14 | 11.175 | 11.44 | 11.51 | 11.56 | 11.57 | 11.66 | 11.755 | 12.1 | 12.165 | 12.565 | 13.26 | 13.995 | 14.03 | 14.03 | 16.66 | 17.05 | 18.87 | 19.76 | 21.84 | 24.26 | 24.545

## Slide 27
Joint Performance/ LTE vs Crack Width
Chart: Crack Width (mil)
Plain Concrete | 86.2247 | 78.6882 | 87.4223 | 76.6208 | 47.2271 | 40.1727 | 33.2389 | 64.6375 | 42.5906 | 55.5433 | 39.0002 | 31.5836 | 22.6077 | 30.6037 | 35.6619 | 16.1064 | 10.3986 | 16.365 | 15.5319 | 10.1204
Plain concrete 2 | 35.6619 | 16.1064 | 10.3986 | 16.365 | 15.5319 | 10.1204
0.25% Vf | 87.704 | 84.8611 | 88.3516 | 90.1432 | 84.2687 | 84.5241 | 73.8497 | 74.3609 | 71.3717 | 67.5601 | 64.5492 | 68.3229 | 57.921 | 63.2359 | 57.6297 | 74.9823 | 47.0767 | 51.6666 | 51.4736 | 48.3903 | 51.3273 | 67.8402 | 35.7349 | 63.0869 | 37.1705 | 44.8943 | 37.5186 | 37.846 | 49.8941 | 23.2395 | 18.8335 | 29.5504 | 17.1765 | 11.302 | 12.5554 | 13.4436
Chart: Crack Width (mil)
| 11.166666666666694 | 12.833333333333327 | 16.666666666666607 | 26.666666666666544 | 36.999999999999773 | 43.333333333333151 | 46.666666666666707 | 47.500000000000021 | 58.333333333333421 | 58.666666666666721 | 59.499999999999886 | 74.833333333333456 | 76.333333333333513 | 79.999999999999773
plain 1 | 10.775 | 13.73 | 11.405 | 15.88 | 21.58 | 20.725 | 22.92 | 17.125 | 18.175 | 25.815 | 24.39 | 26.73 | 20.495 | 28.475
plain 2 | 29.88 | 25.275 | 32.9 | 33.285 | 32.135
0.25% Vf | 7.46 | 8.08 | 9.625 | 8.985 | 11.785 | 11.38 | 14.06 | 11.14 | 10.17 | 15.82 | 14.64 | 13.375 | 11.9 | 12.77 | 15.76 | 13.04 | 19.325 | 16.64 | 14.235 | 17.3 | 12.95 | 14.3 | 22.715 | 15.335 | 19.745 | 13.99 | 19.2 | 16.565 | 17.815 | 23.93 | 27.955 | 24.125 | 21.3 | 21.535 | 24.73 | 28.08

## Slide 28
Nomograph for Quantifying FRC Benefits
Notes: Fiber dosages: standard - corresponding to 20% residual strength ratio (ASTM C1609); enhanced - corresponding to 30% residual strength ratio (ASTM C1609); high – corresponding to 0.75 fibers volume fraction.

## Slide 29
Fiber Relaxation: A concern (?)
Chart: Crack Width (mil)
| 2.6666666666665209 | 31.50000000000016 | 49.83333333333325 | 75.833333333333044 | 94.49999999999973
LTE - Extension 1 | 87.704 | 71.3717 | 57.921 | 51.3273 | 44.8943
LTE - Contraction 1 | 44.8943 | 36.6275 | 86.058
LTE - Extension 2 | 86.058 | 11.302
LTE - Contraction 2 | 11.302 | 15.289 | 86.052
Chart: Crack Width (mil)
| 2.6666666666666692 | 35.499999999999865 | 68.499999999999929 | 86.833333333333172 | 103.83333333333307
LTE - Extension 1 | 83.0194 | 75.4174 | 54.4839 | 42.2521 | 35.6855
LTE - Contraction 1 | 35.6855 | 51.0599 | 83.9675
LTE - Extension 2 | 83.9675 | 19.1115
LTE - Contraction 2 | 19.1115 | 15.1379 | 57.5925
No Fibers
0.25% Vf
0.50% Vf
Chart: Crack Width (mil)
| 10.50000000000025 | 27.500000000000153 | 50.166666666666842 | 79.666666666666771 | 107.0000000000002
Expansion | 84.5187 | 77.4582 | 66.1818 | 58.8053 | 26.4964
Contraction | 26.4964 | 69.3259 | 86.4648
Notes: Fiber dosages: standard - corresponding to 20% residual strength ratio (ASTM C1609); enhanced - corresponding to 30% residual strength ratio (ASTM C1609); high – corresponding to 0.75 fibers volume fraction.

## Slide 30
Field Study
Notes: Fiber dosages: standard - corresponding to 20% residual strength ratio (ASTM C1609); enhanced - corresponding to 30% residual strength ratio (ASTM C1609); high – corresponding to 0.75 fibers volume fraction.

## Slide 31
NRRA-MnROAD FRC Test Sections
Cell number | Length (ft) | Pavement/ overlay Type | Underlying layer (constr. year) | Type of concrete/ fiber dosage* | Panel size W ft x L ft | Panel thickness (inch)
506 | 144 | Thin pavement on grade | 11 in. class 5Q aggregate base (2017) | Plain concrete | 6 x 6 | 5; 6*
606* | 138 |  |  | FRC/ standard |  | 
706 |  |  |  | FRC/ enhanced |  | 
806 |  |  |  | FRC/ high |  | 
139 | 270 | Ultra-thin Pavement on grade | 6 in. class 5 aggregate base (2017) | FRC/ enhanced | 6 x 6 | 3
239 | 273 | Thin Pavement on grade |  |  | 6 x 6 | 4
705 | 144 | Thin unbonded overlay | Concrete (1993) | FRC/ standard | Driving: 14 x 12 Passing: 13 x 12 | 5
805 | 124 |  |  |  | Driving: 6 x 12 and 8 x 12 Passing: 6 x 12 and 7 x 12 | 5
Notes: Fiber dosages: standard - corresponding to 20% residual strength ratio (ASTM C1609); enhanced - corresponding to 30% residual strength ratio (ASTM C1609); high – corresponding to 0.75 fibers volume fraction.

## Slide 32
Research Methodology and Objectives

## Slide 33
Tasks
Tasks | Schedule
Task 1: Literature review | 2017 Nov to 2018 February: COMPLETED, Report available at NRRA webpage
Task 2: Annual cell performance report | 2018 Aug to 2018 October: Year 1 2019 Aug to 2019 October: Year 2 2020 Aug to 2020 October: Year 3
Task 3: Contribution of fibers in reducing panel fatigue cracking | 2019 Jan to 2019 Dec
Task 4: Contribution of fibers in mitigating joint faulting | 2019 May to 2020 April
Task 5: Optimal panel size for FRC overlays | 2019 Aug to 2020 July
Task 6 and 7: Final report | April 2020 to 2020 October

## Slide 34
MnROAD NRRA Section: FWD Data Analysis
Chart: 9/12/2017, Driving Lane, Average of Approach and Leave LTEs
| Cell 506 | Cell 606 | Cell 706 | Cell 806
Joint x | 86 | 92.5805 | 92.5916 | 94
Joint y | 76 | 96.079 | 94.1999 | 92
Joint z | 86 | 89.4139 | 93.9679 | 93
Average | 82.6667 | 92.6911 | 93.5865 | 93

## Slide 35
MnROAD NRRA Section: FWD Data Analysis
Chart: 9/12/2017, Driving Lane, Approach
| Cell 506 | Cell 606 | Cell 706 | Cell 806
Joint x | 94.5497 | 95.3622 | 96.6373
Joint y | 58.3793 | 99.0275 | 92.5632
Joint z | 81.4709 | 89.4056 | 97.1611 | 95.7037
Average | 78.1333 | 92.3839 | 98.0943 | 94.9681
Chart: 9/12/2017, Driving Lane, Leave
| Cell 606 | Cell 706 | Cell 806
Joint x | 77.397 | 89.7988 | 92.5916 | 92.0319
Joint y | 93.2702 | 96.079 | 89.3722 | 90.5402
Joint z | 90.098 | 89.4221 | 90.7747 | 89.485
Average | 86.9217 | 91.7666 | 90.9128 | 90.6857
59

## Slide 36
MnROAD NRRA Section: FWD Data Analysis
Chart: Driving Lane 9/12/2017, Approach slab
| Cell 506 | Cell 606 | Cell 706 | Cell 806
Joint x | 246.52 | 133.6339 | 289.5738 | 155.1814
Joint y | 416.9307 | 209.6304 | 254.9383 | 154.1621
Joint z | 251.1292 | 233.4288 | 324.7988 | 151.0725
Average | 304.86 | 192.231 | 289.7703 | 153.472
Chart: Driving Lane 9/12/2017, Leave slab
| Cell 506 | Cell 606 | Cell 706 | Cell 806
Joint x | 273.4812 | 137.0464 | 299.7061 | 155.5665
Joint y | 304.0014 | 209.8554 | 259.4857 | 149.813
Joint z | 232.1434 | 227.3621 | 331.577 | 153.3221
Average | 269.8753 | 191.4213 | 296.9229 | 152.9006

## Slide 37
MnROAD Old FWD Data
Chart: 2000
| 28.58 | 77.72 | 109.4 | 82.039999999999992 | 27.68 | 27.86 | 61.339999999999996 | 106.16000000000001 | 88.52 | 26.779999999999987
Cell 94 | 0.59567 | 0.8338 | 0.82571 | 0.7034 | 0.66248 | 0.5802 | 0.71198 | 0.75253 | 0.71822 | 0.66666
Cell 95 | 0.85164 | 0.8024 | 0.74358 | 0.69482 | 0.74252 | 0.87414 | 0.81684 | 0.77715 | 0.77612 | 0.68656
Cell 95 had Polyolefin fibers
Crack width increase

## Slide 38
MnROAD Old Crack Width Data
Chart: Cell 94
| Joint 1 | Joint 2 | Joint 3 | Joint 4
10/24/1997 | 0 | 0 | 0 | 0
11/4/1997 | 0.0051181 | 0.033661 | 0.0035433 | 0.002231
2/11/1998 | 0.0052493 | 0.059908 | 0.0003937 | 0.021654
3/26/1998 | 0.0027559 | 0.044554 | 0.0051181 | 0.015486
6/16/1998 | 0 | 0.016076 | 0 | 0.0047244
10/1/1998 | 0.0019685 | 0.068176 | 0.0032808 | 0.042913
1/27/1999 | 0 | 0.058596 | 0.0018373 | 0.027822
7/13/1999 | 0 | 0 | 0.0099738 | 0.012336
10/19/1999 | 0 | 0.062533 | 0.01273 | 0.028609
1/8/2000 | 0 | 0.040748 | 0.013517 | 0.026247
3/28/2000 | 0.015026 | 0.05374 | 0.019029 | 0.012992
7/13/2000 | 0 | 0.038123 | 0.007021 | 0.0076115
Chart: Cell 95
| Joint 1 | Joint 2 | Joint 3 | Joint 4 | Joint 5 | Joint 6
10/24/1997 | 0 | 0 | 0 | 0 | 0 | 0
12/16/1997 | 0.0070866 | 0.03399 | 0.0088583 | 0.0045932 | 0.00052493 | 0.0059055
2/11/1998 | 0.0066929 | 0.049738 | 0.012664 | 0.0044619 | 0.018898 | 0.0074803
7/15/1998 | 0.0019685 | 0.0066929 | 0.0063648 | 0 | 0.0057743 | 0
10/1/1998 | 0.0085302 | 0.062205 | 0.01647 | 0.0052493 | 0.035433 | 0.0030184
1/28/1999 | 0.022966 | 0 | 0.008727 | 0 | 0.018504 | 0
7/13/1999 | 0.0095801 | 0.013714 | 0.019619 | 0.0072178 | 0.026115 | 0.0094488
1/3/2000 | 0.0093176 | 0.070997 | 0.010958 | 0 | 0.024803 | 0.002231
3/28/2000 | 0 | 0.019948 | 0.020276 | 0.0051181 | 0.022178 | 0.0023622
5/29/2000 | 0.011483 | 0.012073 | 0.015289 | 0.0066929 | 0.01168 | 0.0034121
Notes: Fiber dosages: standard - corresponding to 20% residual strength ratio (ASTM C1609); enhanced - corresponding to 30% residual strength ratio (ASTM C1609); high – corresponding to 0.75 fibers volume fraction.

## Slide 39
Concluding Remarks
Structural fibers are contributing; we have evidence
Most commonly used fibers are structural synthetic fibers
Stiffer fibers with crimped, embossed and twisted geometry performs better than the low stiffness
straight fibers, in terms of post crack performance
Fibers can improve 20% load transfer efficiency
We need to look at the fiber relaxation characteristics
These benefits shall be considered in the performance models that would be required for structural
design
Notes: Fiber dosages: standard - corresponding to 20% residual strength ratio (ASTM C1609); enhanced - corresponding to 30% residual strength ratio (ASTM C1609); high – corresponding to 0.75 fibers volume fraction.

## Slide 40: Questions?
mbarman@d.umn.edu
Cell 705
Cell 805

## Slide 41
Thank You