## Slide 1: Concrete Pavement Repair Product Evaluations at MnROAD
Tom Burnham, P.E. | Senior Road Research Engineer, Minnesota Department of Transportation
NRRA Pavement Workshop 2018
5/23/2018

## Slide 2: Typical Condition Before Patching
Original MnROAD concrete pavement cells constructed in 1992
1990 era MnDOT mixes not as durable as today (18 years to 1st repairs)

## Slide 3: Not As Suitable for Partial-Depth Repairs
Options for repair
Short term fix: Fill with sand to one-half depth
(to support mortar)
Long term fix: Change to full-depth repair
Due to surface condition (top 3” is sound) likely to ignore until it’s too late

## Slide 4: Partial-Depth Joint Repairs at MnROAD
Installed in 2011
93 concrete joints repaired
22 different materials (includes asphalt)
Many donated products (some installed by supplier)
Distress and soundness surveys conducted 4 times over 3 years
MnDOT Report 2016-16:
“Performance of Various Partial-Depth Repair
Materials at the MnROAD Facility”
Authors: Tom Burnham, Eddie Johnson, Ben Worel
http://www.dot.state.mn.us/research/TS/2016/201616.pdf

## Slide 5: Repair Area Preparation
Rotary-Head Milling
Sand Blast & Cleaning

## Slide 6: Typical MnDOT Installation
- Pre-wet and prime surface with mortar (for cementitious materials)
- Important to reestablish joint/crack

## Slide 7: Installation by Suppliers
Some did not reestablish joint/crack

## Slide 8: PCC Repair materials installed at MnROAD in 2011

## Slide 9: Performance Parameters
Location
  Frequently Loaded: Wheel paths, corners near shoulders
  Infrequently loaded: Between wheel paths, centerline
Traffic volume
  Driving lane = 80%
  Passing lane = 20%
Condition
Cracking: subjective rating scale 0-5, based on visual survey
  0 = failed, replaced by other material
  5 = no distress (condition similar to new)
Bonding
  Subjective range: None to full
  Determined with ballpeen hammer sounding

## Slide 10: Conditions Surveys
Patch Material | Joint Number | Patch location | Condition rating |  |  |  |  | Bonding condition Oct 2014
 |  |  | Feb 2012 | Oct 2012 | Apr 2013 | Sep 2013 | Oct 2014 | 
BASF 10-61 Surface Repair | 112 | Centerline | 4 | 4 | 3 | --- | 2 | Full
Blow Patch - RCM | 94 | Centerline | 5 | 5 | 4 | --- | 4 | Full
Blow Patch - RCM | 95 | Drive Ln | 4 | 4 | 3 | --- | 0 | Full
Blow Patch - RCM | 95 | Drive Ln | 5 | 4 | 4 | --- | 3 | Full
Blow Patch - RCM | 95 | Pass Ln | 5 | 5 | 3 | --- | 3 | Full
DOTLINE Rapid Repair | 119 | Drive Ln | 5 | 5 | 5 | --- | 2 | Full
EMACO S88 C1 | 114 | Centerline | 5 | 4 | 4 | --- | 3 | Full
Mainline 4 hour PCC | 109 | Pass Ln | 2 | 2 | 1 | --- | 1 | None
MAPEI Plaintop XS | 111 | Pass Ln | 4 | 3 | 3 | --- | 2 | Full
Rapid Set - Green/Orange | 127 | Centerline/Pass Ln | 4 | 4 | 3 | --- | 3 | Full
Rapid Set - Green/Orange | 128 | Centerline/ Drive Ln | 3 | 2 | 2 | --- | 1 | Full
Rapid Set - Green/Orange | 129 | Centerline | 3 | 3 | 3 | --- | 2 | Full
Rapid Set - Green/Orange | 129 | Pass Lane | 4 | 4 | 4 | --- | 4 | Full
Rapid Set - Orange | 125 | Centerline | 4 | 4 | 2 | --- | 1 | Full
Rapid Set - Orange | 126 | Centerline | 4 | 4 | 3 | --- | 3 | Full
Ready Mix 2 - 303A32F | 101 | Centerline | 4 | 4 | 4 | --- | 2 | Partial - NW corner
Ready Mix 2 - 303A32F | 101 | Pass Lane | 5 | 5 | 4 | --- | 2 | Partial - West side
Ready Mix 2 - 303A32F | 102 | Drive Ln | 5 | 4 | 3 | --- | 1 | Full - with patch
Ready Mix 2 - 303A32F | 104 | Drive Ln | 5 | 4 | 3 | --- | 2 | Partial along W side of transv jt
Ready Mix 2 - 303A32F | 104 | Centerline | 5 | 5 | 5 | --- | 4 | Full
Sikacrete + Cement/Sand (Blend) | 117 | Centerline | 4 | 4 | 4 | --- | 3 | Full

## Slide 11: Patch Performance

## Slide 12: Good Performance
Ready mix (not practical for rapid repairs)
Pavemend (only 1 repair on centerline)
Propoxy 2500
Rapid Set DOT
TCC 3U18
Hot Mix

## Slide 13: Evaluation Summary
55 of the 93 (59%) patches remained in good serviceable condition as of October 2014 (3 years of service)
The location of the patch did not seem to affect the performance significantly
  61% of centerline and 67% of the loaded area patches were in good condition
Certain materials were installed by a supplier, with some not following standard installation procedure followed by MnROAD and MnDOT installers
  May have had negative effects on the condition rating, particularly when isolation/expansion joints were not reestablished
Each material type had good and poor performers

## Slide 14: Full-Depth Repairs with RCC (2015)
Cell 38 – 6” JPCP
Cell 162 – 4” BCOA
Cell 505 – 5” UBOL
Applied 80k MnROAD truck loading within 18 hours (no visible cracking)

## Slide 15: Installation of Full-Depth Repairs with RCC
Trial slab to determine surcharge before compaction

## Slide 16: Performance of Full-Depth Repairs with RCC
After 2 years of LVR loading

## Slide 17: Partial-Depth PCC Repairs on WB I-94 (MnROAD Bypass)
Installed in 2017
162 locations repaired
17 different materials (includes asphalt)
Donated products (some installed by supplier)
Distress and soundness surveys will be conducted periodically
Details on locations and mixes can be found in Chapter 9 of:
“Report on 2017 MnROAD Construction Activities” (Available Summer 2018)

## Slide 18: PCC Repair Materials on WB I-94 Bypass
Product Trade Name | Material type | Manufacturer/Supplier
Rapid Set – DOT Repair Mix | Cementitious | CTS
RepCon 928 | Cementitious | SpecChem
FastRac 246 | Cementitious | Western Material and Design
3U18 Modified | Cementitious | TCC Materials
Ecofix | Cementitious | USG
Rapid Set DOT Repair Mix w/Helix 5-25-Standard BA (zinc coated) fibers | Cementitious | CTS/Helix
Rapid Set DOT Repair Mix w/Helix 5-25-SS BA (stainless steel) fibers | Cementitious | CTS/Helix
ProSpec Concrete Patching Mix | Cementitious | TCC Materials
CE 700 HPC | Epoxy | Western Material and Design
PaveSaver Polymeric Concrete Patch | Epoxy | D.S. Brown
FastPatch | Epoxy | Willamette Valley Company
Rapid Surface Repair Easy Mix | Epoxy | Five Star
Rapid Surface Repair Epoxy Fix | Epoxy | Five Star
HP Concrete Cold Patch | Petroleum-based | Crafco
Techcrete-TBR | Hot Mastic | Crafco
Aqua Patch | Asphalt | Aqua Patch Road Materials
Hot Mix Asphalt 2341-A | Asphalt | Ohman Brothers

## Slide 19: Installation Pattern

## Slide 20: Condition - May 2018
Some cracking reported immediately after installation

## Slide 21: Condition - May 2018

## Slide 22: Condition - May 2018

## Slide 23: Condition - May 2018

## Slide 24: Potential Issues?
Some products require special installation equipment/techniques
  Suitable for DOT maintenance forces/budgets?
Recyclability during future removal
  Will it “contaminate” recycled product?
  Will it “gum-up” milling/reclaiming machines?

## Slide 25: 2018 Repairs at MnROAD
Partial and full-depth joint repairs
  3U18
  3U58
  Special HE (3-4 hour opening strength)
Two full panel replacements
  RCC (including dowel bars)
  Internal Cure Mix
Early loading by empty tandem dump truck based on maturity
  ≈ 100 psi flexural first pass

## Slide 26: Acknowledgments
All product suppliers and installers

## Slide 27: Discussion
Discussion on topic