## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Determining Pavement Design Criteria for Recycled Aggregate Base and Large Stone Subbase
TPF-5(341)
Bora Cetin
Assistant Professor
Iowa State University
+ 46 Associate Members

## Slide 2: RESEARCH TEAM
Iowa State University
Principal Investigator – Bora Cetin
  Assistant Professor – Department of Civil, Construction & Environmental Engineering
Co-Principal Investigator – Ashley Buss
  Assistant Professor – Department of Civil, Construction & Environmental Engineering
Co-Principal Investigator – Halil Ceylan
  Professor – Department of Civil, Construction & Environmental Engineering
Co-Principal Investigator – Junxing Zheng
  Assistant Professor – Department of Civil, Construction & Environmental Engineering
Research Personnel – Haluk Sinan Coban
  PhD Student – Department of Civil, Construction & Environmental Engineering
  University of Wisconsin-Madison
Co-Principal Investigator – William Likos
  Professor – Department of Civil and Environmental Engineering
Co-Principal Investigator – Tuncer B. Edil
  Professor Emeritus – Department of Civil and Environmental Engineering

## Slide 3: OUTLINE
Problem Statement
Background
Objectives
Research Plan & Current Progress
Research Progress
Products and Deliverables

## Slide 4: PROBLEM STATEMENT

## Slide 5: PROBLEM STATEMENT

## Slide 6: PROBLEM STATEMENT
2 billion tons/year aggregate produced (FWHA 2004)
200 million tons/year of RCA and 90 million tons/year of RAP generated (FHWA 2011)
(http://www.gratechcompanyltd.com/aggregate.htm)

## Slide 7: PROBLEM STATEMENT
RAP
RCA
(Edil et al. 2012)
Annual Quantity Used

## Slide 8: PROBLEM STATEMENT
Environmental Impact?
Guideline?
Performance?
Fit?
Recycled Aggregates and Large Stone Subbase

## Slide 9: OBJECTIVES
1st Goal – Determine the field and laboratory performance
FWD, LWD, DCP, Intelligent compaction (IC) data
2nd Goal – Develop a method to estimate the stiffness and permeability
Percent crushing of recycled aggregates and LSSB
Sphericity, angularity, and surface texture of aggregates
3rd Goal – Prepare a pavement design and construction specification
Performance
Cost benefits
Unsaturated characteristics, index properties
Gravel, sand, fines content, gravel-to-sand ratio, D10, D30, D50, D60
Life cycle cost

## Slide 10
Task 1 – Literature Review and Recommendations
Task 2 – Tech Transfer “State of Practice”
Task 3 – Construction Monitoring and Reporting
Task 4 – Laboratory Testing
Task 5 – Performance Monitoring, Reporting and Climatic Effects
Task 6 – Instrumentation
Task 7 – Pavement Design Criteria
Task 8 & 9 – Draft/Final Report
RESEARCH PLAN

## Slide 11
Pavement Systems and Base/Subbase Course Applications
  Pavement Systems
  Recycled Materials in Base Course Applications
  Large-Size Aggregates in Subbase Course Applications
  Motivation and Purpose of This Research
  Engineering Properties of RAP, RCA and LSSB Materials
  Gradation Characteristics
  Compaction Characteristics
  Hydraulic Properties
  Strength Properties
  Shear Strength Properties
  Stiffness Properties
  Permanent Deformation Properties
  Creep Properties
  Freeze-Thaw and Wet-Dry Durability
  Environmental Properties of RAP and RCA
  Properties of RAP
    pH Characteristics
    Heavy Metal Leaching Characteristics
    Poly-Aromatic Hydrocarbons (PAHs) Leaching Characteristics
  Properties of RCA
    pH Characteristics
    Heavy Metal Leaching Characteristics
  Geosynthetic Applications
  Functions of Geosynthetics
  Effects of Using Geosynthetics
  Design Methods
  Selected Practices of State DOTs
  Recommendations
  References
Design Methods
AASHTO 1993
MEPDG Design
Selected Practices of State DOTs
MnDOT
CalTrans
MDOT
MoDOT
IDOT
WisDOT
Task 1 – Literature Review and Recommendations

## Slide 12
Determining Pavement Design Criteria for Recycled Aggregate Materials
Determining Pavement Design Criteria for Large Stone Subbase Materials
Task 2 – Tech Transfer Drafts

## Slide 13
Task 3 – Construction Monitoring and Reporting

## Slide 14: PERMEAMETER DATA ANALYSIS
Concept (White et al. 2010)
Variability of in-situ permeability – up to 400%
Gas permeameter test (GPT)
Rapid (< 30 sec) and portable (16 kg)
    Self-contained pressurized gas system
    Self-sealing base plate

## Slide 15: PERMEAMETER DATA ANALYSIS
Concept (White et al. 2010)
where;
Ksat = saturated hydraulic conductivity (cm/s)
Kgas = gas permeability
Krg = relative permeability to gas
μgas = kinematic viscosity of the gas (PaS)
Q = volumetric flow rate (cm3/s)
P1 = absolute gas pressure on the soil surface;
[P1 (Pa) = Po(g) (mm of H2O) x 250 + 101325]
Po(g) = gauge pressure at the orifice outlet (mm of H2O)
P2 = atmospheric pressure (Pa)
r = radius at the outlet (4.45 cm)
Go= Geometric factor (dimensionless factor see Figure 7)
Se = effective water saturation [Se = (S – Sr)/(1-Sr)]
λ = Brooks-Corey pore size distribution index
Sr = residual water saturation
S = water saturation
ρ = density of water (g/sm3)
g = acceleration due to gravity (cm/s2)
μwater = absolute viscosity of water (gm/cm-s)

## Slide 16: PERMEAMETER DATA ANALYSIS
Concept (White et al. 2010)
    S  from in-situ dry unit weight and moisture content
    Sr and λ  from soil water characteristic curves (SWCC)
    SWCC  need to know gradation
(Likos et al. 2013)
af, bf, cf, and yr  SWCC curve fitting parameters correlated with material gradation properties
SWCC parameters are derived, then Sr and l values are calculated using the Brooks and Corey (35) approach.

## Slide 17: PERMEAMETER DATA ANALYSIS
Concept (White et al. 2010)
Typical Sr and λ values (alternative)

## Slide 18: PERMEAMETER DATA ANALYSIS
Data Analysis

## Slide 19: PERMEAMETER DATA ANALYSIS
Data Analysis
Inside
Outside
Notes: After analyzing the test data, it was determined that some of the saturated hydraulic conductivity values were negative. The ISU team has gotten in contact with Dr. White regarding the unexpected negative values. It was told by Dr. White that the reason might have been some possible error during the testing or the malfunction of the gas permeameter test equipment. As a result, it was determined by the ISU team that negative values would be ignored.

## Slide 20: PERMEAMETER DATA ANALYSIS
Effect of Compaction
Inside
Outside

## Slide 21: LWD DATA ANALYSIS
Concept (Vennapusa and White 2009)

## Slide 22: LWD DATA ANALYSIS
Data Analysis

## Slide 23: LWD DATA ANALYSIS
08.21.2017
09.19.2017
NCHRP UTEP

## Slide 24: DCP DATA ANALYSIS
188 – Subgrade A – 01.24.2018 (NCHRP UTEP)

## Slide 25
Task 4 – Laboratory Testing

## Slide 26
Photographic Portrayal by Xiaodong Wang &
Craig H. Benson
UW-Madison Flexible-Wall Permeameter for Coarse-Textured Soils

## Slide 27
Permeameter with Constant Head Reservoirs for Headwater & Tailwater

## Slide 28
KSAT TEST RESULTS TO DATE

## Slide 29
SWCC TEST RESULTS TO DATE

## Slide 30
SWCC TEST RESULTS TO DATE

## Slide 31
The following data will be collected and analyzed:
    FWD, frost heave-thaw settlement, IRI, rutting, surface survey.
    Temperature, moisture, matric suction, strain data.
      Determine freeze-thaw cycle numbers and its impact on pavement performance
      Determine impact of frost heave and thaw settlements on pavement performance
      Predict frost/thaw depth
Task 5 & 6 – Performance Monitoring, Reporting, and Climatic Effects

## Slide 32
FWD elastic modulus of RCA base layer during 7 years (Data collected from MnDOT 2008 project).
Task 5 & 6 – Performance Monitoring, Reporting, and Climatic Effects

## Slide 33
a) Cumulative number of F-T cycles since 2008 in RCA base layer and b) field elastic modulus of RCA, RCA-VA blend, RAP, and Class 5 aggregate field test sections with F-T cycles (Edil et al. 2017).
Task 5 & 6 – Performance Monitoring, Reporting, and Climatic Effects

## Slide 34
(Li et al. 2016)
Task 5 & 6 – Performance Monitoring, Reporting, and Climatic Effects

## Slide 35: FIELD TESTING

## Slide 36
Prepare a report that:
    Summarizes the findings from the laboratory and field tests
    Provides detailed review on pavement design inputs in terms of benefits and costs
    Analyzes the cost effectiveness of using recycled materials and LSSB
    Shows correlations between the index properties and stiffness/permeability of geomaterials tested
    Provides the results of sustainability assessment analyses
Task 7 – Determine Pavement Design Criteria

## Slide 37
Task 8 & 9 – Draft/Final Report

## Slide 38: SCHEDULE
TASKS | MONTHS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33
Task 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 39: PRODUCTS & DELIVERABLES
Quarterly progress reports as required
Draft final report
Final report
Technology transfer brief
A copy of the executive final presentation

## Slide 40
Thank You

## Slide 41: DCP DATA ANALYSIS
328 - 09.18.2017

## Slide 42: DCP DATA ANALYSIS
428 - 09.18.2017

## Slide 43: DCP DATA ANALYSIS
528 - 09.18.2017

## Slide 44: DCP DATA ANALYSIS
628 - 09.18.2017

## Slide 45: DCP DATA ANALYSIS
528 – 08.21.2017 (Example)