## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Research Project Flexible Team LT1: Developing Best Practices for Rehabilitation of Concrete with Hot Mix Asphalt Overlays Related to Density and Reflective Cracking
Eshan V. Dave
Jo Sias Daniel and Katie Haslett
University of New Hampshire
+ 46 Associate Members

## Slide 2: Outline
Introduction and Project Overview
  Goals and Objectives
  MnROAD Sections
  Project Tasks
Research Approach
  Lab Tests
  Performance Models
Early Performance Results
Summary

## Slide 3
Appearance of a cracking pattern in the surface of an overlay that reflects the cracking/joint pattern in the underlying pavement
Allows water to infiltrate into underlying pavement structure, leading to further deterioration
One of the predominant failure modes in rehabilitated pavements
Reflective Cracking in Asphalt Overlays

## Slide 4: Reflective Cracking Performance in Minnesota
Chart: Construction Type
| Thin O/L | Thick O/L | O/L on FDR | New Const.
Thin O/L Thick O/L O/L on FDR New Const. | 8.3195 | 3.2155 | 0.738 | 0
26 Pavement Sections from Minnesota:
  Thin and Thick Overlays on milled pavement
  Full depth reclamation
Chart: Construction Type
| Thin O/L | Thick O/L | O/L on FDR | New Const.
Thin O/L Thick O/L O/L on FDR New Const. | 19.6869 | 14.7496 | 3.2877 | 0
Thin (mill and) overlay sections show an average cracking rate of 16%/yr. where as FDR and overlay sections average at 4%/yr.

## Slide 5: Project Overview
This research aims to develop a simple decision tree tool for selecting suitable asphalt mixtures and overlay designs to prolong overlay lives by lowering reflective cracking and improving in-situ density.

## Slide 6: Project Objectives
Slow reflective (and thermal and fatigue) cracking
Improve pavement life cycle costs
Suitability of lab tests for reflective cracking performance
Evaluate constructability considerations, including time needed to perform testing
Assess density evolution of mixes (current vs. Superpave 5 and retrogressed AV approaches)
Develop LCCA (Cost vs. benefit) decision tree for treatment of rigid pavement and selection of overlays

## Slide 7: Pavement Sections and Materials
12 cross sections with varying surface course and interlayer properties
  Surface course
    Thickness, gradation, density
  Interlayer
    Polymer modified, tack coat application and type
Control Section (983)
9.5" PCC 27X12 PANELS 1.25" DOWELS
5" CLASS 5 BASE AGGREGATE
CLAY SUBGRADE

## Slide 8
1.5" HMA (9.5 mm) Conventional Paver (0.08-0.10 gal/sy)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.5" HMA (12.5 mm) Conventional Paver (0.05-0.06 gal/sy)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.75" HMA (12.5 mm) Spray Paver (0.10 gal/sy)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.5" HMA (9.5 mm)
2.5" HMA (19 mm)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.75" HMA (12.5 mm, 4% AV)
2.25" HMA (19 mm)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.75" HMA (9.5 mm, AASHTO M323 #8)
2.25" HMA (19 mm)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.5" HMA (9.5 mm)
1" HMA (High Polymer Asphalt)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.5" HMA (9.5 mm)
1" HMA (PSAB/PASSRC)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.5" HMA (9.5 mm) Conventional Paver (0.08 – 0.10 gal/sy)
9.5" PCC 27X12 PANELS 1.25" DOWELS
0.75" UTBWC 0.20 gal/sy (Polymer mod. Membrane)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.75" HMA (12.5 mm, 5% AV)
2.25" HMA (19 mm)
9.5" PCC 27X12 PANELS 1.25" DOWELS
1.75" HMA (12.5 mm, 3% AV)
2.25" HMA (19 mm)
9.5" PCC 27X12 PANELS 1.25" DOWELS
Cell 984
Cell 985
Cell 986
Cell 987
Cell 988
Cell 989
Cell 990
Cell 991
Cell 992
Cell 993
Cell 994
Cell 995

## Slide 9: NRRA LT1 Research Tasks (1/2)
Task 1: Literature Review (ongoing)
Task 2: Gathering Past Performance Data and Laboratory Testing (ongoing)
  Field performance data, MnROAD and NRRA state agencies
  Survey for agencies (coming soon)
  Lab performance testing
Task 3: Mechanistic Analysis of HMA Overlays
  Performance simulations using PavementME (NCHRP 1-41) and FE Reflective Cracking Model
Task 4: Asphalt Density Evolution Over Time
  Density changes with time/traffic and relationship to performance

## Slide 10: NRRA LT1 Research Tasks (2/2)
Task 5: Life and Performance Curves for Asphalt Overlays
  Comparisons between mix properties, lab tests and field performance
  Cost effectiveness comparison (user and agency) of overlay structure options using LCCA
Task 6: Establish State of the Practice for PCC Condition
  Guidelines to assess existing PCC pavement conditions
Task 7: Establish State of the Practice for HMA Mixtures and their Effects on Reflective Cracking
  Simple decision tree based tool for selection of asphalt mixture and overlay design
Task 8: Reporting

## Slide 11: Outline
Introduction and Project Overview
  Goals and Objectives
  MnROAD Sections
  Project Tasks
Research Approach
  Lab Tests
  Performance Models
Early Performance Results
Summary

## Slide 12: Mix Tests
I-FIT (SCB) – IDOT
Texas Overlay Tester (OT) – IDOT
Disk-shaped Compact Tension (DCT) – MnDOT
AASHTO T-283 TSR - MODOT
Hamburg Wheel Tracking Test – WisDOT
MiST - MTU
Indirect tensile Strength and Creep (IDT) – MnDOT
Dynamic Modulus Test (E*) – MnDOT and UNH
Ideal-CT – (TTI/TAMU)
MN Semi-Circular Bend – UMN
Direct Tension Cyclic Fatigue (S-VECD) – UNH
Compact Tension (CT) - UNH

## Slide 13: Testing: S-VECD Fatigue (AASHTO TP 107)
Direct tension cyclic fatigue
Test temperatures ((PGHT-PGLT)/2)-3°C
Number of specimens: Typically 4 (1 at each strain level)
Outcome: Damage Characteristic Curve (DCC) and Energy dissipation for fatigue damage
Outcomes are utilized in pavement structural analysis model (FHWA Flexpave, part of PEMD initiative)

## Slide 14: Testing: Compact Tension (CT)
Test procedure tailored to measure fracture resistance of UTBWC
Crack propagation in reflective crack direction

## Slide 15: CT Fracture Test: Effects of Tack Type, Rate and Construction Method
1
2
3
4
5
Missouri Route-T

## Slide 16
Field Performance
Missouri Route-T

## Slide 17: Overlay Life and Performance Curve Development
Combination of field performance, lab performance test results, performance modeling and life cycle cost analysis
Field Performance: 12 MnROAD sections
Performance Models:
  More than 12 sections
    AASHTOWare PavementME
    Finite Element Reflective Cracking Model (In-house)
Life Cycle Cost Analysis:
  FHWA RealCost
  Pavement Roughness-based User Cost Calculations

## Slide 18: Life Cycle Cost Analysis (LCCA)
An economic analysis
  Compares design or rehabilitation alternatives
  Considers all significant costs
  Evaluates the alternatives over scientifically correct analysis periods
Importance of LCCA
  All costs can be taken into account
    Agency costs (data will be collected from NRRA member states)
    User costs
    Salvage value
  Alternative strategies can be compared
    On an equivalent basis

## Slide 19: UNH Study on Maintenance Alternatives Selection: Vehicle Fuel Efficiency vs. IRI
Linking of EPA MOVES (Mobile Vehicle Emissions Simulator) and pavement roughness to estimate fuel consumption
Chart: IRI (in/mi)
| 50 | 100 | 150 | 200
RTTD | 497.3667 | 499.5013 | 501.6358 | 503.7703
Baseline | 465.1677 | 467.3192 | 469.4707 | 471.6222
RTTD: Real Time Traffic Data

## Slide 20: UNH Study on Maintenance Alternatives Selection
I-494 Case-study
IRI curves generated for 6 scenarios
  Baseline: No maintenance until terminal condition
  Mill & Overlay
  Crack Sealant (CS)
  Microsurfacing (MS)
  Cold-In-Place (CIR) Recycling
Steady flow versus Real-time traffic data (RTTD)
Simulation conditions:
  Initial IRI = 63 in/mi; Terminal IRI = 172 in/mi; Minimum of 3 cycles

## Slide 21: Maintenance Alternatives Life Cycle Cost Comparison
Total Net Present Value (NPV) |  |  |  |  |  | 
Cross Section | Maintenance Alternative |  |  |  |  | 
 | Baseline | Crack Sealant | MS (IRI =140) | MS (IRI =160) | CIR | Thin Overlay
ARGG -1 | $231,618,958 | $219,152,098 | $187,105,111 | $190,671,362 | $158,051,156 | $156,954,499
ARGG -2 | $230,873,072 | $219,152,047 | $186,925,693 | $190,632,806 | $157,966,037 | $156,950,403
T - 1 | $231,618,958 | $223,500,437 | $187,105,111 | $190,634,818 | $158,039,813 | $156,950,403
THS - 1 | $266,628,116 | $251,815,947 | $218,765,220 | $198,617,699 | $159,240,577 | 
SHM - 1 | $298,528,698 | $277,218,842 | $253,118,168 | $214,731,747 | $160,287,057 | 
Average percent difference from 2 inch mill & overlay alternative
CIR = 0.7 %
MS at IRI 160 in/mi = 19.4 %
MS at IRI 140 in/mi = 17.5 %
CS = 33.7 %
Baseline = 38.3 %
Most Economical
Least Economical

## Slide 22: Life Cycle Costs (Agency and User)
Chart: Yearly Cost Comparison
| Microsurface (IRI 160) | Crack Sealant | Mill and Fill | Baseline | CIR | Microsurface (IRI 140) | Microsurface (IRI 160) | Crack Sealant | CIR | Mill and Fill | Baseline | Microsurface (IRI 140) | Microsurface (IRI 140) | Baseline | CIR | Microsurface (IRI 160) | Crack Sealant | Mill and Fill | Baseline | Crack Sealant | CIR | Microsurface (IRI 140) | Microsurface (IRI 160) | Baseline | Microsurface (IRI 140) | CIR | Crack Sealant | Microsurface (IRI 160) | ARGG -1 | ARGG -2 | SHM -1 | T-1 | THS - 1
Operation Cost | 15.0331 | 21.6815 | 22.9627 | 23.1147 | 23.1258 | 23.7728 | 18.6361 | 21.4568 | 22.6433 | 22.6458 | 22.9535 | 23.6 | 18.4146 | 21.3371 | 22.3771 | 22.6894 | 23.4869 | 23.1186 | 28.857 | 31.148 | 32.4397 | 33.8071 | 33.8164 | 24.4933 | 25.6007 | 26.4714 | 26.8558 | 28.0051
Construction/Maintenance Cost | 0.88684 | 1.4708 | 1.1211 | 1.6663 | 1.1371 | 1.386 | 0.90352 | 1.461 | 1.1124 | 1.1053 | 1.6491 | 1.3745 | 1.1019 | 1.5 | 1.1626 | 1.1289 | 1.386 | 1.6663 | 2.7388 | 2.7447 | 1.6524 | 2.7217 | 2.3089 | 2.0353 | 1.7501 | 1.316 | 2.1161 | 1.7423
56% difference in operations cost (users)
68% difference in construction/maintenance cost (agency)

## Slide 23: Outline
Introduction and Project Overview
  Goals and Objectives
  MnROAD Sections
  Project Tasks
Research Approach
  Lab Tests
  Performance Models
Early Performance Results
Summary

## Slide 24: Early Results: DCT Fracture Energy and Cracking Amounts (1 of 3)
Chart: Fracture Energy, Gf, J/m2
| 984 | 985 | 986 | 987
 | 448.73 | 491.035 | 491.035 | 510.1667
 | 448.73
Total Ft. of Reflective Cracks | 173 | 178 | 146 | 64
Acknowledgements: D. Ghosh and D. Van Deusen (MnROAD/MnDOT)

## Slide 25: Early Results: DCT Fracture Energy and Cracking Amounts (2 of 3)
Acknowledgements: D. Ghosh and D. Van Deusen (MnROAD/MnDOT)
Chart: Fracture Energy, Gf, J/m2
| 988 | 989 | 990 | 991
SPWEC440E | 510.1667 | 510.1667 | 510.1667 | 510.1667
 | 491.035 | 477.1491 | 509.905 | 448.73
Total Ft. of Reflective Cracks | 62 | 12 | 0 | 36

## Slide 26: Early Results: DCT Fracture Energy and Cracking Amounts (3 of 3)
Acknowledgements: D. Ghosh and D. Van Deusen (MnROAD/MnDOT)
Chart: Fracture Energy, Gf, J/m2
| 992 | 993 | 994
 | 571.635 | 448.73
 | 448.73 | 448.73
Total Length of Reflective Cracks | 85 | 50 | 300

## Slide 27: Summary
Project is underway, simultaneous focus on reflective cracking and density/volumetrics
Majority of test data is now available
Field performance data after one winter is also now available
Researchers are starting to make comparisons between field performance and lab tests
Agency surveys are being prepared to obtain cost data, current practice review and past performance data

## Slide 28: Thank you for your attention!
Contact:
  Email: eshan.dave@unh.edu
  Phone: 603-862-5268

## Slide 29
Thank You!

## Slide 30: Appendix

## Slide 31: Cross Sections

## Slide 32: Material Information
CELL | DESC | TRAFF LEVEL | AGG SIZE | BINDER | DES VOIDS | COMMENT
992 | HMA over concrete | 4 | 4.75 | 58E-34 | 3 | Lift 1 (interlayer)
991 |  |  |  | 58H-28 | 4 | Lift 2
984, 994 | HMA over concrete | 4 | 9.5 | 58H-28 | 4 | Lift 1
987 |  |  |  |  |  | Lift 2
992 |  |  |  |  |  | Lift 2 (over interlayer)
993 |  |  |  |  |  | Lift 2 (over PASSRC)
985, 986 | HMA over concrete | 4 | 12.5 | 58H-28 | 4 | Lift 1
988, 989, 990 |  |  |  |  |  | Lift 2
987-991 | HMA over concrete | 4 | 19 | 58H-28 | 4 | Lift 1

## Slide 33: Timeline – Year 1
Tasks |  | Month |  |  |  |  |  |  |  |  |  |  | 
 | Month of Contract: | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
 | Calender Month: | F | M | A | M | J | J | A | S | O | N | D | J
Task- 1 | Literature Review |  |  |  |  |  |  |  |  |  |  |  | 
Task- 2 | Data Collection and Lab Testing |  |  |  |  |  |  |  |  |  |  |  | 
Task- 3 | Mechanisitic Analysis of HMA overlay |  |  |  |  |  |  |  |  |  |  |  | 
Task- 4 | Asphalt Density Evolution Over Time |  |  |  |  |  |  |  |  |  |  |  | 
Task- 5 | Life and Performance Curves |  |  |  |  |  |  |  |  |  |  |  | 
Task- 6 | State of Practice or PCC Conditions |  |  |  |  |  |  |  |  |  |  |  | 
Task- 7 | State of Practice for HMA Mixtures and effects on Reflective Cracking |  |  |  |  |  |  |  |  |  |  |  | 
Task- 8 | Reporting |  |  |  |  |  |  |  |  |  |  |  | 
8.1 | Quarterly Staus Reports |  |  |  |  |  |  |  |  |  |  |  | 
8.2 | Technical Committee Meetings |  |  |  |  |  |  |  |  |  |  |  | 
8.3 | Progress Reports |  |  |  |  |  |  |  |  |  |  |  | 
8.4 | Final Report and Recommendations |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 34: Timeline – Year 2
Tasks |  | Month |  |  |  |  |  |  |  |  |  |  | 
 | Month of Contract: | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24
 | Calender Month: | F | M | A | M | J | J | A | S | O | N | D | J
Task- 1 | Literature Review |  |  |  |  |  |  |  |  |  |  |  | 
Task- 2 | Data Collection and Lab Testing |  |  |  |  |  |  |  |  |  |  |  | 
Task- 3 | Mechanisitic Analysis of HMA overlay |  |  |  |  |  |  |  |  |  |  |  | 
Task- 4 | Asphalt Density Evolution Over Time |  |  |  |  |  |  |  |  |  |  |  | 
Task- 5 | Life and Performance Curves |  |  |  |  |  |  |  |  |  |  |  | 
Task- 6 | State of Practice or PCC Conditions |  |  |  |  |  |  |  |  |  |  |  | 
Task- 7 | State of Practice for HMA Mixtures and effects on Reflective Cracking |  |  |  |  |  |  |  |  |  |  |  | 
Task- 8 | Reporting |  |  |  |  |  |  |  |  |  |  |  | 
8.1 | Quarterly Staus Reports |  |  |  |  |  |  |  |  |  |  |  | 
8.2 | Technical Committee Meetings |  |  |  |  |  |  |  |  |  |  |  | 
8.3 | Progress Reports |  |  |  |  |  |  |  |  |  |  |  | 
8.4 | Final Report and Recommendations |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 35: Timeline – Year 3
Tasks |  | Month |  |  |  |  |  |  |  |  |  |  | 
 | Month of Contract: | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36
 | Calender Month: | F | M | A | M | J | J | A | S | O | N | D | J
Task- 1 | Literature Review |  |  |  |  |  |  |  |  |  |  |  | 
Task- 2 | Data Collection and Lab Testing |  |  |  |  |  |  |  |  |  |  |  | 
Task- 3 | Mechanisitic Analysis of HMA overlay |  |  |  |  |  |  |  |  |  |  |  | 
Task- 4 | Asphalt Density Evolution Over Time |  |  |  |  |  |  |  |  |  |  |  | 
Task- 5 | Life and Performance Curves |  |  |  |  |  |  |  |  |  |  |  | 
Task- 6 | State of Practice or PCC Conditions |  |  |  |  |  |  |  |  |  |  |  | 
Task- 7 | State of Practice for HMA Mixtures and effects on Reflective Cracking |  |  |  |  |  |  |  |  |  |  |  | 
Task- 8 | Reporting |  |  |  |  |  |  |  |  |  |  |  | 
8.1 | Quarterly Staus Reports |  |  |  |  |  |  |  |  |  |  |  | 
8.2 | Technical Committee Meetings |  |  |  |  |  |  |  |  |  |  |  | 
8.3 | Progress Reports |  |  |  |  |  |  |  |  |  |  |  | 
8.4 | Final Report and Recommendations |  |  |  |  |  |  |  |  |  |  |  |