## Slide 1: Fracture Energy Performance Testing of 2017 NRRA Mixtures
Debaroti Ghosh, PhD
Dave Van Deusen, PE
Minnesota Department of Transportation
NRRA Pavement Workshop 2018
5/23/2018

## Slide 2: Overview of Several Studies _ NRRA 2017 Construction
    Concrete rehab w/HMA overlays and HMA compaction over concrete
    Geotechnical sections – recycled aggregate base and large-stone subbase
    Cold Central Plant Recycling
    Maintaining poor pavements (Thinlay)
Mix Type used for various lift thickness (6 types) | Traffic Level | Agg Size, mm | Binder Type | Design Air voids, %
SP WE A 4 40 E; SP WE B 4 40 E; SP WE C 4 40 E; SP WE B 4 50 E; SP WE B 4 30 E; SP WE D 4 30 I | 3; 4 | 4.75; 9.5; 12.5; 19.0 | PG 58H-28; PG 58E-34 | 2.0-5.0
Mix Type for Single Lift | Traffic Level | Agg size, mm | Binder Type | Design Air voids, %
SP WE D 4 40 E | 4 | 4.75 | 58H-28 | 4.0
Mix Type for Both Lift | Traffic level | Agg size, mm | Binder Type | Design Air voids, %
SP WE B 3 40 C | 3 | 12.5 | PG 58H-34 | 4.0
Mix Type for Single Lift | Traffic Level | Agg Size, mm | Binder Type | Design Air voids, %
SP WE B 3 40 C | 3 | 12.5 | 58H-34 | 4.0

## Slide 3: MAP
C Compaction study, Cells 988-991
B
B Overlay study, Cells 984-987

## Slide 4: NRRA Construction Report

## Slide 5: Objectives
  Present overall results of DCT testing
  Preliminary cracking performance of HMA overlays of concrete
  Disk Shaped Compact Tension Test
Mixture Type: 8; Replicate: 12; Test Temperature: -21.4°C
Chart: CMOD, mm
Wf

## Slide 6: Overview of Fracture Energy for Different Experiments

## Slide 7: HMA over Concrete _ Concrete Rehab
Chart: Fracture Energy, Gf, J/m2
| 984 | 985 | 986 | 987
 | 448.73 | 491.035 | 491.035 | 510.1667
 | 448.73
Total Ft. of Reflective Cracks | 173 | 178 | 146 | 64

## Slide 8: HMA over Concrete _ Compaction Study
Chart: Fracture Energy, Gf, J/m2
| 988 | 989 | 990 | 991
SPWEC440E | 510.1667 | 510.1667 | 510.1667 | 510.1667
 | 491.035 | 477.1491 | 509.905 | 448.73
Total Ft. of Reflective Cracks | 62 | 12 | 0 | 36

## Slide 9: HMA over Concrete_ Concrete Rehab
Chart: Fracture Energy, Gf, J/m2
| 992 | 993 | 994
 | 571.635 | 448.73
 | 448.73 | 448.73
Total Length of Reflective Cracks | 85 | 50 | 300

## Slide 10: Correlation between Lift Thickness and Length of Cracking based on Preliminary Performance
Cell No. | Experiment Type | Lift Thickness, inch | Total Length of Reflective Cracking, ft
984 | Concrete rehab w/HMA overlays | 1.5 | 173
985 |  | 1.5 | 178
986 |  | 1.75 | 146
987 |  | 4 | 64
988 | HMA compaction over concrete | 3.5 | 62
989 |  | 3.5 | 12
990 |  | 3.5 | 0
991 |  | 3.5 | 36
992 | Concrete rehab w/HMA overlays | 2.5 | 85
993 |  | 2.5 | 50
994 |  | 1.5 | 300
Chart: Lift Thickness, inch
| 2.5 | 2.5 | 1.5 | 1.5 | 1.5 | 1.75 | 4 | 3.5 | 3.5 | 3.5 | 3.5
 | 85 | 50 | 300 | 173 | 178 | 146 | 64 | 62 | 12 | 0 | 36

## Slide 11: Preliminary Statistical Analysis of Mixture Fracture Energy
Mix | Aggregate size, mm | PG | Average Fracture Energy, Gf, J/m2 | Maximum Gf | Minimum Gf | Range | Standard Deviation | p-value, (95% CI)
SP WE B 4 40 E | 12.5 | 58H-28 | 491 | 564 | 406 | 159 | 54 | Control
SP WE A 4 40 E | 9.5 | 58H-28 | 449 | 635 | 380 | 256 | 64 | 0.05
SP WE B 3 40 C | 12.5 | 58H-34 | 447 | 599 | 350 | 249 | 83 | 0.07
SP WE B 4 30 E | 12.5 | 58H-28 | 510 | 628 | 417 | 211 | 68 | 0.23
SP WE B 4 50 E | 12.5 | 58H-28 | 477 | 582 | 384 | 198 | 164 | 0.29
SP WE C 4 40 E | 19.5 | 58H-28 | 510 | 729 | 438 | 291 | 87 | 0.26
SP WE D 4 30 I | 4.75 | 58E-34 BLEND2 | 572 | 643 | 454 | 189 | 58 | 0.00
SP WE D 4 40 E | 4.75 | 58H-28 | 466 | 556 | 383 | 173 | 58 | 0.14
Student T-test was performed for p-value to determine significantly different mix compared to the control mix SPWEB440E.

## Slide 12: Distribution of replicate-sets identified as significantly different based on p-value
Chart: Fracture Energy, Gf, J/m2
| 405.8 | 427.11 | 430.67 | 468.1 | 469.24 | 474.81 | 493.18 | 508.25 | 540.82000000000005 | 554.52 | 555.58000000000004 | 564.34
SPWEB440 (Control Mix) | 0.0021517 | 0.003678 | 0.003963 | 0.0067051 | 0.006763 | 0.007009 | 0.0073215 | 0.0069699 | 0.0048237 | 0.0037129 | 0.0036289 | 0.0029602
SPWEA440E | 0.0034729 | 0.0044098 | 0.005708 | 0.0059179 | 0.0059212 | 0.0059763 | 0.0062283 | 0.0062291 | 0.0062366 | 0.006218 | 0.0058255 | 8.9106e-05
SPWED430I | 0.00086843 | 0.0051872 | 0.005232 | 0.0052839 | 0.0059985 | 0.0067973 | 0.0063981 | 0.0063591 | 0.0050636 | 0.0045411 | 0.0032106 | 0.0031886

## Slide 13: Effects of Various Mixture Properties on Fracture Energy
Pearson Correlation Coefficient was calculated to observe the effects of various mixture properties individually on Fracture Energy.
Chart: 
| Total % AC, Pb | Virgin % AC, Pbv | Effective % AC. Pbe | AFT Adj | % Air Voids | #4 | #8 | #200 | %RAP | Mix Agg Sp.G, Gsb
Mix Design | 0.59676 | 0.59618 | 0.6459 | 0.3015 | -0.62029 | 0.3637 | 0.3185 | 0.37792 | -0.39625 | 0.38697
Production | 0.2858 | 0.61895 | 0.27973 | 0.064016 | -0.53309 | 0.38251 | 0.34643 | 0.35363 | -0.45367 | 0.44026

## Slide 14: Fracture Energy Prediction Model (in progress)
Chart: Actual Log Gf
MnDOT DCT Master database has around 1500 replicates test results,
157 different mixes,
More than 12 different projects.
Model Based on 861 data points from master database

## Slide 15: Prediction of NRRA 2017 Mixture Fracture Energy Using Prediction Model
Chart: 
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E
Actual from DCT test | 448.73 | 446.545 | 509.905 | 491.035 | 477.1491 | 510.1667
Prediction using MDR | 356.1221 | 561.3959 | 417.4492 | 428.5567 | 431.422 | 527.8981
Prediction using TSS | 427.277 | 590.9611 | 440.1028 | 402.8916 | 485.6573 | 410.5601

## Slide 16
Thank you