## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Reliability Evaluation Of MnDOT’s Concrete Rehabilitation Sections
Bernard Igbafen Izevbekhai P.E., Ph.D.
Research Operations Engineer MnDOT
+ 46 Associate Members

## Slide 2: Pavement Planning Predictions & Prognostications
Purposes and Objectives are Deterministic
Solution Matrix is Stochastic
Expected Results are Probabilistic
      Reliability Analysis ≈ Reliable Approach !!

## Slide 3: Reliability is a Probabilistic Approach
Hazard
Time
Time
Reliability

## Slide 4: Used Weibull Method For Reliability Analysis
Assumes no Distribution Type but Discovers What it is
Provides the Three Parameters and More
Applicable to all Fields of Human Endeavor
Needs more Usage in Infrastructure
Notes: Assumes no Distribution Type but Discovers What it is

## Slide 5
THREE VITAL RELIABILITY PARAMETERS
Scale Parameter :How long does this treatment last?
(Characteristic Life, μ )
Location Parameter: How much preventive maintenance window
does this fix provide?
(Threshold Time To Failure, t0 )
Shape Parameter: What Kind of Failure mode does it present? (Shape Factor β) Infantile? β<1; Random? β ;Wear-out? β >1
Notes: 1) How Long does thuis pavement Last

## Slide 6: IMPORTANT WEIBULL CHARACTERISTICS
t0 Threshold time-to-failure, or guaranteed life. In many cases of wear-out the first failure does not appear until some significant running time t0 has elapsed.
= Characteristic life. When t – to = , P(t) = exp (-1) = 0.37, is the interval between to and the time at which it can be expected that 63.2% of the items will have failed (It is pivotal).
.
β= Shape Factor or Failure Mode: A measure of burn-in, random failure or wear-out.

## Slide 7: WHY CONCRETE REHABILITATION
Area Normalized By Cost of Fix is the Actual Benefit Indicator
Preventive/Preservative
Rehabilitation
Benefit Area
Replace
Reconstruct

## Slide 8
RIGHT TREATMENT RIGHT PURPOSE RIGHT TIME
Notes: RIGHT TREATMENT RIGHT PURPOSE RIGHT TIME

## Slide 9
A STRONG CASE FOR REHAB
Notes: A STRONG CASE FOR REHAB

## Slide 11: WEIBULL PROCESS MINIMIZES RIGOR
Normal Distribution
Weibull Distribution
Good News

## Slide 12
= slope of best line (identifying t0) = Shape factor
=
Finding the Weibull Parameters

## Slide 13: INTERSTATE MAJOR REHABILITATION
Chart: RSL

## Slide 14: Weibull Results for Major CPR WITH GRIND
INT from LnLn((1-Ft)-1) Vs Ln t-to | -8.433
Failure Mode (Beta) = | 2.904
Mu=e (ABS(INT))/Beta) = | 18.25

## Slide 15: Reliability Without Presumption

## Slide 16: Reliability Without Presupposition

## Slide 17: SNAPSHOT: SUMMARY RESULTS IS 35 IS 94
 | Meaning
Beta= 2.86 | End of Life Slightly higher than the lognormal distribution
Intercept = -7.6 | 
=14.14 | Characteristic Life is 14 Years on the Interstate 35 M-Records.
 | Meaning
Beta= 2.86 | End of Life Slightly higher than the lognormal distribution
Intercept = -7.6 | 
 | Characteristic Life is 14 Years on the Interstate 35 M-Records.

## Slide 18: Shape Function For Concrete Rehab
Chart: LN (t-0)

## Slide 19: Rehab Hazard Function
Chart: Post Rehab Age

## Slide 20: Hazard Function for Major Concrete Rehabilitation

## Slide 21: Concrete Rehab US Highways Hazard Function
Chart: Post Rehab Age
INT= | 3.6366
Beta = | 1.32
Mu= | 15.7

## Slide 22: US HIGHWAY WEIBULL VARIABLES
INT= 3.6366
Beta = 1.32
Mu= 15.7

## Slide 23: RQI AT REHAB US HIGHWAYS BEFORE Vs AFTER
Chart: RQI
| 3.6 | 3 | 3.5 | 3.5 | 3.4 | 3.5 | 2.6 | 1.9 | 2.5 | 1.3 | 3 | 3.1 | 2.6 | 3.5 | 3.3 | 3.3 | 2.8 | 2.9 | 3 | 2.8 | 3 | 3 | 3.1 | 3.1 | 3.1 | 3 | 3.2 | 3.2 | 3.3 | 3.1 | 3.3 | 3.2 | 3.1 | 3.5 | 3.3 | 3.4 | 3.1 | 3.4 | 3.5
Spike /RQI | 0.13889 | 0.16667 | 0.071429 | 0.028571 | 0.058824 | 0.057143 | 0.57692 | 0.36842 | 0.4 | 1.9231 | 0.066667 | 0.064516 | 0.26923 | 0.057143 | 0.060606 | 0.060606 | 0.21429 | 0.068966 | 0.2 | 0.071429 | 0.033333 | 0.13333 | 0.032258 | 0.032258 | 0.064516 | 0.13333 | 0 | 0.1875 | 0.060606 | 0.064516 | 0.060606 | 0.21875 | 0 | 0.085714 | 0.21212 | 0.029412 | 0 | 0.029412 | 0

## Slide 24: Influence of Time to Rehab on RSL
Chart: 

## Slide 25: Threshold Time to Failure Can be Challenging
Data seems to emanate from to which makes it stochastic.,
Ft vs time
Convex portion of curve
Where to is the location parameter, t1 is the lower
extreme abscissa t2 is upper extreme abscissa tm is
the abscissa corresponding to the mid point of
the convex portion

## Slide 26: US Highways Rehab M. Record Performance
INT= | 3.64
Beta (Shape Parameter)= | 1.32 (Random)
Mu (Scale Parameter)= | 15.7 Years
Chart: Ln (T-4)
| 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.69314718055994529 | 0.69314718055994529 | 0.69314718055994529 | 0.69314718055994529 | 0.69314718055994529 | 0.69314718055994529 | 1.3862943611198906 | 1.3862943611198906 | 1.3862943611198906 | 1.791759469228055 | 1.791759469228055 | 1.791759469228055 | 1.9459101490553132 | 1.9459101490553132 | 1.9459101490553132 | 1.9459101490553132 | 2.0794415416798357 | 2.3978952727983707 | 2.4849066497880004 | 2.4849066497880004 | 2.4849066497880004 | 2.5649493574615367 | 2.7725887222397811 | 2.8332133440562162 | 2.8332133440562162 | 2.8903717578961645 | 2.8903717578961645 | 2.8903717578961645 | 2.8903717578961645 | 2.8903717578961645 | 2.9444389791664403 | 2.9444389791664403 | 2.9444389791664403 | 2.9444389791664403 | 2.9957322735539909 | 2.9957322735539909 | 2.9957322735539909 | 3.044522437723423 | 3.044522437723423 | 3.044522437723423 | 3.0910424533583161 | 3.0910424533583161 | 3.1354942159291497 | 3.1780538303479458 | 3.1780538303479458 | 3.2188758248682006 | 3.2188758248682006 | 3.2958368660043291
LNLN (1-Fx)-1 | -3.0146 | -3.0146 | -2.3345 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.5519 | -1.5519 | -1.5519 | -1.2077 | -1.2077 | -1.2077 | -1.0463 | -1.0463 | -1.0463 | -1.0463 | -0.89152 | -0.46381 | -0.33245 | -0.33245 | -0.33245 | -0.20621 | 0.14441 | 0.25273 | 0.25273 | 0.35715 | 0.35715 | 0.35715 | 0.35715 | 0.35715 | 0.45787 | 0.45787 | 0.45787 | 0.45787 | 0.5551 | 0.5551 | 0.5551 | 0.64902 | 0.64902 | 0.64902 | 0.73979 | 0.73979 | 0.82759 | 0.91257 | 0.91257 | 0.99486 | 0.99486 | 1.1519
Chart: Ln(T-2)
| 0 | 0 | 0.69314718055994529 | 1.0986122886681098 | 1.0986122886681098 | 1.0986122886681098 | 1.0986122886681098 | 1.0986122886681098 | 1.0986122886681098 | 1.3862943611198906 | 1.3862943611198906 | 1.3862943611198906 | 1.3862943611198906 | 1.3862943611198906 | 1.3862943611198906 | 1.791759469228055 | 1.791759469228055 | 1.791759469228055 | 2.0794415416798357 | 2.0794415416798357 | 2.0794415416798357 | 2.1972245773362196 | 2.1972245773362196 | 2.1972245773362196 | 2.1972245773362196 | 2.3025850929940459 | 2.5649493574615367 | 2.6390573296152584 | 2.6390573296152584 | 2.6390573296152584 | 2.7080502011022101 | 2.8903717578961645 | 2.9444389791664403 | 2.9444389791664403 | 2.9957322735539909 | 2.9957322735539909 | 2.9957322735539909 | 2.9957322735539909 | 2.9957322735539909 | 3.044522437723423 | 3.044522437723423 | 3.044522437723423 | 3.044522437723423 | 3.0910424533583161 | 3.0910424533583161 | 3.0910424533583161 | 3.1354942159291497 | 3.1354942159291497 | 3.1354942159291497 | 3.1780538303479458 | 3.1780538303479458 | 3.2188758248682006 | 3.2580965380214821 | 3.2580965380214821 | 3.2958368660043291 | 3.2958368660043291 | 3.3672958299864741
LNLN (1-Fx)-1 | -3.0146 | -3.0146 | -2.3345 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.5519 | -1.5519 | -1.5519 | -1.2077 | -1.2077 | -1.2077 | -1.0463 | -1.0463 | -1.0463 | -1.0463 | -0.89152 | -0.46381 | -0.33245 | -0.33245 | -0.33245 | -0.20621 | 0.14441 | 0.25273 | 0.25273 | 0.35715 | 0.35715 | 0.35715 | 0.35715 | 0.35715 | 0.45787 | 0.45787 | 0.45787 | 0.45787 | 0.5551 | 0.5551 | 0.5551 | 0.64902 | 0.64902 | 0.64902 | 0.73979 | 0.73979 | 0.82759 | 0.91257 | 0.91257 | 0.99486 | 0.99486 | 1.1519
Chart: Ln T-0)
| 0 | 0 | 1.3862943611198906 | 1.6094379124341003 | 1.6094379124341003 | 1.6094379124341003 | 1.6094379124341003 | 1.6094379124341003 | 1.6094379124341003 | 1.791759469228055 | 1.791759469228055 | 1.791759469228055 | 1.791759469228055 | 1.791759469228055 | 1.791759469228055 | 2.0794415416798357 | 2.0794415416798357 | 2.0794415416798357 | 2.3025850929940459 | 2.3025850929940459 | 2.3025850929940459 | 2.3978952727983707 | 2.3978952727983707 | 2.3978952727983707 | 2.3978952727983707 | 2.4849066497880004 | 2.7080502011022101 | 2.7725887222397811 | 2.7725887222397811 | 2.7725887222397811 | 2.8332133440562162 | 2.9957322735539909 | 3.044522437723423 | 3.044522437723423 | 3.0910424533583161 | 3.0910424533583161 | 3.0910424533583161 | 3.0910424533583161 | 3.0910424533583161 | 3.1354942159291497 | 3.1354942159291497 | 3.1354942159291497 | 3.1354942159291497 | 3.1780538303479458 | 3.1780538303479458 | 3.1780538303479458 | 3.2188758248682006 | 3.2188758248682006 | 3.2188758248682006 | 3.2580965380214821 | 3.2580965380214821 | 3.2958368660043291 | 3.3322045101752038 | 3.3322045101752038 | 3.3672958299864741 | 3.3672958299864741 | 3.4339872044851463
LNLN (1-Fx)-1 | -3.0146 | -3.0146 | -2.3345 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -2.1262 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.9266 | -1.5519 | -1.5519 | -1.5519 | -1.2077 | -1.2077 | -1.2077 | -1.0463 | -1.0463 | -1.0463 | -1.0463 | -0.89152 | -0.46381 | -0.33245 | -0.33245 | -0.33245 | -0.20621 | 0.14441 | 0.25273 | 0.25273 | 0.35715 | 0.35715 | 0.35715 | 0.35715 | 0.35715 | 0.45787 | 0.45787 | 0.45787 | 0.45787 | 0.5551 | 0.5551 | 0.5551 | 0.64902 | 0.64902 | 0.64902 | 0.73979 | 0.73979 | 0.82759 | 0.91257 | 0.91257 | 0.99486 | 0.99486 | 1.1519
Location Parameter t0 = 2.5 Years

## Slide 27: Location Parameter for US Highway Rehab
Chart: RSL
| -1 | -1 | 2 | 3 | 3 | 3 | 3 | 3 | 3 | 4 | 4 | 4 | 4 | 4 | 4 | 6 | 6 | 6 | 8 | 8 | 8 | 9 | 9 | 9 | 9 | 10 | 13 | 14 | 14 | 14 | 15 | 18 | 19 | 19 | 20 | 20 | 20 | 20 | 20 | 21 | 21 | 21 | 21 | 22 | 22 | 22 | 23 | 23 | 23 | 24 | 24 | 25 | 26 | 26 | 27 | 27 | 29
cdf | 0.047882 | 0.047882 | 0.092312 | 0.11245 | 0.11245 | 0.11245 | 0.11245 | 0.11245 | 0.11245 | 0.13554 | 0.13554 | 0.13554 | 0.13554 | 0.13554 | 0.13554 | 0.19092 | 0.19092 | 0.19092 | 0.25835 | 0.25835 | 0.25835 | 0.29618 | 0.29618 | 0.29618 | 0.29618 | 0.33637 | 0.46681 | 0.51187 | 0.51187 | 0.51187 | 0.55677 | 0.68505 | 0.72405 | 0.72405 | 0.76051 | 0.76051 | 0.76051 | 0.76051 | 0.76051 | 0.79417 | 0.79417 | 0.79417 | 0.79417 | 0.82485 | 0.82485 | 0.82485 | 0.85246 | 0.85246 | 0.85246 | 0.87699 | 0.87699 | 0.89851 | 0.91715 | 0.91715 | 0.93309 | 0.93309 | 0.95776
t1=12; tm=18; t2 =28 Therefore t0=3

## Slide 28: Bandaids are not Cost Effective
Perform CPR:
Regrades are Very Expensive
Notes: 1) Pavement Distress

## Slide 29: Acknowledgements
Glenn Engstrom
Jeff Brunner
Curt Turgeon
Dave Janisch
Debaroti Ghosh
Brandon Ong
MnDOT District Materials Engineers

## Slide 30
Thank You