## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Utilization of MnROAD as part of NCHRP 24-45: Evaluating Mechanical Properties of Earth Material During Intelligent Compaction
+ 46 Associate Members
Soheil Nazarian, PhD, PE, D.GE
Professor, The University of Texas at El Paso
How lucky we are to have access to MnROAD and have NRRA as partner

## Slide 2: Goal of Project
“to develop procedure(s) that measure
mechanical properties
of earth materials to
facilitate adoption
of IC technologies for field
acceptance”
Straightforward specification
Solid to minimize dispute
E (modulus)?
k (stiffness)?
Thank you Caterpillar

## Slide 3: Calibration of Forward Model
Simulation of Roller Measurements
Select Roller Parameters
Select Material Type for Layers
Estimate Layer Properties
Chart: Displacement, mm
| 1.57 | 0.67 | 0.33
Field Data | 0 | 0.6 | 1.2
FE Model | 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2 | 2.3 | 2.4 | 2.5

## Slide 4: Test Strip at MnROAD Low Volume Road
185
186
188
189
Geophones and
Pressure Cells Locations
9 @ 7.5 m (25 ft) spacing
70 m (225.5 ft)
9 @ 7.5 m (25 ft) spacing
70 m (226 ft)
Cell 186
Cell 185
9 @ 7.5 m (25 ft) spacing
70 m (226 ft)
9 @ 7.5 m (25 ft) spacing
70 m (226.5 ft)
Cell 188
Cell 189
Cell 187
A
B
C
D
2.1 m (7 ft)
2.1 m (7 ft)
2.1 m (7 ft)
Spot test (LWD, DCP)
North Side
South Side
MnROAD Low Volume Road

## Slide 5: Components of UTEP Developed Data Acquisition System (DAQ)
Data Acquisition Box and Laptop
Accelerometer
3D Geophone
Pressure Cell
3D Geophone
Accelerometer
GPS
Pressure Cell

## Slide 6: Instrumentation of IC Roller for Mapping
RTK GPS
Mounted
Accelerometers
Accelerometers and Connections to DAQ
Smooth Drum IC Rollers
Mounting Accelerometers

## Slide 7: Installation of Ground Sensors
300 mm (12 in.)
Coarse RCA
90 mm (3.5 in.)
Select Granular Borrow
Subgrade
Sand
300 mm (12 in.)
Fine RCA
90 mm (3.5 in.)
Select Granular Borrow
Subgrade
Sand
90 mm (3.5 in.)
Select Granular Borrow
Subgrade
Clay
Subgrade
Clay
150 mm
(6 in.)
Cell 185
Cell 186
Cell 188
Cell 189
Geophone
Pressure Cell
300 mm
(12 in.)
300 mm
(12 in.)
150 mm
(6 in.)
600 mm
(24 in.)
*Not to scale
300 mm (12 in.)
Recycled Aggregate Base Class 6
90 mm (3.5 in.)
Select Granular Borrow
300 mm (12 in.)
Limestone Aggregate Base Class 6
Embedding 3D Geophones
Embedding Pressure Plate

## Slide 8: Vibration Data Collection Process
Closer view of time-record of acceleration
Time-record of velocity data
from embedded geophone
Closer view of time-record of velocity
Fast Fourier Transform
Time domain
Frequency domain
Time-record of acceleration data
from mounted accelerometer

## Slide 9: Vibration Response of Mounted Accelerometer
28 Hz Vibration Frequency (Standard) – Low Amplitude
Chart: Cell 185, Line B
Chart: Cell 186, Line B
Amplitude

## Slide 10: Vertical Response of Embedded Sensors
Chart: Distance from Geophone, ft
Moving Direction

## Slide 11: Calibration of Forward Model
Simulation of Roller Measurements
Select Roller Parameters
Select Material Type for Layers
Estimate Layer Properties
Chart: Field Measured Displacement, mm
| 2.4700000000000002 | 1.35 | 0.74 | 0.49006622516556292 | 0.25165562913907286 | 0 | 3.1 | 1.05 | 0.56000000000000005 | 1.38 | 0.63 | 0.32 | 1.57 | 0.67 | 0.33 | 0.79 | 0.28000000000000003 | 0.16
Fe Model (Disp_mm) | 6.5865 | 3.1494 | 1.6643 | 0.94736 | 0.4186 | 0.21966 | 5.2555 | 2.4895 | 1.3137 | 3.7328 | 1.7454 | 0.91958 | 5.3046 | 2.5137 | 1.3266 | 3.623 | 1.6924 | 0.89145
Line of Equality | 0 | 8
+/- 25% Uncertainty Bounds | 0 | 12.05
+/- 25% Uncertainty Bounds | 0 | 7.23
Chart: Displacement, mm
| 1.57 | 0.67 | 0.33
Field Data | 0 | 0.6 | 1.2
FE Model | 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2 | 2.3 | 2.4 | 2.5

## Slide 12: IC Mapping
CMV
Frequency (Hz)
Coefficient of Variation of CMV
Speed (mph)
> 35%
25% < COV < 35%
< 25%
Color Code of Coefficient of Variation of CMVs
Cell 188 – Subgrade, Clay

## Slide 13: Performing Spot Tests
Light Weight Deflectometer
(LWD)
Dynamic Cone Penetrometer
(DCP)
Falling Weight Deflectometer
(FWD)
Nuclear Density Gauge (NDG)

## Slide 14: Spot Test Moduli
CMV
LWD
Modulus (ksi)
FWD
Modulus (ksi)
Cell 188 – Subgrade, Clay
D
C
A
B
Stiffness from Roller

## Slide 15: Thank you!! Can you help us with a site for Phase III?
nazarian@utep.edu or (915) 747-6911

## Slide 16
Thank You