## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Quantifying Moisture in Granular Materials for Mechanistic Pavement Design
Soheil Nazarian, PhD, PE, DGE
Professor of Civil Engineering, UTEP
+ 46 Associate Members

## Slide 2: Behavior of Soils (from Unsaturated Soil Principles)
Sr = w Gs rd/( Gs rw – rd)
Gs = specific gravity
rd = dry mass density
rw = mass density of water
Degree of Saturation, % | 120
 | 115
 | 110
 | 105
 | 100
 | 95
 | 90
 | 85
 | 80
 | 75
 | 70
 | 65
 | 60
 | 55
 | 50
 | 45
 | 40
 | 35
 | 30
 | 25
 | 20
 | 15
 | 10
 | 5
 | 0
 |  | Moisture Content, % |  |  |  |  |  |  |  |  |  | 
 |  | 5% | 7% | 9% | 11% | 13% | 15% | 17% | 19% | 21% | 23% | 25%
Dry Density, pcf | 90 | 15% | 22% | 28% | 34% | 40% | 46% | 53% | 59% | 65% | 71% | 77%
 | 95 | 17% | 24% | 31% | 38% | 45% | 52% | 59% | 66% | 72% | 79% | 86%
 | 99 | 19% | 27% | 35% | 43% | 50% | 58% | 66% | 74% | 81% | 89% | 97%
 | 104 | 22% | 31% | 39% | 48% | 57% | 66% | 74% | 83% | 92% | 101% | 109%
 | 109 | 25% | 35% | 45% | 55% | 65% | 75% | 85% | 95% | 105% | 115% | 125%
 | 115 | 29% | 40% | 52% | 64% | 75% | 87% | 98% | 110% | 121% | 133% | 145%
 | 121 | 34% | 48% | 61% | 75% | 88% | 102% | 116% | 129% | 143% | 156% | 170%
 | 127 | 41% | 57% | 74% | 90% | 106% | 123% | 139% | 155% | 172% | 188% | 204%
 | 133 | 51% | 71% | 91% | 111% | 131% | 152% | 172% | 192% | 212% | 233% | 253%
 | 140 | 65% | 91% | 118% | 144% | 170% | 196% | 222% | 248% | 274% | 300% | 327%
 | 147 | 90% | 127% | 163% | 199% | 235% | 271% | 308% | 344% | 380% | 416% | 452%
 | 154 | 143% | 200% | 257% | 314% | 371% | 428% | 486% | 543% | 600% | 657% | 714%

## Slide 3: Estimating Design Modulus
Determine nonlinear parameters k1 through k3 for each material
Conducting laboratory resilient modulus tests before structural design
Utilizing results from a catalog of most common soils that have been tested
Estimating modulus based on calibrated models that are functions of index parameters
Using presumptive design values based on experience
Best Option Worst Option
θ = bulk stress
τoct = octahedral shear stress
Pa = atmospheric pressure
k1,2,3 = regression constants

## Slide 4: Laboratory Tests

## Slide 5
Loading Sequence (Base)
NCHRP 1-28A
AASHTO T-307

## Slide 6
Resilient Modulus (Base)
Chart: Stress Path for Base AASHTO T-307
| 21.75
Preconditioning | 6.75
Stress Path | 1.35 | 2.7 | 4.05 | 2.25 | 4.5 | 6.75 | 4.5 | 9 | 13.5 | 4.5 | 6.75 | 13.5 | 6.75 | 9 | 18
Chart: Stress Path for Base NCHRP 1-28A
| 30
Preconditioning | 15
Modified Stress Path | 0.75 | 1.5 | 2.5 | 3.75 | 5 | 1.5 | 3 | 5 | 7.5 | 10 | 3 | 6 | 10 | 15 | 20 | 4.5 | 9 | 15 | 22.5 | 30
There is a need once and for all to standardize MR Test

## Slide 7: Factors Impacting Modulus
State of Stress
Moisture Content (Suction, Degree of Saturation)
  at compaction
  at testing
Density
Gradation and Plasticity

## Slide 8: Calibrated Models for Estimating Modulus
Model Type | Developed by | Gradation and Plasticity Parameters Included
 | Malla and Joshi (2008) | Percent passing 3” sieve Percent passing 1” Percent Passing 1.5 “ sieve Percent passing #40 sieve Percent passing #10 sieve Percent fine sand Percent passing #200 sieve CU=Uniformity coefficient CC= Coefficient of curvature
 | Santha (1994) | S40=Percent passing sieve No.40 Percent of clay Percent of silt Percent of swell Percent shrinkage Liquid limit and plastic limit
 | Glover and Fernando (1995) | Liquid limit and plastic limit Specific gravity of soil binder Percent passing number 40 Dialectic constant
 | Mohammad (1999) | Liquid limit and plastic limit
 | Amber (2002) | Percentage passing sieve #3/8 Percentage passing #4 Percentage passing #40 Liquid limit and plastic limit
State of Stress
Index Properties

## Slide 9: Major Moisture Models Considered
MEPDG (well publicized)
Zapata (Modification of MEPDG to be soil dependent)
3. Siekmeier (Incorporates SWCC)

## Slide 10: Verification of Moisture Model from Lab Results
Chart: S-Sopt, %
| -32.157277501339991 | -12.61924865713388 | 0 | 3.0041306432026298 | 3.7038719415183579
GW | 1.1985 | 1.2729 | 1 | 0.69356 | 0.84575
ML | 1.1405 | 1.0489 | 1 | 0.9815 | 0.8765
GP | 1.4325 | 1 | 0.97666
SC | 2.1893 | 1.33 | 1 | 0.46924 | 0.27214
CH | 1.0626 | 0.94854 | 1 | 0.66238 | 0.52973
CL | 0.91797 | 1.139 | 1 | 0.91429 | 0.88783
Chart: S-Sopt, %
| -32.157277501339991 | -12.61924865713388 | 0 | 3.0041306432026298 | 3.7038719415183579
GW | 1.1985 | 1.2729 | 1 | 0.69356 | 0.84575
CL | 0.91797 | 1.139 | 1 | 0.91429 | 0.88783
GP | 1.4325 | 1 | 0.97666
ML | 1.1405 | 1.0489 | 1 | 0.9815 | 0.8765
SC | 2.1893 | 1.33 | 1 | 0.46924 | 0.27214
CH | 1.0626 | 0.94854 | 1 | 0.66238 | 0.52973
Zapata
MEPDG
Chart: Error, %
| 0 | 10% | 20% | 30% | 40% | 50% | More
Zapata Model | 0 | 0.52174 | 0.6087 | 0.73913 | 0.82609 | 0.82609 | 1
MEPDG Model | 0 | 0.33333 | 0.45833 | 0.58333 | 0.66667 | 0.75 | 1
Zapata Model (wPI=0) | 0 | 0.59091 | 0.72727 | 0.81818 | 0.81818 | 0.90909 | 1

## Slide 11: Field Tests
Light Weight Deflectometer
(LWD)
Dynamic Cone Penetrometer
(DCP)
Falling Weight Deflectometer
(FWD)
Nuclear Density Gauge (NDG)

## Slide 12: Recommended Moisture Models
Chart: Error, %
| 0 | 10% | 20% | 30% | 40% | 50% | More
Zapata Model | 0 | 0.39655 | 0.51724 | 0.60345 | 0.67241 | 0.74138 | 1
MEPDG Model | 0 | 0.37931 | 0.56897 | 0.65517 | 0.82759 | 0.89655 | 1
Zapata Model (wPI=0) | 0 | 0.65517 | 0.86207 | 0.93103 | 0.94828 | 0.94828 | 1
Based on Small Scale Tests
Chart: Error, %
| 0 | 10% | 20% | 30% | 40% | 50% | More
Zapata Model | 0 | 0.52174 | 0.6087 | 0.73913 | 0.82609 | 0.82609 | 1
MEPDG Model | 0 | 0.33333 | 0.45833 | 0.58333 | 0.66667 | 0.75 | 1
Zapata Model (wPI=0) | 0 | 0.59091 | 0.72727 | 0.81818 | 0.81818 | 0.90909 | 1
Based on Lab Tests

## Slide 13: Impact of Moisture Content at Time of Testing relative to Moisture Content at time of Compaction: Prepared at OMC
Chart: Moisture Content at Testing
| 0.7 OMC | 0.8 OMC | 0.9 OMC | OMC | 1.1 OMC | 1.2 OMC
Compacted at OMC | 101.6683 | 75.8774 | 47.5296 | 26.161
Constant Density Specimens prepared at MDD

## Slide 14: Impact of Moisture Content at Time of Testing relative to Moisture Content at time of Compaction: Prepared at OMC and 1.2 OMC
Chart: Moisture Content at Testing
| 0.7 OMC | 0.8 OMC | 0.9 OMC | OMC | 1.1 OMC | 1.2 OMC
Compacted at 1.2 OMC | 136.6868 | 95.7905 | 44.0082 | 31.4678 | 18.3996 | 13.5487
Compacted at OMC | 101.6683 | 75.8774 | 47.5296 | 26.161
Constant Density Specimens prepared at MDD

## Slide 15: Impact of Moisture Content at Time of Testing relative to Moisture Content at time of Compaction: Prepared at OMC, 1.2OMC and -1.2 OMC
Chart: Moisture Content at Testing
| 0.7 OMC | 0.8 OMC | 0.9 OMC | OMC | 1.1 OMC | 1.2 OMC
Compacted at 1.2 OMC | 136.6868 | 95.7905 | 44.0082 | 31.4678 | 18.3996 | 13.5487
Compacted at OMC | 101.6683 | 75.8774 | 47.5296 | 26.161
Compacted at 0.8 OMC | 32.4621 | 32.6079
Constant Density Specimens prepared at MDD

## Slide 16: Impact of Moisture Content at Time of Testing relative to Moisture Content at time of Compaction: Recommended Model: MEPDG with a = -0.1119, b = 0.7887 and km = 12.372
Chart: S-Sopt. ,%
0.8 OMC | 1.3106 | 1.3047 | 2.4141 | 2.601
0.9 OMC | 1.0873 | 1.1556 | 1.5322 | 1.9396 | 1.9741 | 2.4651 | 3.0708 | 3.6394 | 4.0336 | 4.2543
OMC | 1 | 1.0515 | 1.9103 | 2.1793 | 2.2873 | 3.0497 | 4.0863 | 5.0338 | 5.522 | 5.8727
1.1 OMC | 0.66225 | 0.70347 | 0.92736 | 1.1831 | 1.2665 | 1.5759 | 2.0728 | 3.0906 | 4.3651 | 5.3157
1.2 OMC | 0.54455 | 0.56724 | 0.73952 | 0.97938 | 0.98755 | 1.2648 | 1.7688 | 2.5745 | 3.85 | 5.4938 | 6.4212
98% MDD | 1.4708 | 1.4532 | 1.4457 | 1.5299 | 1.6172 | 1.6606 | 1.8878 | 2.0732 | 2.164 | 2.4138
96% of MDD | 1.1235 | 1.2839 | 1.3086 | 1.2732 | 1.2684 | 1.305 | 1.3541 | 1.5193 | 1.5457 | 1.6628
Chart: Error, %
| 0 | 10% | 20% | 30% | 40% | 50% | More
Zapata | 0 | 0.56757 | 0.75676 | 0.91892 | 0.97297 | 0.97297 | 1
MEPDG Fine | 0 | 0.56757 | 0.72973 | 0.72973 | 0.83784 | 0.89189 | 1
Modified MEPDG Fine | 0 | 0.7027 | 0.86486 | 0.97297 | 0.97297 | 1 | 1
Zapata (wPI=0) | 0 | 0.21622 | 0.35135 | 0.59459 | 0.72973 | 0.81081 | 1

## Slide 17: Impact of Moisture Content at Time of Testing relative to Moisture Content at time of Compaction
Chart: MCCompaction-MCTesting, %

## Slide 18: Thank you

## Slide 20: Conclusions and Observations
Impact of moisture content of base and subgrade should be considered in terms of change in
  Degree of Saturation (more fundamentally correct)
  Moisture content (better understood in Pavement Geotechnics)
Pavements should be designed by considering
  Laboratory Test Results (for major projects)
  Quality of construction (for major as well as minor projects)

## Slide 21: Thank you!!
nazarian@utep.edu or (915) 747-6911

## Slide 22
Thank You