## Slide 1: 2018 Pavement Workshop May 23-24, 2018
I-FIT and Overlay Test Update
Brian Pfeifer
Engineer of Materials
+ 46 Associate Members

## Slide 2: I-FIT Results
Chart: Flexibility Index
| SPWED440E | SPWED430I | SPWEA440E | SPWEB340C | SPWEB430E | SPWEB450E | SPWEB440E | SPWEC440E
 | 18 | 26.4 | 18.6 | 18.2 | 14.8 | 25.8 | 22.6 | 15.7
White – 4.75mm NMAS
Orange – 9.50mm NMAS
Blue – 12.5mm NMAS
Gray – 19.0mm NMAS
Notes: The information in each box at the bottom of each bar represents the asphalt contents determined by MnDOT and sent to each participating lab
  The 6.1% AB shown for SPWED440E was also verified at the IDOT CBM HMA lab
The error bars represent one standard deviation on either side of the average FI value
Typical FI trends were seen with increased asphalt binder content in both 4.75mm and 12.5mm mixtures
  SPWED440E and SPWED430I in 4.75mm mixtures
  SPWEB430E and SPWEB450E in 12.5mm mixtures
Last, but not least, all mixtures produced FI values well above the 8.0 minimum threshold considered in Illinois
  These mixtures would be expected to perform well in terms of cracking resistance

## Slide 3: I-FIT – Effect of Total Binder Content
Chart: Total Binder Content (%)
| 6.1 | 8.4
4.75mm NMAS | 18 | 26.4
9.50mm NMAS | 18.6
12.5mm NMAS | 18.2 | 14.8 | 25.8 | 22.6
19.0mm NMAS | 15.7
Notes: The graph shows the effect of total asphalt binder content on FI
The white, orange, blue, and gray circle colors represent the different nominal maximum aggregate size mixtures tested
FI generally trended with total asphalt binder content
  4.75mm mixtures, noting only two data points were available, saw increased FI with increased total binder content
  12.5mm mixtures generally saw increased FI with increased total binder content
  Similar trend seen with effective asphalt binder content

## Slide 4: Overlay Test Results
Chart: Texas Overlay Test
| SPWED440E | SPWED430I | SPWEA440E | SPWEB340C | SPWEB430E | SPWEB450E | SPWEB440E | SPWEC440E
 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000
White – 4.75mm NMAS
Orange – 9.50mm NMAS
Blue – 12.5mm NMAS
Gray – 19.0mm NMAS
Notes: Overlay tests were completed according to TEX-248-F procedure
  Note that the tests were ran to 2,000 cycles as opposed to the TEX-248-F procedure maximum of 1,000 cycles using a 93% load reduction criteria
All mixtures ran out to 2,000 cycles
  If the cycle count is the only criteria, it would be challenging to delineate between mixtures
  Mixture load reduction percentages were plotted vs. cycle count to further analyze the data

## Slide 5: Overlay Test – Load Reduction Plot
Chart: Cycles
Notes: The largest difference using this plotting method was seen with SPWED430I (4.75mm mix with the highest FI)
Other mixtures were a bit more challenging to delineate based on Load Reduction Percentage vs. Cycle Count

## Slide 6
Thank You