## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Cold Central Plant Recycling (CCPR)
David Rettner
President and Principal Engineer
American Engineering Testing, Inc.
+ 46 Associate Members

## Slide 2: What is CCPR?
5/24/2018 | NRRA Workshop | 2
CIR methods with stockpiled RAP
Add binder as required
Pave as usual
CCPR vs CIR
Avoids possible concerns about in-place material
Using stockpiled material reduces variability
  Fractionating the RAP can produce a more consistent material
Additional costs of CCPR for hauling, storing, processing, etc

## Slide 3: Project Objectives
5/24/2018 | NRRA Workshop | 3
Survey NRRA members about CCPR practice, costs, and needs
Laboratory testing and analysis of MnROAD CCPR
Summary of MnROAD CCPR field performance
Technical briefs summarizing:
  CCPR state of the practice
  CCPR costs
  CCPR characterization and testing

## Slide 4: MnROAD field sections
5/24/2018 | NRRA Workshop | 4
Single-source, non-fractionated RAP
Constructed in Fall 2017
Compacted CCPR had final average thickness of 3.5”
Placed on 12” Class 6, clay/loam subgrade
CELL | SURFACE | SPEC | BINDER | LTC req.
133 | Double chip seal FA-3/FA-2.5 | Emulsion (58S-28) | CIR-EE (H) | -21.4°C
233 | Double chip seal FA-3/FA-2.5 | Foam (58S-28) | 58S-28 | -21.4°C
135 | 1.5” HMA SPWEB340C | Foam (XX-34) | 52-34 | -21.4°C
235 | 1.5” HMA SPWEB340C | Emulsion (XX-34) | CIR-TEC M | -21.4°C

## Slide 5: Mix Designs
5/24/2018 | NRRA Workshop | 5
BINDER TYPE | Emulsion | 
MnROAD CELL | 133 | 135
SURFACING | DCS | 1.5" SP
PG | 58S-28 | XX-34
BINDER ADDED, % | 2.0 | 
Voids @ Opt, % | 11.5 | 11.7
Max Dens @ Opt, pcf | 133.1 | 132.8
Marshall @ Opt, lbs | 1272 | 1365
Ret. Stability @ Opt, % | 72.1 | 71.0
Raveling, % | 1.60 | 1.70
Est Crit Crack Temp, °C | -35 | -36
IDT @ CC Temp, psi | 155 | 158
Developed at AET in Summer 2017
Exceeded low temp req of -21.4°C
Exceeded dry stability of 1250 lb
While no MnDOT requirement for raveling, foamed mixes did not meet target of 2.0%

## Slide 6: Mix Designs
5/24/2018 | NRRA Workshop | 6
BINDER TYPE | Foamed | 
MnROAD CELL | 233 | 235
SURFACING | DCS | 1.5" SP
PG | 58S-28 | XX-34
BINDER ADDED, % | 1.5 | 
Voids @ Opt, % | 12.2 | 10.8
Max Dens @ Opt, pcf | 131.8 | 133.8
Marshall @ Opt, lbs | 1311 | 1272
Ret. Stability @ Opt, % | 70.4 | 73.2
Raveling, % | 3.30 | 2.50
Est Crit Crack Temp, °C | -34 | -34
IDT @ CC Temp, psi | 128 | 132
Developed at AET in Summer 2017
Exceeded low temp req of -21.4°C
Exceeded dry stability of 1250 lb
While no MnDOT requirement for raveling, foamed mixes did not meet target of 2.0% of emsulsion mixes

## Slide 7: Challenges to lab tests
5/24/2018 | NRRA Workshop | 7
Building on past studies in CCPR materials
AET experience adapting SCB/IDT to test CIR samples
Obtaining viable samples
Actual LLD gauge measuring range

## Slide 8: Materials for sample preparation
5/24/2018 | NRRA | 8

## Slide 9: MnROAD Performance: Cell 233
April 2018
Cell 233
Foamed 58S-28, Double Chip
5/24/2018 | NRRA Pavement Workshop | 9
March 2018
Based on Cell 233, lab work started with foamed 58S-28

## Slide 10: MnROAD Performance: Cell 133
5/24/2018 | NRRA Pavement Workshop | 10
May 2018
Cell 133
Emulsion 58S-28, Double Chip

## Slide 11: Research products & timeline
5/24/2018 | NRRA Workshop | 11
Surveys
Summaries of
  State of practice
  Performance testing and analysis
  Spec recommendations
Final report

## Slide 12
Principal Investigator | Technical Liaison
David Rettner, AET | Dave Van Deusen, MnDOT