## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Patching Materials for Partial Depth Repair of Concrete Pavements John Roberts
Executive Director IGGA/ACPA CP3
+ 46 Associate Members

## Slide 2: Introduction
John H. Roberts
Executive Director - International Grooving and Grinding Association
Vice President – American Concrete Pavement Association’s Concrete Pavement Preservation Partnership (CP3)

## Slide 3: International Grooving & Grinding Association
Industry association founded in 1972
Comprised of contractors, manufacturers, suppliers, consultants and public officials
Partnering to promote, strengthen and advance the industry
Affiliated with ACPA in 1995 to represent their newly formed Pavement Restoration Division

## Slide 4: IGGA Mission and Vision
IGGA mission:
The mission of the International Grooving and Grinding Association (IGGA) is to serve as the leading technical resource for acceptance and proper use of diamond grinding and grooving as well as concrete pavement preservation and restoration.
IGGA vision:
IGGA seeks to be recognized internationally as a leading authority of pavement surface characteristics and PCC pavement preservation/restoration.

## Slide 5: IGGA Current Status
Offices located in NY, Chicago and Arizona
Staffing:
  Executive Director
  Office Manager
  Director of Engineering and Research – Mesa AZ
  Consultant Promoters
  Constructive Communications Inc.
  Shared Staff with ACPA

## Slide 6: Scope of Services
Research and Development (e.g. NGCS)
Technical Service
Marketing
Communications
Public Relations
Guideline and Specification Development
Membership Recruitment
Market Measurement

## Slide 7: IGGA Core Markets
Diamond Grinding
Safety Grooving (Highways)
Runway Grooving
Dowel Bar Retrofit
Full Depth Repair
Partial Depth Repair
Slab Stabilization
Joint Resealing
Cross/Slot Stitching

## Slide 8: International Market Development
Australia
Austria
Canada
China
Czech Republic
England
Germany
Hong Kong
Hungry
Indonesia
Japan
Korea
Mexico
Poland
Russia

## Slide 9: Strategic Partnerships
American Concrete Pavement Association
ACPA Affiliated Chapter/State Paving Associations (21)
National Concrete Pavement Technology Center
Portland Cement Association
National Road Research Alliance

## Slide 10: Patching Materials for PDR of PCCP
Objective: To provide a guide for NRRA members and other agencies to establish an effective partial depth repair program. The final report will guide the reader through product selection, installation techniques, equipment needed for completing the repair, typical performance cost, along with the life expectancy of the repair products.

## Slide 11: Design
Ensure that the installation of each material reflects work typically done by maintenance personnel.
Achieve 3 to 5 years of service life with 2 – 4 hr. cure.
PDR constructed on WB lanes of I-94 built in 1973 as 9-inch PCCP w/ skewed 27-foot transverse joints.
A total of 15 test sections consisting of three contiguous panels and two transition panels, one at either end.
Seven different patch types were created
Thirteen different proprietary products were offered by vendors for evaluation. Additionally, asphalt patching mix was used in two of the 15 sections.

## Slide 12: Typical Layout for PDR Study

## Slide 13: General Installation and Workflow
Joint distresses were created prior to preparation with a milling machine by a local vendor under contract.
MnDOT District 3 Maintenance staff performed minimal preparation (i.e., sand blasting) and installed materials.
Manufacturers were present onsite in most cases but the intent of the research is to reflect the performance the patch materials under the actual installation conditions (maintenance personnel, simple tools).
Three consecutive panels allocated for each product.

## Slide 14: Patching Material Manufacturers
CTS Rapid Set – DOT Repair Mix
SpecChem – Rep Con 928
Western Material and Design – FasTrac 246
D.S. Brown - PaveSaver Polymeric Concrete
Western Material and Design - CE 700 HPC
Willamette Valley Company – FastPatch
Five Star - Rapid Surface Repair Easy Mix
Five Star - Rapid Surface Repair Epoxy Fix

## Slide 15: Patching Material Manufacturers
TCC Materials - ProSpec Concrete Patching Mix
Aqua Patch Road Materials - Aqua Patch
Crafco - HP Concrete Cold Patch
Crafco - Techrete-TBR
TCC - 3U18 Modified
USG – Ecofix
CTS, Rapid Set DOT Repair Mix and Helix 5-25-Standard BA (Zinc Coated) and Helix 5-25-SS BA (Stainless Steel)

## Slide 16: What Can We Expect?
The final report will include technical data sheets, manufacturer recommended time to reach required opening strength under varying conditions, etc.
Specific procedures for each patch were documented by field personnel and will be included in the final report.
Products will be monitored for performance over time.
This information, along with other follow-up data requests, will be compiled, analyzed, and included with the final project report to be prepared by the consultant.
Current practices for PDR used by NRRA agency members will be compiled and summarized.

## Slide 17: What’s Next?

## Slide 18
Thank You