## Slide 1: 2018 Pavement Workshop May 23-24, 2018
Evaluation of Spray Applied Rejuvenators and Surface Sealers; a First Look
Phil Ruffus
Senior Pavement Specialist –MoDOT
Phillip.ruffus@modot.mo.gov
+ 46 Associate Members

## Slide 2
Overview Evaluation of Rejuvenators and Surface Sealing Products to Extend Asphalt Pavement Life
Presentation to:
NRRA Pavement Workshop
May 23, 2018

## Slide 3: Objective & Goals
Objective:
  Provide MoDOT with recommendations for creating a performance-based specification for rejuvenating or surface sealing products used to extend the life of asphalt concrete mixtures.
Project Goals:
  Determine if these penetrating sealers extend asphalt pavement life and to quantify the expected length of extending pavement service life.
  If service life is extended; Determine if the added cost to apply these materials to the wearing surface is cost-effective.
  If cost is offset – quantify and prepare a draft performance based specification, as well as establish recommendations to apply the sealers in terms of selecting those projects with features that will provide the best value to Missouri.

## Slide 4: Major Tasks/Activities
Request for Proposal: May 2017
Consultant Selection: Applied Research Associates
Kickoff meeting with Industry: February 2018
Data Collection: Pre-Application of Rejuvenators and Sealers: April 2018
Product Application:
  Application along mainline - May 2018, except for 3 test sections along route N.
  Application along centerline joint – September 2017
Post Application Investigation - ONGOING.
Prepare Final Report and Project Documentation.

## Slide 5: Pre-Application Testing
Mainline Sections:
Distress surveys - PaVision
Friction testing; ASTM E274 using FN40R
Field permeability tests
Wear resistance
Cores
Centerline Joint Sections:
Distress surveys – PaVision
Joint width
Field permeability tests
Reflectivity tests
Wear resistance, visual

## Slide 6: Pre-Application Testing: Cores
Mainline Sections Only:
AASHTO T 300 – Force Ductility Test
AASHTO T 315 – Dynamic Shear Rheometer Test
AASHTO T 350 – Multiple Stress Creep Recovery Test

## Slide 7: Locations of Test Sections
Mainline Sections:
Route N in St. Charles County
Centerline Joint Sections:
Route 30 in Jefferson County
Route 52 in Morgan County

## Slide 9: Mainline Test Section Layout - Example

## Slide 10: Centerline Joint Test Section Layout - Example

## Slide 11: Material Suppliers Included in Study
Mainline Sections:
Asphalt Materials, Inc.; RPE
Asphalt Systems, Inc.; GSB-Friction Seal
Asphalt Systems Ohio; Biorestor
BlackRoads; MSS-P, RoadLock I, RoadLock II, and RoadLock III
Corrective Asphalt Materials; CRF Maltene Seal and Reclamite Malene
Hutchens Construction; Onyx
Unique Paving Materials; RavelCheck
Control Sections

## Slide 12: Material Suppliers Included in Study
Centerline Joint Sections:
Asphalt Materials; RPE
Asphalt Systems Ohio; Biorestor
BlackRoads; LCJ 100
Corrective Asphalt Materials, Joint Bond
Unique Paving Materials; RavelCheck
Control Sections

## Slide 13: Processes Included on Mainline Project
Single step application process
Multi-step application process
Single Step Process
Multi-Step Process

## Slide 14: Activities During Application
Mainline Sections:
Photographs and videos of application process.
1-gallon sample of material.
Pads for application rates.
Centerline Joint Sections:
Photographs and videos of application process.
1-gallon sample of material.
Reflectivity testing, if applicable.
Pads for application rates, only Route 30:
  Route 52 – pads were eliminated because of pending rain.

## Slide 15: Water-Based Field Permeability Test

## Slide 17: Friction Testing

## Slide 18: Cracking/Condition Maps
Route N, mainline
Routes 30 and 52, centerline joint

## Slide 19: Monitoring Product Application Rates
Pads removed after product application
Pads placed prior to product application

## Slide 20: Why study was sponsored by MODOT
Do rejuvenators/sealers extend the life and/or reduce the maintenance cost of asphalt pavements, and if they do, is the application expense cost effective?
How does the use of rejuvenators/sealers ultimately fit into the MoDOT Asset Management Plan?
Ultimately, can we classify these products and assign them a spot on the Prequalified Products List?

## Slide 21: What questions/answers does MoDOT expect?
The following are some examples from other studies that have been completed.

## Slide 22: Q1: Is the friction significantly affected by applying the product to the pavement surface, and if so, what is the magnitude of the effect?

## Slide 23: Q2: How does permeability change over time with and without the products being applied at the surface?

## Slide 24: Q3: How does the surface distress change over time with and without the products in terms of cracking and other defects?

## Slide 25: Q4: Control versus Treated Sections: Can the distress be quantified for use in predicting the overall performance of the flexible pavement for use in determining the cost benefit of the product?

## Slide 26: Q5: Can we realistically establish a Life Cycle Cost Analysis?
Equivalent annual pavement costs.
Cost differential for treated surface to be cost effective.

## Slide 27: Final Thoughts

## Slide 28
Thank You
Questions?