## Slide 1: 2018 Pavement Workshop May 23-24, 2018
CONCRETE PAVEMENT JOINT DISTRESS
(Cause and Mitigation)
Gordon L. Smith, PE
Associate Director
National Concrete Pavement Technology Center
+ 46 Associate Members

## Slide 2: A Touch of History
Pavement jointing methods and designs have evolved over the past century plus.
In 1952, air entrainment was required to mitigate freeze-thaw damage.
D-cracking was researched extensively and poor aggregate sources identified in the 1970s+
Early 1990’s saw incidents of “early joint deterioration” leading to more research into vibration, air content, saturation levels, and expansion of paste via calcium oxychloride.
Moscow Road 2014
Built in 1914, 18’ wide, no longitudinal joint, 25’ formed transverse joints

## Slide 3: Materials Related Distress (Reactive & Expansive)

## Slide 4: Loss of Support/Load Transfer

## Slide 5: Load Transfer Failures

## Slide 6: Curling and Warping

## Slide 7: Compression Failures/Spalling

## Slide 8: The New Challenges -
Notes: Every joint or just transverse

## Slide 9: Striving for more durable concrete for today’s pavement environments
Notes: Shadowing leading to severe distress

## Slide 10: The Clues . . . .
Predominately in cold, wet places
Notes: Zone 1

## Slide 11: Types and Mechanisms of Joint Deterioration
Saturated Freeze-thaw Damage
Volume of pores
  Measure mass change from oven dry to vacuum saturated
Degree of saturation
  Compare mass of sample with oven dry and saturated masses
Sorption / Saturation
  ASTM C 1585 (modified)
Jason Weiss

## Slide 12: Types and Mechanisms of Joint Deterioration
Calcium Oxychloride Formation, Expansion, and Damage
Chemical Reaction
  Calcium chloride and calcium hydroxide forms calcium oxychloride – cracking due to volume change
Mitigate
  Use SCMs
  Reduces calcium hydroxide
  Use low w/c ratios to reduce fluid transport
  Proper entrained air-void system

## Slide 13: The Causes
Saturation/freeze thaw
Oxychloride formation
Sawing practice
Notes: Summary of the problem

## Slide 14: Saturation
Damage occurs where the concrete does not dry out
Water needs space to expand into

## Slide 15: Saturation/freeze thaw distress
Marginal w/cm
Marginal air
Poor local drainage
Leads to:
Rapid saturation
Shadowing
Thin flakes
Notes: Summary of the problem

## Slide 16: Saturation/Enhanced!
Notes: Mag chloride will suck water out of the air and go from a crystal to a puddle that never dries out.

## Slide 17: The Causes
Saturation/freeze thaw
Oxychloride formation
Sawing practice
Notes: Summary of the problem

## Slide 18: Oxychloride formation (Salts can cause chemical attack)
Calcium oxychloride
  Calcium hydroxide
  Chlorides from salts (MgCl2 and CaCl2)
  Expands >30%
  At ~40°F
  Use SCMs to reduce CaOH
Sutter
CaCl2 @ 40°F
Notes: There are signs of chemical attack in some cases. The oxychloride later decomposes and disappears. This from Larry Sutter’s work for SD. Have to have the right temperature.

## Slide 19: The Causes
Saturation/freeze thaw
Oxychloride formation
Sawing practice
Notes: Summary of the problem

## Slide 20: What is the common denominator?

## Slide 21: The Objective
Notes: Work continues on these tasks
Input is welcome -

## Slide 22: Preventing Joint Deterioration in New Pavements
Soil, Subgrade, and Base systems
  Stabilized subgrade
  Granular subbase
  Drainage of pavement system
Concrete Mixture Recommendations
  Low water-cement ratio
  Supplementary cementitious materials
  Well-graded aggregates
  Air-void system

## Slide 23: Preventing Joint Deterioration in New Pavements
Construction Practices
  Curing
    Ensure adequate coverage and application rate
  Sawing joints
    Sawing window and proper depth
  Sealing joints
    If seal, have to maintain the seal
    Consider drainable base
  Surface Sealers
    If use, consider high solids content
    Research is ongoing

## Slide 24: Maintenance Activities to Reduce Joint Deterioration Risk
Routine Maintenance
  Joint cleaning and sealing
  Surface sealers
  Drainage
Winter Maintenance
  Deicing/anti-icing chemicals
    #1 state was IA, averaging the application of 20,209,040 gal of NaCl brine in the last three years applied to 19,279 ln mi
    #1 state was NY, averaging 920,866 tons NaCL in the last three years over 43,603 ln mi
    Calcium chloride and magnesium chloride are more detrimental to cement paste than sodium chloride
  Do not expose concrete to salt for at least 30 days after placement

## Slide 25
So…
  The game has changed . . . . .
    Water has to be prevented from saturating the concrete
    Permeability of the concrete should be as low as practical
    The air void system in the in-place concrete must be adequate
Notes: Fence is only as good as the weakest point – note the lock on the gate

## Slide 26: The Lessons
Significant change seems to be deicing salt selections
Concrete ingredient changes may contribute
Acknowledging that safety is paramount, we need to make better concrete to resist these salts
  Air void system
  w/cm
  SCM dose
Notes: Summary of the problem

## Slide 27: A Better Specification through the Performance Engineered Mixture Initiative
Require the things that matter
  Transport properties (everywhere)
  Aggregate stability (everywhere)
  Strength (everywhere)
  Cold weather resistance (cold locations)
  Shrinkage (dry locations)
  Workability (everywhere)

## Slide 28: In Short
Low w/cm ratio – consider 0.4 target
Adequate entrained air – 5% to 8% w/5% min in place
SCMs
  20-25% class F fly ash
  30-35% class C fly ash
  Combination 20% slag and 20% C fly ash
Well graded aggregates
Use chemicals appropriately
  Salts
  Penetrating sealers

## Slide 29: http://www.intrans.iastate.edu/research/documents/research-reports/2016_joint_deterioration_in_pvmts_guide.pdf http://www.cptechcenter.org/technical-library/documents/Joint-Performance-Guide.pdf

## Slide 30: http://www.cproadmap.org/publications/MAPbriefJune2015.pdf http://www.cproadmap.org/publications/MapbriefJune2014.pdf

## Slide 31
Thank You

## Slide 32: Concrete Pavement Joint Distress
Cause and Mitigation