## Slide 1: 2018 Pavement Workshop Flexible Session May 23-24, 2018
Tensile Strength Ratio (AASHTO T 283)
Testing Brett Trautman, PE
Physical Laboratory Director
Construction and Materials Division
Missouri DOT
+ 46 Associate Members

## Slide 2: History in Missouri
Been performing on field samples for over 15 years
Allows contractors options (hydrated lime, anti-strips, etc…)
Samples taken at the asphalt plant
Material retain for dispute resolution purposes
Sampling Frequency
QC: 1 sample per 10,000 tons
QA: 1 sample per 50,000 tons

## Slide 3: History in Missouri
Incentive/Disincentive pay factors
Price adjustment based on QC data
Need favorable comparison between QA and QC test results
The following pay adjustment table used:

## Slide 4: Molding Process
Samples received at the Central Laboratory
Bucket place into oven set at 5 deg. C below the molding temperature
Achieve a workable mix
Max. time limit of 2 hours
Weigh out material for molding specimens
Use quartering method

## Slide 5: Molding Process
Samples then placed into an oven set at the molding temperature
Max. time limit of 2 hours
Samples compacted to 95 mm
Achieve 7.0 +/- 0.5% air voids
Trial specimen molded to verify the mix weight is correct
Prevent wasting material

## Slide 7: Mix Designs
TYPE | AGG SIZE | BINDER | DES VOIDS | MODIFIED NDES
SPWEB340C | 12.5 | 58H-34 | 4.0 | 0
SPWED440E | 4.8 | 58H-28 | 4.0 | 0
SPWEA440E | 9.5 | 58H-28 | 4.0 | 0
SPWEB450E | 12.5 | 58H-28 | 5.0 | 50
SPWEB440E | 12.5 | 58H-28 | 4.0 | 0
SPWEC440E | 19.0 | 58H-28 | 4.0 | 0
SPWEB430E | 12.5 | 58H-28 | 3.0 | 0
SPWED430I | 4.8 | 58E-34 | 2.0-3.0 | 50
UTBWC | - | - | - | 0

## Slide 8
Chart: Average No. of Gyrations
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E | SPWED430I | SPWED440E | UTBWC
Average Gyrations | 26.25 | 24.75 | 34.375 | 20.375 | 16 | 32.875 | 12.125 | 25.375 | 50.125

## Slide 9
Chart: 
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E | SPWED430I | SPWED440E | UTBWC
Wet Set | 6.8 | 7.2 | 7.1 | 7.1 | 6.9 | 7 | 6.8 | 6.8 | 10.8
Dry Set | 6.8 | 7.4 | 7.1 | 7.2 | 7 | 7.2 | 7 | 6.9 | 10.9

## Slide 10
Chart: 
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E | SPWED430I | SPWED440E | UTBWC
Average Gyrations | 75 | 77 | 78 | 80 | 78 | 78 | 79 | 80 | 72

## Slide 11
Chart: Tensile Strength Ratio (TSR)
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E | SPWED430I | SPWED440E | UTBWC
Tensile Strength Ratio | 0.99346 | 0.85097 | 0.89511 | 0.91094 | 0.94641 | 0.96 | 0.94379 | 0.98092 | 0.70886

## Slide 12
Chart: 
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E | SPWED430I | SPWED440E | UTBWC
Conditioned | 106.3 | 74.8 | 100.7 | 84.9 | 83 | 103.2 | 72.2 | 97.7 | 39.2
Unconditioned | 107 | 87.9 | 112.5 | 93.2 | 87.7 | 107.5 | 76.5 | 99.6 | 55.3

## Slide 13: Questions