## Slide 1: MTU MIST Results
Zhanping You
Michigan Technological University
May 24, 2018

## Slide 2: Test Procedures
Compaction Process
  Pre-heat samples at a temperature of 5 °C lower than the compaction temperature for 2 hours
  Quarter the samples
  Place the samples in the oven for 1 hour to reach the compaction temperature
  Molds are in the other oven at a temperature of 5 °C higher than the compaction temperature
  Compact sample to design height, 63.5mm

## Slide 3: Test Procedures
Gmb tests (AASHTO T166)
MIST tests (ASTM D7870, at 55 °C, 40 psi)
  3 samples under 500 cycles
  3 samples under 3500 cycles
IDT tests (AASHTO T283)

## Slide 4: TSR Results
Chart: Mix Type
| SPWEA440E | SPWEB340C | SPWEB430E | SPWEB440E | SPWEB450E | SPWEC440E | SPWED430I | SPWED440E
TSR_500 | 0.89856 | 0.87487 | 0.98908 | 0.78495 | 0.90985 | 1.0091 | 1.3008 | 1.1848
TSR_3500 | 0.83212 | 0.54989 | 0.83582 | 0.80881 | 0.82336 | 0.912 | 1.3624 | 1.2597

## Slide 5: TSR Results
TSR values of most of the mixes over 0.80
Mix SPWEB340C has a low TSR value of 0.55
Mix SPWEB440E may be moisture susceptible
Mix SPWED430I and mix SPWED440E have high TSR values of greater than 1

## Slide 6: Discussion
Mixs SPWED430I and SPWED440E
  Difficult to obtain required air voids percent
  Anti-stripping agent
MIST difference between 500 cycles and 3500 cycles