## Slide 1: FHWA Mobile Concrete Technology Center (MCTC)
Taking Technology Transfer to the Next Level
Jim Grove, P.E.
ATI Inc / Consultant to FHWA

## Slide 2: Change is the only constant!
Formally…..
The Mobile Concrete Laboratory
Then.....
The Mobile Concrete Trailer
Now…..
The Mobile Concrete Technology Center

## Slide 3: Program Goals
Implement new and proven concrete technologies
Evaluate new tests and equipment
Demonstrate the benefits of statistical materials acceptance in both agency acceptance programs and industry quality control applications
Assist states with concrete issues
Specification review and development
Technical assistance
Forensics

## Slide 4: MCT Staff
Mike Praul
Jagan Gudimettla
Jim Grove
Nicolai Morari
Jerry Clemons

## Slide 5: MCT Activities
Field visits to active construction projects
Quality in the Concrete Paving Process Workshop
Assist with (PEM) implementation
Equipment Loan Program
One-on-one Training
Conferences, papers, and other activities

## Slide 6: MCT Field Visits
Active field project for a two week period
Traditional and Innovative concrete testing
Data in control chart format
Kick-Off Meeting
Testing
Testing
Week 1

## Slide 7: MCT Field Visits
NDT pavement testing
Conduct and Open House
Hold a Close-Out meeting
Testing
Testing
Open House
Week 2

## Slide 8: QA Workshop
Two-day workshop on the benefits a Quality Assurance Program
Agency and Contractor Participation
Quality in the Concrete Paving Process

## Slide 9: Equipment Loan Program
States or industry can borrow MCT equipment
MCT staff will provide training, if desired
Substantial new equipment purchase
PEM focus

## Slide 10: One Pagers
New effort to use MCT data
Narrowly focused
Meant to stir interest and point reader to resources
  1st : Cement Content
  2nd: Optimized Mix Design
  3rd : Cores vs. Cylinders
  4th : NDT Thickness Measurement
  5th: Surface Resistivity
  6th: Texture of Concrete Pavements
  7th: Maturity
  8th: Curing
  9th: SCMs
  10th: Calorimetry

## Slide 11: MCT Visits (since 2008)
WA
NV
MO
KS
IN
GA
NC
CA
WI
MN
IA
MI
PA
VA
CO
OR
AZ
AL
AR
NM
TX
OK
UT
FL
ID
WY
ND
NE
SD
IL
KY
WV
MD
DE
NJ
RI
VT
NH
ME
NY
OH
MT
MS
TN
LA
AK
SC
MA
CT

## Slide 12: Resent New Technologies / Tests
Optimized Gradation
  Overall Durability
Super Air Meter
  Freeze -Thaw Durability
Surface Resistivity
  Permeability
Phoenix
  Water Content
MIT Scan T3
  Nondestructive Pavement Thickness
Dowel Scan
  Dowel bar alignment
PEM
Construction

## Slide 13: 1. Optimized Combined Gradation
Maximize Aggregate Volume

## Slide 14: Optimized Combined Gradation
What will it do for me?
Less paste=> Lower permeability
Less paste=> Reduced thermal shrinkage
Less paste=> Reduced drying shrinkage
Less paste => Lower cost
Less paste => More sustainability

## Slide 15
Volume of Paste Calculations
% Paste should be less than 25% for lowering the crack tendency of concrete
Reducing the Crack Tendency

## Slide 16: 2. Air Content
Total air (4.0% - 8.0%)
Pressure air meter
  Measure total air in the field
  But, the air void system is what counts
Which is freeze / thaw durable?

## Slide 17: Super Air Meter (SAM)
Measures the Air Void System
Modification of existing air test
  Measures air system quality
  Small bubbles implode
  Test Method
    Test three times at different pressures
    Repeat
    Field friendly
    8-12 Minutes
    Measures total air content

## Slide 18: SAM Principle
Provisional Test Method
  AASHTO TP 118
Resultant Pressure
14.5 psi
30 psi
45 psi
Pressure Introduced
SAM Number
2nd Pressure curve
1st Pressure curve
Time
Standard air pot total air value

## Slide 19: SAM vs. ASTM C457

## Slide 20: 3. Permeability
Became standard in 1981
Most common test
Indicator of vulnerability to water and chloride ingress
Generally 24 hours to condition and 6 hours for testing
Rapid Chloride Penetrability Test (Indirectly)
AASHTO T 277

## Slide 21: Permeability (Surrogate Tests for Durability)
State specification
  Several states
28-day age is being used
Instant results on hardened concrete
Easily measures the right property
Non-destructive test
Surface Resistivity Test (Indirectly)
AASHTO T 358

## Slide 22: Permeability
Surface Resistivity Test matches well with Rapid Chloride Penetrability Test
RCP (Coulombs)
Surface Resistivity (KOhm-cm)
Florida DOT

## Slide 23: 4. Phoenix
New test to measure the water in fresh concrete
Developed by Dr. Tyler Ley, Oklahoma State University
Easy to operate
Once the test begins, no attention is required
A hot plate and a “branding iron” heat the concrete
Run it on the back of a pickup

## Slide 24: Phoenix Procedure
Step 1
Step 2
Step 4
Step 3
Measure unit weight of Concrete
Weigh the pan and concrete
Heat the concrete
Weigh the pan and concrete

## Slide 25: Pulse Induction Technology
Easy to use
High accuracy
Non-destructive
Almost real time
Rapid measurement
Significant cost savings
Independent of the base material
Advantages

## Slide 26: Pulse Induction Technology
Quality Control and Agency Acceptance
AASHTO Test Method (AASHTO T 359-18)
ASTM Test Method in the works
Step 1
Place the target
Step 2
Pave over it
Step 3
MIT Scan T3
Locate the target

## Slide 27: Pulse Induction Technology
FHWA Mobile Concrete Trailer Data
MIT Scan T3

## Slide 28: State of the Practice
Iowa DOT
Wisconsin DOT
Minnesota DOT
West Virginia DOT
Illinois Tollway
Alabama DOT
Nevada DOT
Pennsylvania DOT
Full-Fledged Implementation
Washington State DOT
North Dakota DOT
Implementing in 2019
2019 or beyond
Delaware DOT
Florida DOT
Indiana DOT
North Carolina DOT
Arizona DOT

## Slide 29: Pulse Induction Technology
No track is required
Utilizes a laser
Has wheels so it can move on the pavement
Dowel Scan

## Slide 30: Field visits 2019
WA
NV
MO
KS
IN
GA
NC
CA
WI
MN
IA
MI
PA
VA
CO
OR
AZ
AL
AR
NM
TX
OK
UT
FL
ID
WY
ND
NE
SD
IL
KY
WV
MD
DE
NJ
RI
VT
NH
ME
NY
OH
MT
MS
TN
LA
AK
SC

## Slide 31
https://www.fhwa.dot.gov/Pavement/concrete/mclfly.cfm
MCT Website