## Slide 1: Performance of Whitetopping in Minnesota
Tom Burnham, P.E. | Senior Road Research Engineer
NRRA Pavement Workshop, St. Paul, MN
5/23/2019

## Slide 2: Outline
BCOA (Whitetopping) Study
  Objectives
  Field condition surveys
  Performance curves
  Impact of design features
  Life prediction model
Recent findings

## Slide 3: Acknowledgements
BCOA project
  Coauthors: Bernard Izevbekhai, Chago Huerta, Joseph Gallagher
  American Engineering Testing
  MnDOT, Q3, and County Traffic Control Forces
  MnDOT Concrete and Pavement Management Units
  Tim Andersen - Technical Liaison
  TAP members

## Slide 4: Whitetopping Study Objectives
Review performance in Minnesota
Develop performance curves for MnDOT Pavement Management System
Identify best practices for design, construction, and maintenance in Minnesota

## Slide 5: Study Approach
Gather performance data on BCOA projects in Minnesota
Develop performance curve for each project
Identify impact of design features on performance
Develop performance prediction models
Identify best practices

## Slide 6: Literature Search
  Louisiana (10+ years)
    4” thick, 4’x4’ panels
    2+ mm faulting after 8 years
    Steady decline in performance over time
Source: Chen, X. 2014

## Slide 7: Literature Search
  Illinois (2-14 years)
    Crack counts and FWD testing
    Longitudinal cracking and faulting in large panels
    Slab migration
    Benefits from use of fiber-reinforced concrete
Source: King and Roesler, 2014

## Slide 8: Literature Search
  Iowa (< 10 years of data for short panels)
    Performance measure = PCI
    Less than 40 faulted joints/mile
      Considered low severity joint faulting between 0.12 and 0.24 in (3 and 6 mm)
Source: Gross et al, 2017

## Slide 9: Database of Minnesota Projects
26 Large scale projects (built before 2015)
  MnDOT
    TH30 (1993)
    TH212 (2009)
    I-35 (2009)
    TH56 (2010)
    TH24 (2014)
  County
    20 projects (2009-2014)
21 MnROAD test sections
    Test cells (1997-2013)

## Slide 10: Project Population (pre 2015)
(includes MnROAD sections)

## Slide 11: Project Population (pre 2015)
(includes MnROAD sections)

## Slide 12: Project Population (pre 2015)
(includes MnROAD sections)

## Slide 13: Project Population (pre 2015)
Other design details
  Remaining asphalt thickness from 3” to 14”
  20.5 of 46 projects with unsealed joints
  No network projects with structural fibers
    MnROAD FRC BCOA Cells 160-162 (2013)

## Slide 14: Field Condition Surveys
2015: GPR for thickness variation
2015: 3 core samples from each project
  Assess bond quality
  GPR thickness calibration
  HMA assessment (also used in project selection study)
2015-2018: Visual distress surveys
  Crack counts and characterization
  Photographs
2015-2018: Fault measurements
2015-2018: Ride quality profiles (IRI)

## Slide 15: Field Condition Summaries

## Slide 16: Field Condition Summaries

## Slide 17: Field Condition Summaries

## Slide 18: Field Observations
Most projects are in good to very good condition
  Most less than 10 years old
  Some longitudinal cracking
  Very few transverse reflective cracks
    I-35 cracked early, but has stabilized (no repairs)
Little to no maintenance on most projects
  Typically repairs of construction errors
  Repairs on CSAH 46 - partial dowels in OWP only

## Slide 19: Field Survey Observations
Faulted transverse joints on projects with heavy traffic volumes/loads
  Matching overlay joints to underlying HMA cracks
    Early faulting caused by full-depth vertical movement
  TH22 Olmsted County project: Significant faulting in 5 years
    Retrofit dowels and diamond grind
With shorter joint spacing, not all joints deploy early
  Dominant joints form ~ 60 ft
Joint seals (hot-pour asphalt)
  Often breeched in < 2 years
  Lack of seals can lead to buckling

## Slide 20: Core Sample Observations
Revealed various bonding and asphalt conditions
Bond affected by age, location in panel
Bond fails first near joints (typically < 5 years)

## Slide 21: Field Observations
CSAH 18 – Andover, Anoka County (2011)
6” thick, 6’x6’/6’x7’ panels
2017 Conditions | 
% panels cracked | < 1
Average IRI (in/mi) | 59
Average Faulting (mm) | 0.5
@ age 5 years

## Slide 22: Field Observations
TH 30 – Amboy, MnDOT D-7 (1993)
6” thick, 12’x12’ panels, skewed joints
2017 Conditions | 
% panels cracked | N/A
Average IRI (in/mi) | 128
Average Faulting (mm) | N/A
@ age 22 years
Update: 2019 Avg Faulting = 2.5 mm
Max = 6.2 mm

## Slide 23: Field Observations
CSAH 9 – Harris, Chisago County (2010)
7” thick, 15’L x 14’W panels, 3 dowels OWP
2017 Conditions | 
% panels cracked | 17
Average IRI (in/mi) | 76
Average Faulting (mm) | 0.70
@ age 6 years

## Slide 24: Field Observations
CSAH 46 – Albert Lea, Freeborn County (2009)
6” thick, 15’L x 13.5’W panels, 3 dowels OWP
2017 Conditions | 
% panels cracked | 85
Average IRI (in/mi) | 84
Average Faulting (mm) | N/A
@ age 7 years

## Slide 25: Field Observations
I-35 - North Branch, MnDOT D-Metro (2009)
6” thick, 6’x6’ panels
2017 Conditions | 
% panels cracked | N/A
Average IRI (in/mi) | 90
Average Faulting (mm) | N/A
@ age 6 years
Update: 2019 Avg Faulting = 1.4 mm
Max = 2.7 mm

## Slide 26: Field Observations
TH 56 – West Concord, MnDOT D-6 (2010)
6” thick, 15’L x 13.5’W panels, full dowels
2017 Conditions | 
% panels cracked | < 1
Average IRI (in/mi) | 80
Average Faulting (mm) | 0.46
@ age 6 years

## Slide 27: Field Observations
CSAH 1 – Gordonsville, Freeborn County (2014)
5” thick, 6’ x 6’W panels
2016 Conditions | 
% panels cracked | < 1
Average IRI (in/mi) | 67
Average Faulting (mm) | N/A
@ age 1 year

## Slide 28: Field Observations
CSAH 7 – Hutchinson, McLeod County (2009)
5” thick, 6’L(var)x6’W/6’L(var)x7W’ panels
2017 Conditions | 
% panels cracked | 7
Average IRI (in/mi) | 85
Average Faulting (mm) | 0.80
@ age 7 years
Update: 2019 Avg Faulting = 1.0 mm
Max = 2.8 mm

## Slide 29: Field Observations
CSAH 22 – Rochester, Olmsted County (2011)
2016 Conditions | 
% panels cracked | 2
Average IRI (in/mi) | 167
Average Faulting (mm) | 3.4
6.5” thick, 12’ x 12’ panels
@ age 5 years
Retrofit dowels and diamond grind in 2016

## Slide 30: Performance Curves
Plots of MnDOT performance indices:
  IRI (measured)
  RQI = 6.634 (0.353)( ) (inches/mile)
  SR = e(1.386 (0.045)(TWD))
  PQI =
Note: RQI, SR, PQI are derived indices based on statistical correlation with MnDOT rating panels, none of which have traveled over short panel whitetopping projects

## Slide 31: CSAH 22 – Nowthen: IRI
Chart: CSAH 22 Nowthen
| 0 | 4.0027397260273974 | 4.4219178082191783 | 5.0054794520547947 | 6.0054794520547947 | 6.4027397260273968 | 7.4 | 7.1698630136986301
 | 54.4 | 66.9 | 70.7 | 68.7 | 74.35 | 84.5 | 92 | 90.4
6” thick, 6’x6’/6’x7’ panels

## Slide 32: TH 30 – Amboy: IRI
6” thick, 12’x12’ panels, skewed joints
Rehab project

## Slide 33: TH 56 – West Concord: IRI
6” thick, 15’L x 13.5’W panels, full dowels

## Slide 34: MnROAD – Whitetopping Cells
21 MnROAD test sections (constructed 1997-2013)
  Many variables
    Thickness
    Panel size
    Remain HMA thickness
    Dowels (round @ 2’ c. to c. spacing, plates)
    Fiber-reinforced concrete
    Seal/no seal joints
  Interstate traffic (avg ≈ 1 million ESALs/yr)
  Good for revealing distress mechanisms
  Ride quality not representative of typical projects

## Slide 35: MnROAD – Cell 94: IRI

## Slide 36: MnROAD – Cell 97: Faulting

## Slide 37: Performance Review
Impact of design features
Thickness vs % change in ride quality (IRI)
Thickness vs cracking
Panel size vs % change in IRI
Panel size vs cracking
Remaining HMA thickness vs % change in IRI
Remaining HMA thickness vs cracking
Traffic vs % change in IRI
Traffic vs cracking

## Slide 38: Performance Models
Develop model(s) to predict service life to poor condition
  Predict time to first major rehab (minimal maintenance)
  Not comfortable using MnDOT RQI until calibrated for whitetoppings
  Chose FHWA poor condition IRI limit of 170 in/mi
  Models developed for undoweled whitetoppings on lower volume roads
    Fully doweled projects behave like standard concrete pavement on base

## Slide 39: Performance Models
“I/B” (Izevbekhai/Burnham) Model:
  IRI =Const+(TRAFα1)+(RRSα2)+(DOWα3)+(JSLα4)+(AGE α5)+(HMA α6)+(PANL α7)
where:
  Const = constant
  TRAF = annual traffic (ESALs)
  RRS = Radius of relative stiffness (in)
  DOW = Dowels present (= 0.7 for full dowels, = 2 for partial dowels, =3 for no dowels)
  JSL = Transverse joint sealed (= 1 sealed, =2 for breached*, =3 unsealed)
  AGE = Age (years)
  HMA = Remaining HMA thickness (in)
  PANL = Panel length (in)
* Based on field observations, a sealed joint is assumed to be breached after 4 years.

## Slide 40: Performance Models
“TB” (Tom Burnham) Model:
IRI = Const[e α(AGE)]
where:
  Const = constant
  AGE = Age (years)

## Slide 41: Performance Model Fit

## Slide 42: Performance Model Fit

## Slide 43: Performance Model Fit

## Slide 44: Overall Performance Model
Based on 6 projects with most data (TH 30 used to test fit)

## Slide 45: Overall Performance Model
Based on 6 projects with most data (TH 30 used to test fit)

## Slide 46: Overall Life Prediction – Undoweled Projects
Typical life to poor condition = 18 years (max ≈ 25 yrs)
  Assumes few construction errors
  Few projects have developed severe faulting yet
    Actual age to reach poor condition may be sooner
  Recent improvements in design, construction and materials may extend performance life
    Profile milling (uniformity of overlay thickness)
    Fiber-reinforced concrete mixes (less faulting)
  Preventive/routine maintenance could extend life (timing?)

## Slide 47: Joint Activation Determination Using MIRA
MIRA = Low-Frequency Ultrasonic Tomographer
  48 Shear-wave transducers
Diagram from Germann Instruments MIRA™ Operation Manual

## Slide 48: Joint Activation Determination Using MIRA
Joint Not Deployed
Joint Deployed

## Slide 49: Whitetopping Joint Activation
  Used frequency of 35 kHz based on report by Tran and Roesler (ICT-19-003, March 2019)

## Slide 50: Whitetopping Joint Activation
  Used frequency of 35 kHz based on report by Tran and Roesler (ICT-19-003, March 2019)

## Slide 51: Questions?
Tom Burnham
tom.burnham@state.mn.us