## Slide 1: 2019 Pavement Workshop May 21-23, 2019
Determining Pavement Design Criteria for Recycled Aggregate Base and Large Stone Subbase
TPF-5(341)
Bora Cetin
Assistant Professor
Iowa State University
+ 46 Associate Members

## Slide 2: RESEARCH TEAM
Iowa State University
Principal Investigator – Bora Cetin
  Assistant Professor – Department of Civil, Construction & Environmental Engineering
Co-Principal Investigator – Ashley Buss
  Assistant Professor – Department of Civil, Construction & Environmental Engineering
Co-Principal Investigator – Halil Ceylan
  Professor – Department of Civil, Construction & Environmental Engineering
Co-Principal Investigator – Junxing Zheng
  Assistant Professor – Department of Civil, Construction & Environmental Engineering
Research Personnel – Haluk Sinan Coban
  PhD Student – Department of Civil, Construction & Environmental Engineering
  University of Wisconsin-Madison
Co-Principal Investigator – William Likos
  Professor – Department of Civil and Environmental Engineering
Co-Principal Investigator – Tuncer B. Edil
  Professor Emeritus – Department of Civil and Environmental Engineering
  Visiting Scholar – Askin Ozocak
  Associate Professor – Sakarya University

## Slide 3: OUTLINE
Introduction
Research motivation
Objectives
Research plan
Construction
Field testing
Laboratory testing
What have we learned?
Future expectations

## Slide 4: INTRODUCTION
Recycled concrete aggregate (RCA)
  Old & failed concrete pavement surfaces
  Other structures
Recycled asphalt pavement (RAP)
  Old & failed asphalt pavement surfaces
Large stones
  Single crushing operation
  Energy consumption (Kazmee et al. 2015)
https://atlasconcrete.co.nz/benefits-of-recycling-concrete/
https://arthuge.com/dirt_sand_gravel_limestone_fill_sand_prices
https://greelysand.com/shop/decorative-stone-river-rock/granite-stone/
RCA
RAP
Large stones

## Slide 5: RESEARCH MOTIVATION
Inconsistent design methods & construction specifications
Prediction of engineering properties from index properties
Variety & uncertainty of RCA and RAP
Limitations of the test apparatus for large stones

## Slide 6: OBJECTIVES
1st Goal – Determine the field and laboratory performance
FWD, LWD, DCP, intelligent compaction (IC) data
2nd Goal – Develop a method to estimate the stiffness and permeability from
Percent crushing of particles after compaction
Sphericity, angularity, and surface texture
3rd Goal – Prepare a pavement design and construction specification
Performance
Unsaturated & saturated characteristics
Gravel, sand, fines content, gravel-to-sand ratio, D10, D30, D50, D60
Life-cycle cost analysis
Index & engineering properties

## Slide 7: RESEARCH PLAN
Task 1 – Literature review and recommendations
Task 2 – Tech transfer “state of practice”
Task 3 – Construction monitoring and reporting
Task 4 – Laboratory testing
Task 5 – Performance monitoring and reporting
Task 6 – Instrumentation
Task 7 – Pavement design criteria
Task 8 & 9 – Draft/final report
Green – Completed
Red – In Progress

## Slide 8: CONSTRUCTION
Test Facility
Minnesota Road Research Project (MnROAD) Low Volume Road (LVR)
  Two-lane closed loop
  Inside lane – traffic simulation
  Outside lane – environmental & dynamic response monitoring

## Slide 9: CONSTRUCTION
Test Cells
TX = Triaxial Geogrid
BX = Biaxial Geogrid
GT = Nonwoven Geotextile
S. Granular Borrow = Select Granular Borrow

## Slide 10: CONSTRUCTION
Test Materials

## Slide 11: FIELD TESTING
Field Tests
Lightweight deflectometer (LWD) test
Gas permeameter test (GPT)
Intelligent compaction (IC) test
Automated plate load testing (APLT)
Falling weight deflectometer (FWD) test

## Slide 12: FIELD TESTING

## Slide 13: FIELD TESTING
Falling Weight Deflectometer (FWD) Test
Geophones – 0 to 72 in (0 to 1830 mm) away from the center plate
Deflection basin
Influence depth = 1.5 to 2.2 in (0.45 to 0.68 m) (Mooney et al. 2010; Vennapusa et al. 2012)
https://www.clrp.cornell.edu/nuggets_and_nibbles/articles/2005/fwd.html
Dynatest Model 8002 FWD device

## Slide 14: FIELD TESTING
Falling Weight Deflectometer (FWD) Test
Before & after paving
Composite analysis
Layered analysis
  Asphalt
  Base+subbase
  Subgrade
Composite
Subgrade
Base+ subbase
Composite
Subgrade
Base+ subbase
Asphalt

## Slide 15: FIELD TESTING
Falling Weight Deflectometer (FWD) Test
Before paving

## Slide 16: FIELD TESTING
Falling Weight Deflectometer (FWD) Test
After paving

## Slide 17: LABORATORY TESTING
Task 4 - Laboratory Testing
Iowa State University
Soil-water characteristic curve
University of Wisconsin-Madison
Sieve analysis & hydrometer test
Gyratory compaction & percent crushing
Contact angle measurement
Atterberg limits
Proctor compaction
Specific gravity & absorption
Image analysis
Asphalt & cement content determination
Permeability
Green – Completed
Red – In Progress

## Slide 18: LABORATORY TESTING
Material | Gravel (%) | Sand (%) | Fines (%)
Coarse RCA | 61.7 | 34.9 | 3.4
Fine RCA | 38.3 | 54.6 | 7.1
Limestone | 52.3 | 32.6 | 15.1
RCA+RAP | 41 | 50.4 | 8.6
Class 6 Aggregate | 35.1 | 58.6 | 6.3
Class 5Q Aggregate | 65.9 | 30.9 | 3.2
S. Granular Borrow | 31.1 | 56.5 | 12.4
LSSB | 99.6 | 0.3 | 0.1
Sand Subgrade | 27.6 | 59.8 | 12.6
Clay Loam | 3.1 | 37.2 | 59.7
Sieve Analysis & Hydrometer Test
ASTM C136 & D6913 – Sieve analysis
ASTM D7928 – Hydrometer test
Fines = silt and clay

## Slide 19: LABORATORY TESTING
Atterberg Limits
LL = liquid limit; PL = plastic limit; PI = plasticity index; NA = not available; NP = non-plastic
Material | LL | PL | PI
Coarse RCA | NA | NA | NP
Fine RCA | 32.7 | NA | NP
Limestone | 17.9 | NA | NP
RCA+RAP | 27.4 | NA | NP
Class 6 Aggregate | 27.4 | NA | NP
Class 5Q Aggregate | NA | NA | NP
S. Granular Borrow | 18.9 | NA | NP
LSSB | NA | NA | NP
Sand Subgrade | 19.9 | NA | NP
Clay Loam | 36.3 | 23.9 | 12.4

## Slide 20: LABORATORY TESTING
Classification
Material | Gravel (%) | Sand (%) | Fines (%) | Cu | Cc | LL | PL | PI | USCS (ASTM D2487) |  | AASHTO M 145
 |  |  |  |  |  |  |  |  | Symbol | Definition | 
Coarse RCA | 61.7 | 34.9 | 3.4 | 34.5 | 1.75 | NA | NA | NP | GW | Well-Graded Gravel with Sand | A-1-a
Fine RCA | 38.3 | 54.6 | 7.1 | 33.9 | 1.12 | 32.7 | NA | NP | SW-SM | Well-Graded Sand with Silt and Gravel | A-1-a
Limestone | 52.3 | 32.6 | 15.1 | 211.3 | 1.91 | 17.9 | NA | NP | GM | Silty Gravel with Sand | A-1-b
RCA+RAP | 41 | 50.4 | 8.6 | 49.4 | 0.98 | 27.4 | NA | NP | SP-SM | Poorly-Graded Sand with Silt and Gravel | A-1-a
Class 6 Aggregate | 35.1 | 58.6 | 6.3 | 23.8 | 0.60 | 27.4 | NA | NP | SP-SM | Poorly-Graded Sand with Silt and Gravel | A-1-a
Class 5Q Aggregate | 65.9 | 30.9 | 3.2 | 33.7 | 2.60 | NA | NA | NP | GW | Well-Graded Gravel with Sand | A-1-a
S. Granular Borrow | 31.1 | 56.5 | 12.4 | 30.3 | 1.10 | 18.9 | NA | NP | SM | Silty Sand with Gravel | A-1-b
LSSB | 99.6 | 0.3 | 0.1 | 1.84 | 1.08 | NA | NA | NA | GP | Poorly-Graded Gravel | A-1-a
Sand Subgrade | 27.6 | 59.8 | 12.6 | 33.1 | 1.24 | 19.9 | NA | NP | SM | Silty Sand with Gravel | A-1-b
Clay Loam | 3.1 | 37.2 | 59.7 | NA | NA | 36.3 | 23.9 | 12.4 | CL | Sandy Lean Clay | A-6
Fines = silt and clay; Cu = coefficient of uniformity; Cc = coefficient of curvature; LL = liquid limit; PL = plastic limit; PI = plasticity index; NA = not available; NP = non-plastic; USCS = unified soil classification system; AASHTO = American Association of State Highway and Transportation Officials

## Slide 21: LABORATORY TESTING
Specific Gravity & Absorption
ASTM C127 – for coarse aggregates
ASTM C128 – for fine aggregates
ASTM D854 – for soil solids
https://www.globalgilson.com/specific-gravity-bench
https://www.pavementinteractive.org/reference-desk/testing/aggregate-tests/fine-aggregate-specific-gravity/
https://www.pavementinteractive.org/reference-desk/testing/aggregate-tests/fine-aggregate-specific-gravity/
ASTM C127
ASTM C128
ASTM D854

## Slide 22: LABORATORY TESTING
Specific Gravity & Absorption
Material | Oven-Dry (OD) Specific Gravity |  |  | Absorption (%) |  | 
 | Coarse Fraction | Fine Fraction | Combined (Coarse + Fine) | Coarse | Fine | Combined (Coarse + Fine)
Coarse RCA | 2.40 | 2.00 | 2.25 | 4.05 | 11.68 | 6.97
Fine RCA | 2.45 | 1.99 | 2.17 | 3.70 | 11.73 | 8.65
Limestone | 2.65 | 2.68 | 2.66 | 1.91 | 1.51 | 1.72
RCA+RAP | 2.47 | 2.15 | 2.28 | 3.09 | 5.22 | 4.34
Class 6 Aggregate | 2.45 | 2.30 | 2.35 | 3.00 | 4.32 | 3.86
Class 5Q Aggregate | 2.39 | 2.07 | 2.28 | 4.62 | 9.62 | 6.32
S. Granular Borrow | 2.70 | 2.58 | 2.62 | 1.14 | 1.71 | 1.53
LSSB | 2.60 | NA | 2.60 | 0.36 | NA | 0.36
Sand Subgrade | 2.70 | 2.56 | 2.60 | 1.08 | 2.13 | 1.84
Clay Loam | NA | 2.68 | 2.68 | NA | NA | NA
Coarse fraction = materials retained on No. 4 sieve; fine fraction = materials passing through No. 4 sieve; combined = weighted average of coarse and fine fractions

## Slide 23: LABORATORY TESTING
Proctor Compaction
MDD = maximum dry density; OMC = optimum moisture content; NA = not available
Material | MDD |  | OMC (%)
 | (pcf) | (kN/m3) | 
Coarse RCA | 122.9 | 19.31 | 11.3
Fine RCA | 121.6 | 19.10 | 11.1
Limestone | 142.2 | 22.34 | 6.2
RCA+RAP | 125.6 | 19.73 | 10
Class 6 Aggregate | 128.2 | 20.14 | 8.3
Class 5Q Aggregate | 122.6 | 19.26 | 11
S. Granular Borrow | 138.6 | 21.77 | 5.4
LSSB | NA | NA | NA
Sand Subgrade | 136.6 | 21.46 | 5.7
Clay Loam | 123.9 | 19.46 | 10

## Slide 24: LABORATORY TESTING
Summary of Other Index Properties
Material | MDD |  | OMC (%) | Combined Oven-Dry (OD) Specific Gravity | Combined Absorption (%)
 | (pcf) | (kN/m3) |  |  | 
Coarse RCA | 122.9 | 19.31 | 11.3 | 2.25 | 6.97
Fine RCA | 121.6 | 19.10 | 11.1 | 2.17 | 8.65
Limestone | 142.2 | 22.34 | 6.2 | 2.66 | 1.72
RCA+RAP | 125.6 | 19.73 | 10 | 2.28 | 4.34
Class 6 Aggregate | 128.2 | 20.14 | 8.3 | 2.35 | 3.86
Class 5Q Aggregate | 122.6 | 19.26 | 11 | 2.28 | 6.32
S. Granular Borrow | 138.6 | 21.77 | 5.4 | 2.62 | 1.53
LSSB | NA | NA | NA | 2.60 | 0.36
Sand Subgrade | 136.6 | 21.46 | 5.7 | 2.60 | 1.84
Clay Loam | 123.9 | 19.46 | 10 | 2.68 | NA
MDD = maximum dry density; OMC = optimum moisture content; NA = not available

## Slide 25: LABORATORY TESTING
Image Analysis
2D Particle Shape Analysis
3D Particle Shape Analysis
  Stereophotography
  Shining 3D – EinScan-SP
https://www.dream3d.co.uk/product/shining-3d-einscan-sp/
http://junxing.public.iastate.edu/research.html
Stereophotography
Shining 3D – EinScan-SP

## Slide 26: LABORATORY TESTING
Stereophotography
Position 1
(Left)
Position 2
Position 3
(Right)
Position 1 (Left)
Position 2
Position 3 (Right)
Camera
Camera slider
Test material

## Slide 27: LABORATORY TESTING
Stereophotography
Calibration
Background with text and shapes
for calibration

## Slide 28: LABORATORY TESTING
Stereophotography
Stereophotography
Parameters
  Area sphericity
  Diameter sphericity
  Circle ratio sphericity
  Perimeter sphericity
  Width to length ratio sphericity
  Circularity
  Convexity
  Roundness
Notes: Several parameters can be determined by the stereophotography. Parameters are listed and a table is provided with their descriptions and formulas. In addition, their references are provided. This table is taken from one of Quan’s papers (not published yet I guess), who is Dr. Zheng’s PhD student.

## Slide 29: LABORATORY TESTING
Stereophotography
LSSB – 4766 particles (one barrel)
(Zheng and Hryciw 2017)
Notes: For the large stones, ISU team received 2 barrels from the MnDOT. Stereophotography was performed only for one of the barrels, which contains 4766 large stone particles retained on No. 4 sieve. Particles passing No. 4 sieve cannot be used for image analysis with the current image station setup. d1, d2, d3, and de parameters, which are related to particle sizes, are also obtained by the stereophotogtaphy. The equation of ‘de’ is also provided in this slide.
Particle size distribution of large stones were determined by both conventional sieve analysis and stereophotography. With the sieve analysis, percent passing values are determined by weight. On the other hand, with the stereophotography, percent passing values are determined by volume. As seen from the figure, image analysis and sieve analysis provided similar results. One comment is that now ISU team is working on improving the MATLAB codes to reduce noise and increase accuracy. Therefore, ISU team is expecting that the results will be much closer to each other after modifying the codes.

## Slide 30: LABORATORY TESTING
Stereophotography
Stereophotography
(Zheng and Hryciw 2017)
Notes: Elongation ratio, flatness ratio, and elongation and flatness ratio can be determined from the data obtained by the stereophotography. Their scatter plots are provided in this slide. Distribution of the values among 4766 large stone particles are shown. From these figures, distribution of the ratios by percent finer by volume can be observed. Overall or weighted elongation ratio, flatness ratio, and elongation and flatness ratio can be determined. Further numerical analysis has not been performed yet because the ISU team is working on improving the MATLAB codes, which will change the values slightly. More accurate results will be shown later.

## Slide 31: LABORATORY TESTING
Stereophotography
Stereophotography
http://www.sourcecatalog.com/terminology/terminology.html
Notes: In addition to the previous distributions, roundness (angularity) and sphericity values and their distributions can be determined. As said previously, no further data analysis has not been performed yet.

## Slide 32: LABORATORY TESTING
Particles retained on 2.5-in sieve
Particles retained on 2-in sieve
Particles retained on 1.5-in sieve
Particles retained on 1-in sieve
Particles retained on 3/4-in sieve
Particles retained on 3/8-in sieve
Particles retained on No. 4 sieve
Stereophotography vs Shining 3D – EinScan-SP
Comparison
Randomly selected particles
  For each sieve between 2.5-in and No. 4 sieves
Notes: To check the accuracy of the stereophotography, Shining 3D – EinScan-SP 3D scanner is also being used on selected particles. Since we need to scan the large stone particles one by one with the 3D scanner, 175 particles in total was selected for comparison. Sieve analysis was performed and the particles were separated based on their particles sizes. 25 particles from each sieve were collected. The pictures in this slide do not show all 25 particles retained on each sieve. The pictures are provided only to show the differences in particles sizes.
All 3D images were captured and their data are being analyzed right now. 3D image analysis data and their comparison with stereophotography will be provided later.

## Slide 33: LABORATORY TESTING
Shining 3D – EinScan-SP
Test material
White background for noise
elimination
EinScan-SP
Notes: This slide shows the Shining 3D – EinScan-SP setup. After several trials, we decided to place a white background to eliminate the noise that occurs frequently during scanning. After the placement of white background, the noise was reduced significantly. On the right-hand side, two examples are shown regarding the 3D images created.

## Slide 34: LABORATORY TESTING
Shining 3D – EinScan-SP
Side view
Top view
Notes: The data is saved in 3D Builder format. This slide only shows side and top views as an example of the created 3D image.

## Slide 35: LABORATORY TESTING
Asphalt Content Determination
Quantitative extraction – AASHTO T 164
Ignition method – AASHTO T 308
  RCA+RAP  3.2% asphalt binder
  Class 6 aggregate  3.3% asphalt binder
RCA+RAP
Class 6 Aggregate
Notes: For asphalt content determination, both quantitative extraction and ignition methods were decided to be performed. Loss of fines is expected with the ignition method; therefore, higher-than-actual amount of asphalt binder can be determined. The reason is that fine asphalt particles have very low specific gravity, which means that they are lighter than other particles. During the ignition, burned asphalt turns into ash and collected by the fume hood. In addition to the ash, lightweight fine particles can also be collected by the fume.
Ignition method is very straightforward. To check the accuracy of the ignition method, quantitative extraction will also be used. So far, only two ignition tests could be completed for RCA+RAP and Class 6 aggregate materials. Other tests are in progress and their data will be provided shortly.

## Slide 36
Specimens prepared in standard compaction mold
Flexible wall permeameter
Permeability Test
ASTM D5084
LABORATORY TESTING

## Slide 37
Permeability Test
LABORATORY TESTING
DOC = degree of compaction

## Slide 38
LABORATORY TESTING
Permeability Test
Degree of compaction
  100, 95, and 90%

## Slide 39
Pressure plates
Soil-Water Characteristic Curve (SWCC) Test
ASTM D6836
Hanging column test  Pressure plate test
Cementation of RCA during the test period
Activity meter
Cementation of RCA
LABORATORY TESTING

## Slide 40
Soil-Water Characteristic Curve (SWCC) Test
Van Genuchten (1980) model
Chart: Cell 186 – Fine RCA (18617GS007)
| 0.28115520566451274 | 0.2811467142880088 | 0.28113534453358829 | 0.28112267076119735 | 0.28110906993418866 | 0.28107979298325864 | 0.28101530574691197 | 0.28083224445196298 | 0.2806290780861766 | 0.28041208600363354 | 0.28018455989210306 | 0.27994858315609444 | 0.27945674363362244 | 0.27841700712967815 | 0.27732941480047063 | 0.27621336097923893 | 0.27508103609070916 | 0.27394077493149893 | 0.27279855943467574 | 0.27165881270646636 | 0.27052486614096816 | 0.26501271239825269 | 0.25985029796053077 | 0.25065669166264948 | 0.24281197569388288 | 0.23606229881053226 | 0.23018715836167022 | 0.22501463221274604 | 0.22041340438485704 | 0.21628285607441644 | 0.21254505248531852 | 0.15677657844506696 | 0.13608137401486622 | 9.7410134351595498E-2 | 8.4283948850620211E-2 | 6.9594362184295086E-2 | 6.0205356259279551E-2 | 5.2082120486397133E-2 | 3.7198195914173018E-2 | 3.4174127035655734E-2 | 3.217881214288433E-2
Fitted Data | 0.001 | 0.025 | 0.05 | 0.075 | 0.1 | 0.15 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 15 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 500 | 1000 | 5000 | 10000 | 25000 | 50000 | 100000 | 500000 | 750000 | 1000000
Pressure Plate Test | 0.001 | 3.4485 | 6.897 | 13.794 | 27.588 | 55.176 | 110.352 | 220.704 | 441.408
Activity Meter | 2590 | 6850 | 13360 | 36560 | 150180
= Normalized volumetric water content
= Soil volumetric water content
= Residual volumetric water content
= Saturated volumetric water content
= Matric suction
, n, and m : Van Genuchten fitting parameters
Parameter | Value
θr | 0
θs | 0.2812
α | 0.0317
n | 1.2091
m | 0.1730
LABORATORY TESTING

## Slide 41
Soil-Water Characteristic Curve (SWCC) Test
LABORATORY TESTING

## Slide 42
Soil-Water Characteristic Curve (SWCC) Test
Degree of compaction initial volumetric water content
LABORATORY TESTING

## Slide 43
Recycled Aggregate Base Layers
  No considerable problem during construction
Stiffness of coarse & fine RCA > limestone & RCA+RAP
  Cementation of unhydrated cement
  Higher angularity and rougher surface texture
Stiffness of fine RCA > coarse RCA
  Fines content unhydrated cement content
Stiffness of RCA+RAP limestone
  Literature RCA & RAP > VA
WHAT HAVE WE LEARNED?

## Slide 44
Recycled Aggregate Base Layers
Stiffness of RCA+RAP < coarse & fine RCA
  Literature stiffness of RCA > RAP
  Higher angularity and rougher surface texture
  Hydrophobicity of RAP
Coarse & fine RCA stress-hardening
Limestone & RCA+ RAP stress-softening
  Soft or wet subgrade condition
WHAT HAVE WE LEARNED?

## Slide 45
Large Stone Subbase with or without Geosynthetics
Problematic construction of LSSB
  Impracticality of two-lift construction for 18 in LSSB
  Subgrade soil pumping due to large opening size of LSSB
  Rutting
Varying stiffness in LSSB sections
  May be due to compactability of LSSB
Stiffness of class 5Q < class 6
Speculations:
  Instability of 9 in LSSB
  Insufficient compaction of class 5Q
  Suitability of 18 in LSSB
Effects of geosynthetics were not discernable
WHAT HAVE WE LEARNED?

## Slide 46
Test Materials
Class 6 & class 5Q not natural
  Class 6 has some RAP
  Class 5Q has some RCA
Clay loam considerably lower Ksat than those of aggregates
Degree of compaction Ksat
Cementation of RCA during tests
Good integrity between pressure plate and activity meter
WHAT HAVE WE LEARNED?

## Slide 47
Compositions of materials – asphalt & cement content
Other physical properties – image analysis
  Angularity and sphericity
  Particle size distribution
Hydrophilicity & hydrophobicity – contact angle measurements
Degradation – gyratory compaction & percent crushing
Long-term performance evaluation
FUTURE EXPECTATIONS

## Slide 48
Thank You

## Slide 49
REFERENCES
ACPA (2010). Why Recycle Concrete Pavements? TS043.1P. American Concrete Paving Association, Skokie, IL. http://1204075.sites.myregisteredsite.com/downloads/TS/EB0 43P /TS04 3.1P.pdf.
CalTrans (2015). Standard Specifications. California Department of Transportation, Sacramento, CA.
IDOT (2016). Standard Specifications for Road and Bridge Construction. Illinois Department of Transportation, Springfield, IL.
Kazmee, H., Mishra, D., & Tutumluer, E. (2015). Sustainable alternatives in low volume road base course applications evaluated through accelerated pavement testing. In IFCEE 2015 (pp. 409-418).
Kazmee, H., Tutumluer, E., & Beshears, S. (2016). Pavement working platforms constructed with large-size unconventional aggregates. Transportation Research Record: Journal of the Transportation Research Board, (2578), 1-11.
Li, C., Ashlock, J. C., White, D. J., Jahren, C. T., & Cetin, B. (2017). Gyratory abrasion with 2D image analysis test method for evaluation of mechanical degradation and changes in morphology and shear strength of compacted granular materials. Construction and Building Materials, 152, 547-557.
MnDOT (2014a). Building Temperature Sensing Arrays (Thermocouple Trees), http://www.dot.state.mn.us/mnroad/pdfs/BuildingTemperatureSensors-TCTree(April201 4).pdf.
MnDOT (2014b). Moisture Content – EW (EC, ET), http://www.dot.state.mn.us/mnroad/data/ pdfs/Base_Moisture_EC_EW_ET.pdf.
MoDOT (2018). Missouri Standard Specifications for Highway Construction. Missouri Highways and Transportations Comission.
Mooney, M., Rinehart, R., White, D., Vennapusa, P., Facas, N., & Musimbi, O. (2010). Intelligent soil compaction systems. NCHRP Report 676. National Cooperative Highway Research Program, Washington, D.C.
USGS (2018). Mineral Commodity Summaries. US Geological Survey.
Van Deusen, D., Burnham, T., Dai, S., Geib, J., Hanson, C., Izevbekhai, B., Johnson, E., Palek, L., Siekmeier, J., Vrtis, M., & Worel, B. (2018). Report on 2017 MnROAD construction activities. Report No. MN/RC 2018-16. Minnesota Department of Transportation, St. Paul, MN.
Vennapusa, P. K. R., White, D. J., Siekmeier, J., & Embacher, R. A. (2012). In situ mechanistic characterisations of granular pavement foundation layers. International Journal of Pavement Engineering, 13(1), 52-67.
Vennapusa, P. K., & White, D. J. (2009). Comparison of light weight deflectometer measurements for pavement foundation materials. Geotechnical Testing Journal, 32(3), 1-13.
White, D. J., & Vennapusa, P. (2017) 2017 MnROAD unbound layer evaluation using intelligent compaction: Ingios validated intelligent compaction (VIC) results. Report No. 2017-043. Ingios Geotechnics.
WisDOT (2018). Standard Specifications. Wisconsin Department of Transportation, WI.

## Slide 50: Thank You!
QUESTIONS??

## Slide 51: INTRODUCTION
Flexible pavements
  90% of the paved roads
Load distribution
Aggregate base layer
  Primary load carrying sublayer
  Stiff and permeable
Subbase layer
  Optional
  Secondary load carrying sublayer
  Separation
  Working platform
  Highly permeable

## Slide 52: INTRODUCTION
1.33 billion tons of virgin aggregates (VAs) in 2017 (USGS 2018)
76% for roadway construction (USGS 2018)
Price of conventional VAs (ACPA 2010)
Alternative materials
https://pubs.usgs.gov/of/2011/1119/pdf/OF11-1119_report_508.pdf

## Slide 53: LITERATURE REVIEW
For RCA and RAP
Angularity  RCA > RAP
Maximum dry  VA > RCA & RAP density
Optimum moisture  RCA > VA > RAP content
Hydrophobicity  RAP > RCA
Permeability  RAP > RCA
Stiffness  RCA & RAP > VA
Strength  RCA > VA > RAP
Durability  RCA > RAP > VA

## Slide 54: LITERATURE REVIEW
For LSSB
Limitations of laboratory equipment (Kazmee et al. 2016)
Inconsistent field data (Kazmee et al. 2016)
  Fluctuation of the data
Mobilization of particles (Kazmee et al. 2016)
  Large voids
  Reorientation
Lack of design methods & construction specifications
Limited applications

## Slide 55: CONSTRUCTION
Large Stone Subbase
Non-traditional subgrade preparation
  Weak subgrade
  DCP index between 2.5 – 3.5 in/blow (64 – 89 mm/blow)
  Upper 1 ft (0.3 m)
  Loosening & watering
(White and Vennapusa 2017)
(Van Deusen et al. 2018)

## Slide 56: CONSTRUCTION
Sensors
Environmental monitoring
  Thermocouples
  Moisture probes
Dynamic response monitoring
  Dynamic pressure cells
  Geophones
  Dynamic strain gauges
(MnDOT 2014b)
(Van Deusen et al. 2018)
(Van Deusen et al. 2018)
(Van Deusen et al. 2018)
(MnDOT 2014a)
Thermocouple tree
Moisture probe
Dynamic pressure cell
Geophone
Dynamic strain gauge

## Slide 57: CONSTRUCTION
Cell Number | Environmental Sensors |  | Dynamic Response Sensors |  | 
 | Thermocouples | Moisture Probes | Dynamic Pressure Cells | Geophones | Dynamic Strain Gauges
185 | 12 | 4 | 2 | 4 | NA
186 | 12 | 4 | 2 | 4 | 4
188 | 12 | 4 | 2 | 4 | 4
189 | 12 | 4 | 2 | 4 | NA
127 | 12 | 3 | 2 | NA | NA
728 | 16 | 4 | 2 | NA | 4
TC = Thermocouple
EC = Moisture probe
PG = Dynamic pressure cell
GP = Geophone
LE = Longitudinal dynamic
strain gauge
TE = Transverse dynamic
strain gauge
Sensors

## Slide 58: CONSTRUCTION
Recycled Aggregate Base
      Subgrade  Cells 185 & 186 – sand
      Cells 188 & 189 – clay loam
      Subbase  Select granular borrow
      Base  Cell 185 – coarse RCA
      Cell 186 – fine RCA
      Cell 188 – limestone
      Cell 189 – RCA+RAP blend
      Surface  12.5 mm NMAS Superpave

## Slide 59: CONSTRUCTION
Large Stone Subbase
Non-traditional subgrade preparation – cont’d
  Mellowing
Placement of LSSB
Impractical two-lift construction
(White and Vennapusa 2017)
(White and Vennapusa 2017)

## Slide 60: CONSTRUCTION
Large Stone Subbase with Geosynthetics
Initial plan
  Only two cells
  No geosynthetics
Problems
  Subgrade soil pumping
  Rutting
(White and Vennapusa 2017)
(White and Vennapusa 2017)

## Slide 61: CONSTRUCTION
(Van Deusen et al. 2018)
Large Stone Subbase with Geosynthetics

## Slide 62: CONSTRUCTION
Large Stone Subbase with Geosynthetics
Excavation to subgrade layers
Reconstruction
Reconstruction

## Slide 63: CONSTRUCTION
Large Stone Subbase with Geosynthetics
Non-traditional subgrade preparation procedure
  DCP index between 2.5 – 3.5 in/blow (64 – 89 mm/blow)
Geosynthetics
  Triaxial geogrid (TX)
  Biaxial geogrid (BX)
  Nonwoven geotextile (GT)
(White and Vennapusa 2017)

## Slide 64
Meteorological Data
Air temperature – 40°F (4°C) and 91°F (33°C) during construction
Relative humidity – 15% – 102%
Wind speed & direction
Precipitation
FIELD TESTING

## Slide 65: FIELD TESTING
Nuclear Density Test
Direct transmission mode (ASTM D6938) for 60 seconds
  4 in (102 mm), 6 in (152 mm), or 8 in (203 mm) deep test holes
  Calibration with laboratory measurements

## Slide 66: FIELD TESTING
Nuclear Density Test

## Slide 67: FIELD TESTING
Dynamic Cone Penetrometer (DCP) Test
ASTM D6951
17.6 lb (8 kg) hammer
22.6 in (575 mm) drop height

## Slide 68: FIELD TESTING
Lightweight Deflectometer (LWD) Test
ASTM E2835
Applied stress = 27.5 psi (190 kPa) (Vennapusa and White 2009)
Influence depth = 8 to 12 in (200 to 300 mm) (Mooney et al. 2010; Vennapusa et al. 2012)

## Slide 69: FIELD TESTING
Gas Permeameter Test (GPT)
GPT device containing a self-contained pressurized gas system with a self-sealing base plate.
  Saturated hydraulic conductivity (KSat) is derived from gas flow and pressure measurements by using the Darcy’s Law.
S = saturation level
(White et al. 2010)

## Slide 70: FIELD TESTING
Intelligent Compaction (IC) Test
Preliminary IC mapping
Automated plate load testing (APLT)
Cyclic stress-dependent resilient modulus (MR)
  10 psi (69 kPa) and 30 psi (207 kPa) plate contact stresses
Influence depth = 2.5 to 5 ft (0.8 to 1.5 m) (Mooney et al. 2010; Vennapusa et al. 2012)
(White and Vennapusa 2017)
Vibratory smooth drum roller
IC mapping
APLT

## Slide 71: FIELD TESTING
Intelligent Compaction (IC) Test
Before paving
Composite analysis
Layered analysis
  Base+subbase
  Subgrade
Composite
Subgrade
Base+ Subbase

## Slide 72: FIELD TESTING
Intelligent Compaction (IC) Test

## Slide 73
(White and Vennapusa 2017)
Automated Plate Load Testing (APLT)
FIELD TESTING

## Slide 74: FIELD TESTING
Automated Plate Load Testing (APLT)

## Slide 75: FIELD TESTING
Falling Weight Deflectometer (FWD) Test
Depth to water table

## Slide 76: LABORATORY TESTING
Fall cone penetrometer
Rolling device
Atterberg Limits
BS 1377-2 – Liquid limit (fall cone penetrometer)
ASTM D4318 – Plastic limit (rolling device)
Materials with fines contents more than 5%
Material | Gravel (%) | Sand (%) | Fines (%)
Coarse RCA | 61.7 | 34.9 | 3.4
Fine RCA | 38.3 | 54.6 | 7.1
Limestone | 52.3 | 32.6 | 15.1
RCA+RAP | 41 | 50.4 | 8.6
Class 6 Aggregate | 35.1 | 58.6 | 6.3
Class 5Q Aggregate | 65.9 | 30.9 | 3.2
S. Granular Borrow | 31.1 | 56.5 | 12.4
LSSB | 99.6 | 0.3 | 0.1
Sand Subgrade | 27.6 | 59.8 | 12.6
Clay Loam | 3.1 | 37.2 | 59.7
Fines = silt and clay

## Slide 77: LABORATORY TESTING
Atterberg Limits
LL = liquid limit; PL = plastic limit;
PI = plasticity index; NA = not available; NP = non-plastic
Material | LL | PL | PI
Coarse RCA | NA | NA | NP
Fine RCA | 32.7 | NA | NP
Limestone | 17.9 | NA | NP
RCA+RAP | 27.4 | NA | NP
Class 6 Aggregate | 27.4 | NA | NP
Class 5Q Aggregate | NA | NA | NP
S. Granular Borrow | 18.9 | NA | NP
LSSB | NA | NA | NP
Sand Subgrade | 19.9 | NA | NP
Clay Loam | 36.3 | 23.9 | 12.4

## Slide 78: LABORATORY TESTING
Specific Gravity & Absorption
Three specific gravity terms (ASTM C127 & C128):
  Oven-dry (OD) or bulk specific gravity
  Saturated surface dry (SSD) specific gravity
  Apparent specific gravity
Dry aggregate
Bulk volume
1.
SSD aggregate
Bulk volume
2.
Dry aggregate
Net volume
3.
http://www.ce.memphis.edu/3137/Powerpoint%20Handouts/3%20-%20Relative%20Density%20and%20Absorption.pdf

## Slide 79: LABORATORY TESTING
Proctor Compaction
ASTM D1557 - Modified Proctor
(ASTM D1557)
(ASTM D1557)
6-in mold
5 layers
56 blows per layer
Material passing 3/4-in sieve
4-in mold
5 layers
25 blows per layer
Material passing No. 4 sieve
6-in mold
4-in mold
Material | Test Method
Coarse RCA | Method C
Fine RCA | 
Limestone | 
RCA+RAP | 
Class 6 Aggregate | 
Class 5Q Aggregate | 
S. Granular Borrow | 
LSSB | NA
Sand Subgrade | Method C
Clay Loam | Method A
NA = not available

## Slide 80: LABORATORY TESTING
Proctor Compaction
ASTM D4718 – Correction for oversize particles
MDD = maximum dry density; OMC = optimum moisture content; NA = not available
Material | MDD |  | OMC (%)
 | (pcf) | (kN/m3) | 
Coarse RCA | 122.9 | 19.31 | 11.3
Fine RCA | 121.6 | 19.10 | 11.1
Limestone | 142.2 | 22.34 | 6.2
RCA+RAP | 125.6 | 19.73 | 10
Class 6 Aggregate | 128.2 | 20.14 | 8.3
Class 5Q Aggregate | 122.6 | 19.26 | 11
S. Granular Borrow | 138.6 | 21.77 | 5.4
LSSB | NA | NA | NA
Sand Subgrade | 136.6 | 21.46 | 5.7
Clay Loam | 123.9 | 19.46 | 10
Material | Corrected MDD |  | Corrected OMC (%)
 | (pcf) | (kN/m3) | 
Coarse RCA | 128.6 | 20.19 | 9.5
Fine RCA | 121.7 | 19.12 | 11.1
Limestone | 143.2 | 22.49 | 6.3
RCA+RAP | 125.8 | 19.76 | 10.0
Class 6 Aggregate | 128.6 | 20.19 | 8.3
Class 5Q Aggregate | 128.0 | 20.11 | 9.6
S. Granular Borrow | 140.3 | 22.03 | 5.3
LSSB | NA | NA | NA
Sand Subgrade | 137.7 | 21.63 | 5.6
Clay Loam | 123.9 | 19.46 | 10.0
MDD = maximum dry density; OMC = optimum moisture content; NA = not available
Uncorrected – Test Data
Corrected

## Slide 81: LABORATORY TESTING
Test material
Image station
Camera
Camera slider
Stereophotography

## Slide 82
Sphericity:
Roundness:
LABORATORY TESTING

## Slide 83
Permeability Test
LABORATORY TESTING
Cell Number | Sample ID | Material Description | w (%) | γd |  | Ksat | 
 |  |  |  | pcf | kN/m3 | (in/sec) | (cm/sec)
185 | 18517GS002 | Coarse RCA | 10.5 | 122.4 | 19.22 | 3.93E-05 | 9.97E-05
 | 18517GS004 |  | 10.5 | 122.4 | 19.22 | 1.60E-04 | 4.06E-04
 | 18517GS008 |  | 10.5 | 122.4 | 19.22 | 3.28E-04 | 8.34E-04
186 | 18617GS006 | Fine RCA | 10.9 | 121.1 | 19.02 | 2.09E-04 | 5.32E-04
 | 18617GS007 |  | 10.9 | 121.1 | 19.02 | 1.94E-04 | 4.94E-04
 | 18617GS008 |  | 10.9 | 121.1 | 19.02 | 1.33E-04 | 3.38E-04
188 | 18817GS005 | Limestone | 6.6 | 143.0 | 22.46 | 1.90E-05 | 4.82E-05
 | 18817GS006 |  | 6.6 | 143.0 | 22.46 | 1.93E-05 | 4.89E-05
 | 18817GS008 |  | 6.6 | 143.0 | 22.46 | 1.34E-05 | 3.41E-05
189 | 18917GS002 | RCA+RAP | 10.5 | 123.0 | 19.32 | 4.84E-05 | 1.23E-04
 | 18917GS003 |  | 10.5 | 123.0 | 19.32 | 1.91E-04 | 4.85E-04
 | 18917GS006 |  | 10.5 | 123.0 | 19.32 | 1.10E-04 | 2.80E-04
127 | 12717GS001 | Class 6 Aggregate | 4.2 | 112.4 | 17.65 | 3.31E-03 | 8.40E-03
 | 12717GS002 |  | 3.9 | 112.4 | 17.65 | 2.90E-03 | 7.37E-03
 | 12717GS003 |  | 4.4 | 114.2 | 17.95 | 2.78E-03 | 7.05E-03
 | 12717GS004 |  | 4.2 | 110.5 | 17.36 | 5.28E-03 | 1.34E-02
228 | 22817GS001 | Class 5Q Aggregate | 6.6 | 113.0 | 17.75 | 9.41E-03 | 2.39E-02
 | 22817GS002 |  | 7 | 106.1 | 16.67 | 2.07E-03 | 5.26E-03
 | 22817GS003 |  | 5.3 | 111.1 | 17.46 | 4.61E-03 | 1.17E-02
 | 22817GS004 |  | 6.3 | 108.6 | 17.06 | 2.10E-03 | 5.33E-03

## Slide 84
Permeability Test
LABORATORY TESTING
Cell Number | Sample ID | Material Description | w (%) | γd |  | Ksat | 
 |  |  |  | pcf | kN/m3 | (in/sec) | (cm/sec)
185 | 18517SS006 | Sand Subgrade | 4.5 | 119.2 | 18.73 | 8.50E-04 | 2.16E-03
 | 18517SS007 |  | 3.7 | 119.9 | 18.83 | 6.57E-03 | 1.67E-02
186 | 18617SS006 | Sand Subgrade | 4.78 | 115.5 | 18.14 | 1.69E-04 | 4.30E-04
 | 18617SS007 |  | 4 | 119.2 | 18.73 | 2.54E-04 | 6.46E-04
188 | 18817SS006 | Clay Loam | 10.08 | 123.6 | 19.42 | 1.60E-07 | 4.07E-07
 | 18817SS007 |  | 9.79 | 124.2 | 19.52 | 1.95E-07 | 4.95E-07
127 | 12717SS001 | Clay Loam | 10.07 | 123.6 | 19.42 | 3.75E-08 | 9.53E-08
 | 12717SS002 |  | 9.04 | 119.9 | 18.83 | 2.59E-07 | 6.58E-07
 | 12717SS003 |  | 9.7 | 124.2 | 19.52 | 8.19E-08 | 2.08E-07
227 | 22717SS001 | Clay Loam | 9.69 | 121.7 | 19.12 | 1.5E-07 | 3.92E-07

## Slide 85
Permeability Test
LABORATORY TESTING
Material Description | Degree of Compaction (%) | w (%) | γd |  | Ksat | 
 |  |  | pcf | kN/m3 | (in/sec) | (cm/sec)
Coarse RCA | 100 | 10.97 | 123.0 | 19.32 | 5.00E-05 | 1.27E-04
 | 95 | 10.99 | 117.4 | 18.44 | 1.92E-04 | 4.88E-04
 | 90 | 11.5 | 110.5 | 17.36 | 2.63E-04 | 6.68E-04
Fine RCA | 100 | 11.07 | 121.7 | 19.12 | 1.88E-04 | 4.77E-04
 | 95 | 11.06 | 115.5 | 18.14 | 3.90E-04 | 9.90E-04
 | 90 | 11.05 | 109.2 | 17.16 | 3.98E-04 | 1.01E-03
Limestone | 100 | 6.13 | 143.0 | 22.46 | 3.17E-05 | 8.05E-05
 | 95 | 6.11 | 135.5 | 21.28 | 7.52E-05 | 1.91E-04
 | 90 | 6.08 | 128.0 | 20.10 | 1.29E-04 | 3.28E-04
RCA+RAP | 100 | 9.84 | 125.5 | 19.71 | 5.24E-05 | 1.33E-04
 | 95 | 9.76 | 119.9 | 18.83 | 1.89E-04 | 4.79E-04
 | 90 | 9.94 | 113.0 | 17.75 | 5.79E-04 | 1.47E-03
Clay Loam | 100 | 10.78 | 123.0 | 19.32 | 5.39E-08 | 1.37E-07
 | 95 | 10.92 | 116.7 | 18.34 | 5.94E-07 | 1.51E-06
 | 90 | 10.53 | 111.1 | 17.46 | 2.70E-06 | 6.86E-06

## Slide 86
Increasing Suction, Decreasing Saturation
Soil-Water Characteristic Curve (SWCC)
Hydraulic Conductivity Function (HCF)
(Lu and Likos 2004)
Soil-Water Characteristic Curve (SWCC) Test
LABORATORY TESTING

## Slide 87
Dry Sand
Saturation = 0.17
Saturation = 0.40
Saturation = 0.70
Saturation = 0.80
Soil-Water Characteristic Curve (SWCC) Test
LABORATORY TESTING

## Slide 88
Soil-Water Characteristic Curve (SWCC) Test
LABORATORY TESTING

## Slide 89
Soil-Water Characteristic Curve (SWCC) Test
Parameter | Cell 185 - Coarse RCA |  |  | Cell 186 - Fine RCA |  | 
 | 18517GS002 | 18517GS004 | 18517GS008 | 18617GS006 | 18617GS007 | 18617GS008
θr | 0 | 0 | 0 | 0 | 0 | 0
θs | 0.2765 | 0.2782 | 0.2866 | 0.3004 | 0.2812 | 0.2846
α | 0.1508 | 0.2313 | 0.1174 | 0.1819 | 0.0317 | 0.0465
n | 1.1597 | 1.1559 | 1.7310 | 1.1650 | 1.2091 | 1.1787
m | 0.1377 | 0.1348 | 0.1475 | 0.1416 | 0.1730 | 0.1515
Parameter | Cell 188 - Limestone |  |  | Cell 189 - RCA+RAP |  | 
 | 18817GS005 | 18817GS006 | 18817GS008 | 18917GS002 | 18917GS003 | 18917GS006
θr | 0.0419 | 0.0221 | 0.0520 | 0.0070 | 0.0120 | 0
θs | 0.2414 | 0.2467 | 0.2449 | 0.2997 | 0.2987 | 0.2540
α | 0.1728 | 0.1909 | 0.1881 | 0.2805 | 0.2357 | 0.2960
n | 1.6088 | 1.5436 | 1.6808 | 1.2397 | 1.2602 | 1.1700
m | 0.3784 | 0.3522 | 0.4050 | 0.1934 | 0.2065 | 0.1453
LABORATORY TESTING

## Slide 90
TASKS | MONTHS |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33
Task 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 8 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Task 9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
SCHEDULE