## Slide 1: Density Profiling System: Toward Coreless Continuous Compaction Assessment
Kyle Hoegh, MnDOT (presenter)
Shongtao Dai, MnDOT
Eyoab Zegeye, MnDOT

## Slide 2: Acknowledgements
FHWA/AASHTO
GSSI
MnDOT Districts
MnDOT Bituminous Office
Contractors

## Slide 3: Goals
Use Density Profiling System (DPS) to assess field asphalt compaction in a manner that is:
  Continuous and accurate
  Understandable and timely
  Safe, non-invasive, and robust
Eliminate acceptance cores by using density profile
Reduce early pavement failures due to low compaction (ex. longitudinal joint deterioration)
Enhance IC and PMTP
    IC&PMTP measure processes affecting compaction continuously
    DPS can evaluate achieved compaction continuously

## Slide 4: Method Overview: Data Collection
Robotic
(Project with UMN)
Push Cart Type DPS
Vehicle Mounted RDM

## Slide 5: Method Overview: Dielectric to Air Voids
Field Core Calibration
Gyratory Compacted “Puck” Coreless Calibration

## Slide 6: Method Overview: Required Precision
The method requires an instrument capable of
  Scanning at a rate that allows for continuous collection behind the paving operation
  Measuring an accurate dielectric
Developed method based on plastic with known dielectric constant (HDPE)
Published 2019!

## Slide 7: Method Overview: Field Calibration
Swerve Survey

## Slide 8: Method Overview: Field Calibration

## Slide 9: Method Overview: Swerve Correction Results: Contractor vs. MnDOT
MnDOT vs Contractor Prior to Swerve Correction
4.5 ft MnDOT
4.5 ft Contractor

## Slide 10: Method Overview: Swerve Correction Results: Contractor vs. MnDOT
Contractor vs. MnDOT after Swerve Correction
0.5 ft
2.5 ft
4.5 ft

## Slide 11: Analysis: 100% Joint Coverage
Geospatial Representation

## Slide 12: Analysis: Mat Compaction
Swerve Survey
“Random Cores on Steroids”
Nondestructive
Many Samples

## Slide 13
Better Coverage
  100% joint AV%
  Random Mat sampling (random cores on steroids)
  Reduce field cores!
Coreless Calibration: Importance
Elephant = 6 tons
Hedgehog < 1 pound
For every 100 elephants of mix, we sample and test two hedgehogs (cores)
THAT’S IT?

## Slide 14
Coreless Calibration: Method

## Slide 15: Core Locator Application
4 Measurements used to calculate puck dielectric using travel time at known thickness.
Coreless Calibration: Method

## Slide 16
Isolated Reflection
for travel time calculation
Coreless Calibration: Method
Initial Manuscript to Submit this Week

## Slide 17
Coreless Calibration: Variability

## Slide 18
Coreless Calibration: Results

## Slide 19
Coreless Calibration: Results
HD-Model

## Slide 20
Coreless Calibration: New Model Fit
New Model
Logistic function with an asymptotic term.
Logistic function from
Gottschalk, Paul G., and John R. Dunn. "The five-parameter logistic: A characterization and comparison with the four-parameter logistic." Analytical Biochemistry. 23 May 2005. Academic Press. 09 May 2019
Even better match for field data at exremes

## Slide 21
Coreless Calibration: New Model Fit
HD-Model
New Model

## Slide 22
Coreless Calibration Case Study:
May 20th 2019 TH55 Testing

## Slide 23
Coreless Calibration Case Study:
Puck Vs Cores
District Lab ran pucks at low (3.2%), medium (7.0%), and high (12.3%) air voids, field cores taken at low and high dielectrics.
  Only ran SSD to get Gmb to determined how much grams to add or remove to hit high and low air voids
  Tested using Corelok and dielectric in Materials and Road Research Lab
  Confirmed reasonableness of coreless puck predictions by day 2 of production!

## Slide 24
Coreless Calibration Case Study:
Puck Vs Cores
Do dielectric measurement prior to SSD, especially at high air voids
Or, Corelok (vacuum seal)
Or, core dry?
Water effect

## Slide 25
Coreless Calibration Case Study:
TH 55 Daily Report

## Slide 26
Coreless Calibration Case Study:
TH 55 Daily Report

## Slide 27
Coreless Calibration Case Study:
TH 55 Daily Report

## Slide 28
Coreless Calibration Case Study:
TH 55 Daily Report

## Slide 29
Coreless Calibration Case Study:
TH 55 100 ft. Lot Analysis

## Slide 30
Coreless Calibration Case Study:
TH 55 100 ft. Lot Analysis

## Slide 31
Coreless Calibration Case Study:
TH 55 100 ft. Lot Analysis

## Slide 32: Discussion
DPS is a good tool for mapping a continuous coverage of the relative compaction levels (higher dielectric = higher compaction)
Histograms and general statistics can be used to give a complete assessments of the in-place compaction
Potential to eliminate field coring for DPS calibration:
    Calibrate dielectric to mix with variable air void pucks
    Validate DPS air void prediction with cores
    Monitor mix changes with puck tests in plant (do 60 second dielectric test prior to SSD on Gmb pucks)
    Will want occasional validation cores in field to confirm DPS air voids good
Potential Uses:
    Assess compaction density and uniformity for QC/QA.
    Provide on-site feedback to contractor of high and low compaction locations that they can cross-check with differences in mix or paving strategies in those locations to determine optimal construction procedures
    Identification of trends in the air void content maps that can be cross-checked with IC and other data to determine the most critical factors in achieving higher density

## Slide 33: Thanks!
Questions?

## Slide 34: Method Overview: Field Validation
4.0 Dielectric 6.5
0 Relative Frequency 35
166+50 Stationing, ft. 176+50
3 Dielectric 7
Red – Consultant with Walking Cart RDM
Green-MnDOT with Vehicle Mounted RDM

## Slide 35: Summary Field Use: 2018 TH371 contractor experience – equipment validation
Good agreement between Contractor and
MnDOT data: Median dielectric difference < 0.05
Good agreement with field cores: r^2 = 0.87

## Slide 36: Field Use: Evaluate Mix Design or Construction Operations
Comparison of Test Sections
  Mix B (3/4-) to A(1/2-): not much difference on compaction.
  Adding a roller: density slightly increased on this project.
  .
Median Density:
Blue: 94.1%
Red: 94.2%
Yellow: 93.5%
Green: 93.3%

## Slide 37: Field Use: Roller Technique Evaluation
Group Name | Stationing range, ft. | Offset range, ft. | Color | Samples | Core Taken at 10th %, Air Void Content
Roller Technique #1 | 920+00 to 925+00 | Centered on Joint | Red | 1000 | 9.6%
Roller Technique #2 | 935+00 to 940+00 | Centered on Joint | Green | 1000 | 7.7%
Relative Frequency (Bin Count/Group Samples)
0 30
4.0 Dielectric 5.5
Example 500 ft section where 2 different echelon breakdown roller techniques were used on the joint:
  On-site RDM dielectric indicated greater compaction using technique 2
  Core taken at 10th percentile indicated greater compaction in technique 2
On-site dielectric can be used to give feedback as to what techniques are more effective for compaction

## Slide 38
IC and PMTP Technology
Reduced Paver Speeds
Additional Rollers
Delivery Method Changes
Equipment Considerations
Increased Fleet Management
Tarping Trucks
Modification to Rolling Patterns
Steps to Reduce Number of Paver Stops
Monitor Stockpiles
Requesting Paving Crew Summaries
Caring and taking Pride
Process Changes

## Slide 39: Field Use: 2018 TH14 pick-up machine breakdown investigation
Colormap of all sensors close to 89.2 relative density core location (1413+25) ranging from 1413+00 to 1415+00. The red arrow indicates the location where both core and dielectric results showed low density.

## Slide 40: Field Use – QC Contractor Feedback
On-Site Feedback
Contractor could identify low and high density locations
R01 – dielectric 4.1
R02 – dielectric 4.6
Corresponded to 87.8% and 94.2% relative density respectively

## Slide 41: Field Use: GPS based Core Locator

## Slide 42: Field Use – Core Locator
automatically guide field person to location for field verification