## Slide 1: Superpave5 Superpave Design at Five Percent Air Voids
March 11, 2019

## Slide 2: Question?
Is there a way?
To improve asphalt pavement performance
WITHOUT
Increasing COST?

## Slide 3: Marshall Mix Design
Design Air Voids 3-5%
Field Compaction
  8% after rolling
  4% after traffic
Construction (8%)
Decreases to
Service Life (4%)

## Slide 4: Strategic Highway Research Program
“Marshall” carried forward
Design air voids fixed at 4%
Recommended compaction set at 92% Gmm

## Slide 5: As-Constructed Air Voids?
NCHRP Report 573

## Slide 6: Typical Final Density
NCHRP Report 573 Figure 4.8
91.8%
94.6%

## Slide 7
Superpave5 Concept
Mix Design 5% air voids
Field Compaction 95% Gmm
No change in asphalt content

## Slide 8: Does it Change Asphalt Content?
 | Superpave4 |  | Superpave5 | 
NMAS | VMA | Effective Asphalt (volume) | VMA | Effective Asphalt (volume)
9.5 | 15.0 | 11.0 | 16.0 | 11.0
12.5 | 14.0 | 10.0 | 15.0 | 10.0
19.0 | 13.0 | 9.0 | 14.0 | 9.0
25.0 | 12.0 | 8.0 | 13.0 | 8.0

## Slide 9: Does it Change Asphalt Content?
 | Superpave4 |  | Superpave5 | 
NMAS | VMA | Effective Asphalt (volume) | VMA | Effective Asphalt (volume)
9.5 | 15.0 | 11.0 | 16.0 | 11.0
12.5 | 14.0 | 10.0 | 15.0 | 10.0
19.0 | 13.0 | 9.0 | 14.0 | 9.0
25.0 | 12.0 | 8.0 | 13.0 | 8.0
Asphalt Content
Stays Same

## Slide 10: Asphalt Content
 | Superpave4 |  | Superpave5 | 
NMAS | VMA | Effective Asphalt (volume) | VMA | Effective Asphalt (volume)
9.5 | 15.0 | 11.0 | 16.0 | 11.0
12.5 | 14.0 | 10.0 | 15.0 | 10.0
19.0 | 13.0 | 9.0 | 14.0 | 9.0
25.0 | 12.0 | 8.0 | 13.0 | 8.0
Gradation Changes

## Slide 11: Asphalt Content
 | Superpave4 |  | Superpave5 | 
NMAS | VMA | Effective Asphalt (volume) | VMA | Effective Asphalt (volume)
9.5 | 15.0 | 11.0 | 16.0 | 11.0
12.5 | 14.0 | 10.0 | 15.0 | 10.0
19.0 | 13.0 | 9.0 | 14.0 | 9.0
25.0 | 12.0 | 8.0 | 13.0 | 8.0
Gyrations Change

## Slide 12: Design Gyrations??
 |  | Mixture Type | 
ESAL | Gyrations | 9.5-mm | 19.0-mm
3-10 million | 70 | x | 
 | 50 | x | 
 | 30 | x | 
10-30 million | 70 | x | x
 | 50 | x | x
 | 30 | x | x
Purdue University Evaluated Engineering Properties

## Slide 13: Conclusions
Designs at 4% Air Voids And 93% Gmm Compaction
Designs at 5% Air Voids And 95% Gmm Compaction
100 gyrations
30 gyrations
Stiffness, Rutting ≈

## Slide 14: SR 13, Middlebury, Indiana
2013 Trial Project
  13,400 AADT
  19% heavy trucks
First Project

## Slide 15: Mix Designs
 | Superpave4 | Superpave5
#11 Steel Slag | 40 | 43
#12 Limestone | 20 | 17
Stone Sand | 15 | 18
Natural Sand | 18 | 15
RAS (Shingles) | 7 | 7
 | Superpave4 | Superpave5
Gyration | 100 | 30
Asphalt Content | 5.1% | 5.4%
Recycled Binder Ratio | 0.206 | 0.193
Air Voids | 4.0 | 5.0
VMA | 15.5 | 17.0

## Slide 16: Gradation
Chart: Sieve Opening (mm) Raised to the 0.45 Power
| 0 | 3.766628091140912 | 3.766628091140912 | 0 | 2.7573331550931925 | 2.7573331550931925 | 0 | 2.0161002539629291 | 2.0161002539629291 | 0 | 1.4716698795820382 | 1.4716698795820382 | 0 | 1.0773254099250416 | 1.0773254099250416 | 0 | 0.79463568224020453 | 0.79463568224020453 | 0 | 0.58170736792793831 | 0.58170736792793831 | 0 | 0.42583471830473674 | 0.42583471830473674 | 0 | 0.31172925995349998 | 0.31172925995349998
 | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100 | 0 | 100
 | 0 | 100 | 0 | 100 | 0 | 100
Superpave4 | 100 | 92 | 62 | 46.4 | 32 | 22.7 | 13.4 | 7.5 | 4.8
Superpave5 | 100 | 90 | 54.2 | 40.4 | 28.8 | 20.8 | 12.6 | 7.2 | 4.6

## Slide 17: Counter-Flow Drum Mix Plant

## Slide 18: Superpave4

## Slide 19: Superpave5 Compaction
Same Rolling Train

## Slide 20: Mix Construction Properties
 | Superpave4 |  |  | Superpave5 |  | 
 | Design | QC | QA | Design | QC | QA
Asphalt, % | 5.1 | 5.1 | 5.0 | 5.4 | 5.5 | 5.2
Air Voids, % | 4.0 | 3.5 | 4.1 | 5.0 | 4.5 | 4.0
Density, %Gmm | - | - | 91.6 | - | 94.7 | 96.9

## Slide 21: 2018 Core Locations
Location | Superpave4 | Superpave5
1 | 206+66 | 155+95
2 | 147+37 | 180+25
3 | 124+74 | 214+74

## Slide 22: Six Cores At Each Location

## Slide 23: Core Properties
 | Superpave4 |  |  | Superpave5 |  | 
 | Loc 1 | Loc 2 | Loc 3 | Loc 1 | Loc 2 | Loc 3
Thickness, mm | 37.3 | 37.7 | 34.5 | 35.2 | 36.2 | 42.8
Asphalt, % | 5.34 | 5.35 | 5.56 | 5.67 | 5.36 | 5.82
Density, %Gmm | 91.8 | 94.0 | 92.3 | 95.7 | 93.6 | 96.6
Average Values

## Slide 24: Permeability
Chart: Air Voids, %
| 7.7415532042601143 | 7.7136423590706045 | 8.0675037958719855 | 9.0978608520077842 | 8.3710555209919164 | 8.0620712409114077 | 7.0593322625409343 | 5.7079753827155884 | 6.034774143292438 | 5.7759201314043622 | 5.8797067834671424 | 5.5574770057382921 | 8.2168305579915 | 7.8525479116427448 | 7.5770804558693072 | 6.7761564879856309 | 8.1928936291747618 | 7.3213917263432933
Superpave4 | 10.4366 | 12.0048 | 10.344 | 18.0916 | 0.046402 | 5.7156 | 0.55252 | 0.56706 | 0.5089 | 0.53798 | 0.56706 | 0.55252 | 9.8721 | 18.116 | 49.3013 | 5.4395 | 31.3663 | 57.4912
Superpave5 | 5.4225 | 1.9078 | 0.89948 | 1.3503 | 0.5089 | 2.7867 | 0.5089 | 0.52344 | 6.0802 | 2.8663 | 2.8663 | 0.52344 | 0.69792 | 2.9833 | 0.53798 | 3.5829 | 3.6625 | 2.8663

## Slide 25: Recovered Asphalt Binder Grade
 | Superpave4 |  |  |  | Superpave5 |  |  | 
Location | High Fail Temp., °C | Low Fail Temp m, °C | Low Fail Temp, S, °C | ∆Tc, °C | High Fail Temp, °C | Low Fail Temp, m, °C | Low Fail Temp, S, °C | ∆Tc, °C
1 | 99.1 | -15.6 | -24.8 | -9.2 | 95.4 | -20.5 | -24.9 | -4.4
2 | 97.0 | -20.4 | -25.8 | -5.4 | 96.5 | -18.5 | -23.4 | -4.9
3 | 103.9 | -12.7 | -23.1 | -10.4 | 90.1 | -24.1 | -25.7 | -1.5
Average | 100.0 | -16.2 | -24.6 | -8.3 | 94.0 | -21.0 | -24.7 | -3.6

## Slide 26: Asphalt Binder Grade
Chart: Temperature, C
| Superpave4 | Superpave5
HT | 100 | 94
LT | -16 | -21

## Slide 27: Correlation PG High Temp to In-Place Air Voids
Chart: Air Voids, %
| 5.220990228017115 | 5.8773135977903621 | 3.4945446512353584 | 7.7275977816653523 | 6.3836538226282613 | 8.0346892348171224
 | 95.4 | 96.5 | 90.1 | 99.1 | 97 | 103.9

## Slide 28: Correlation PG Low Temp to In-Place Air Voids
Chart: Air Voids, %
| 5.220990228017115 | 5.8773135977903621 | 3.4945446512353584 | 7.7275977816653523 | 6.3836538226282613 | 8.0346892348171224
 | -20.5 | -18.5 | -24.2 | -15.6 | -20.4 | -12.7

## Slide 29: Correlation Delta Tc to In-Place Air Voids
Chart: Air Voids, %
| 5.220990228017115 | 5.8773135977903621 | 3.4945446512353584 | 7.7275977816653523 | 6.3836538226282613 | 8.0346892348171224
 | -4.4 | -4.9 | -1.5 | -9.2 | -5.4 | -10.4

## Slide 30: Pavement Condition Collection

## Slide 31: Smoothness and Rut Depth from Van
 | Superpave4 |  |  |  | Superpave5 |  |  | 
 | IRI (in/mi) |  | Rut Depth (in) |  | IRI (in/mi) |  | Rut Depth (in) | 
 | LWP | RWP | LWP | RWP | LWP | RWP | LWP | RWP
Average Three Locations | 43 | 91 | 0.22 | 0.31 | 28 | 120 | 0.14 | 0.22
Entire Project | 47 | 119 | 0.13 | 0.26 | 53 | 206 | 0.14 | 0.26

## Slide 32: Crack Data from Automated Collection
 | Superpave4 |  | Superpave5 | 
Location | Length (ft/100 ft) | Crack Density (% area) | Length (ft/100 ft) | Crack Density (% area)
Average Three Locations | 142 | 1.39 | 171 | 2.04
Entire Project | 141 | 1.80 | 299 | 1.97

## Slide 33
Superpave5
Superpave4

## Slide 34
Superpave4

## Slide 35
Superpave5

## Slide 36: Superpave4 Superpave5

## Slide 37: What Did We Learn?
Aging of Asphalt Binder Directly Related to In-Place Air Voids

## Slide 38: What Did We Learn?
Changes to Mix Design Can Reduce Aging

## Slide 39: Asphalt Binder Properties
Construction
  80% PG 70-22
  20% PG 130 -0 (est.)
Five Years in Service
  Superpave4 PG 100-16
  Superpave5 PG 94-21
Effect on Life?

## Slide 40: US 40, Richmond, Indiana
2016 Trial Project
  17,800 AADT
  5% heavy trucks
High Density Trial Project

## Slide 41: Mix Designs
 | Superpave4 | Superpave5
#11 Limestone | 50.5 | 46.5
#12 Limestone | 10.0 | 8.0
Stone Sand | 22.0 | 27.0
RAP Fine | 14.5 | 14.1
RAS (Shingles) | 3.0 | 2.9
 | Superpave4 | Superpave5
Gyration | 100 | 50
Asphalt Content | 6.7% | 7.1%
Recycled Binder Ratio | 0.23 | 0.21
Air Voids | 4.0 | 5.0
VMA | 15.6 | 16.7

## Slide 42
November 2016
40°F to 55°F

## Slide 43: Mix Construction Properties
 | Superpave4 |  | Superpave5 | 
 | Design | QA | Design | QA
Asphalt, % | 6.7 | 6.48 | 7.1 | 6.83
Air Voids, % | 4.0 | 4.76 | 5.0 | 5.88
VMA, % | 15.6 | 14.88 | 16.7 | 16.69
Density, %Gmm | - | 93.3 | - | 95.4

## Slide 44
Superpave5
Superpave4

## Slide 45
Superpave5
Superpave4

## Slide 46
Superpave5
Superpave4

## Slide 47
Superpave5
Superpave4

## Slide 48
Superpave5
Superpave4

## Slide 49: Indiana DOT Implementation
<3 million ESALs 30 gyrations
3 million to >30 million ESALs 50 gyrations

## Slide 50: Superpave5
2018
  12 projects let as Superpave5
  9 projects built or partially built
  11 mix designs
    Four 19.0-mm
    Seven 9.5-mm
2019
  Standard specifications changed January 2019
  Specification effective September 2019
  For 2019, option to change Superpave4 projects to Superpave5
Implementation

## Slide 51: 2018 Superpave5 Projects
How did they turn out?

## Slide 52: OK.
Gyratory Voids 4.58%
Density 93.82% 6.18% voids 1.50% difference
Chart: US 231- 9.5 mm Surface
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Gyratory | 4.97 | 4.46 | 6.69 | 5.31 | 5.89 | 5.29 | 5.52 | 2.13 | 3.3 | 4.89 | 3.82 | 2.7
In-Place | 6.88 | 8.51 | 9.35 | 6.03 | 6.93 | 6.79 | 5.44 | 5.9 | 3.16 | 5.57 | 4.61 | 4.51
AverageDensity | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14 | 6.14
AverageGyratory | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58 | 4.58

## Slide 53: Not so good.
Gyratory Voids 4.37%
Density 93.93% 6.07% voids 1.70% difference
Chart: SR 23 - 9.5 mm surface
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
Gyratory | 5.71 | 4.49 | 4.84 | 3.9 | 4.29 | 3.83 | 3.27 | 4.59
In-Place | 5.57 | 5.99 | 6.53 | 4.75 | 5.2 | 4.98 | 7.73 | 7.79
AverageDensity | 6.1 | 6.1 | 6.1 | 6.1 | 6.1 | 6.1 | 6.1 | 6.1
AverageGyratory | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4

## Slide 54: Good.
19.0 mm Intermediate
  Gyratory Voids 5.42%
  Density 93.73% Gmm (6.27% voids) 0.85% difference
Chart: US 30 Mix #1 - 19.0 mm Intermediate
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23
Gyratory | 5.01 | 5.83 | 4.41 | 6.19 | 5.77 | 5.73 | 6.25 | 6.19 | 5.5 | 5.89 | 5.68 | 4.44 | 5.39 | 5.51 | 5.09 | 5.48 | 5.67 | 5.24 | 5.3 | 4.89 | 4.5 | 5.24 | 5.35 | 5.4152
In-Place | 6.48 | 5.97 | 7.68 | 8 | 7.85 | 5.81 | 6.19 | 7.04 | 6.28 | 5.45 | 5.16 | 8.16 | 6.74 | 5.67 | 5.24 | 5.62 | 4.9 | 5.69 | 4.98 | 5.37 | 5.71 | 8.73 | 5.53 | 6.2717
AverageDensity | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27 | 6.27
AverageGyratory | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42 | 5.42

## Slide 55: Good.
Gyratory Voids 5.19%
Density 94.24% 5.76% voids 0.57% difference
Chart: US 150- 9.5 mm Surface
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22
Gyratory | 4.84 | 5.65 | 3.6 | 5.68 | 6.13 | 5.37 | 5.21 | 5.67 | 5.67 | 5.51 | 4.42 | 5.34 | 5.21 | 5.76 | 4.98 | 4.9 | 5.51 | 5.3 | 4.82 | 5.13 | 4.73 | 4.73
In-Place | 6.28 | 4.56 | 5.56 | 5.48 | 7.02 | 8.36 | 9.28 | 7.17 | 6.71 | 6.46 | 4.48 | 6.55 | 5.03 | 5.09 | 6.28 | 4.88 | 3.57 | 4.57 | 5.94 | 5.23 | 4.15 | 4.15
AverageDensity | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76 | 5.76
AverageGyratory | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19 | 5.19

## Slide 56: Another DOT Implementation
<3 million ESALs 30 gyrations
3 million to >30 million ESALs 50 gyrations

## Slide 57: Performance Testing
Design
  Use Ndesign gyratory specimens
    Hamburg or APA Rut Testing
    DCT or SCB
Construction
  Use Ndesign gyratory specimens from QC or QA
    Hamburg or APA Rut Testing
    DCT or SCB

## Slide 58: Superpave5
Increased Life
No Increased Cost
B/C ratio?