## Slide 1
Intelligent Compaction for Grading Materials

## Slide 2: Intelligent Compaction Status
Natural Progression
Quality
Acceptance
(Design Modulus
Met)
Quality Control
(ICMV Map)
Process Control
(Number of Passes)
Constraints
One pass of roller provide one piece of information (ICMV) that influenced by several layers
ICMV is not an instantaneous value but an average value over the width of the roller and some length of project
Density and stiffness are not necessary related
Uncertainty in nonuniformity of soils and aggregates should be considered in solution
2

## Slide 3: Motivation of Study
There are many known advantages to IC
Significant progress in theoretical, interpretation and instrumentation aspects of IC have been made
How come IC is not implemented more widely?

## Slide 4: Intelligent Compaction Parameters
For Quality Control
(Uniformity)
For Quality Acceptance
(Stiffness Extraction)
CMV
CCV
MDP
Evib
Kb
VCV
4

## Slide 5: Ultimate Goal
“to develop procedure(s) that measure
mechanical properties
of earth materials to
facilitate adoption
of IC technologies for field
acceptance”
Straightforward specification
Solid to minimize dispute
E (Modulus, MPa)
k (Stiffness, MN/m)
5

## Slide 6
Framework of Proposed IC Specifications
Step 1: Estimate properties of all layers as done in design
Step 2: Obtain target ICMV and target modulus
Step 3: Pre-map layer of interest to assess uniformity and condition of foundation layer
Step 4: Let contractor perform compaction to achieve target ICMV/stiffness in his/her judgement
Step 5: Map compacted layer
Step 6: Post-Processing to Extract Mechanical Properties
6

## Slide 7
Only Mapping
A single value
  Equivalent modulus down to influence depth of roller.
Premapping & Mapping
Two values
  Modulus of a top layer
  Equivalent Modulus of foundation layers down to influence depth of roller.
Definition of Mechanical Property
h
7
h

## Slide 8: Desire for Straightforward Specification
To Well-Defined Process
Evib
Kb
VCV
From a Blackbox
8

## Slide 9: Desire to Minimize Dispute
Owners
Contractors
Discuss all aspects of quality management with IC
Deliberate all assumptions
Agree on acceptable assumptions that all can live with
Define criteria for acceptance
Discuss remedial solutions
9

## Slide 10
Best Approach to Measure Mechanical Properties of Geomaterial
    Setting Target Value, ・Extracting Mechanical Properties
10
Practical IC Specification for Earthwork (Some Major Items)
Optimal Simulation Method for Estimating Target Value
    Minimizing Calculation Time, Maximizing Accuracy
Optimal Inverse (Backcalculation) Algorithm
    Ensure Required Level of Accuracy , ・Minimize Amount of Time,
    Consider Depth of Influence of IC Roller
Considering Impact of Non-uniformity on ICMV
    Material-Related, ・Moisture-Related
Practicalities
    Optimal Combination of Roller Size/Vibration Frequency/Amplitude/Speed
    Optimize contractors’ desire for accelerating production vs. obtaining high quality and uniform product, ・How to present the results
10

## Slide 11
How to Set Target ICMV
11
Simulation of Roller Measurements (Forward Model)
Select Roller Parameters
Select Material Type for Layers
Estimate Layer Properties
output
inputs
Set at the time of Pavement Design
Chart: Deflection
Static vs. Dynamic
Stationary vs. Vibratory
Linear vs.
Nonlinear
Layer Thickness
Drum Dimensions
Nonlinear k Parameters
Inputs
Sensitivity Analysis
Soft Computing
?
Understand Behavior then Simplify

## Slide 12
Calibration of Model
12
Embedded
Geophones
h2
h1
Moving Direction
Moving Direction
Mounted
Accelerometer
GPS
Antenna
Roller DAQ
Ground DAQ
GPS Antenna
Accelerometers and Connections to DAQ
Geophones
Accelerometers
Data
Acquisition
Box

## Slide 13
Calibration of Model
13
Embedded
Geophones
h2
h1
Moving Direction
Moving Direction
Mounted
Accelerometer
GPS
Antenna
Roller DAQ
Ground DAQ
Chart: Distance from Drum, m
| -2.1287075552611112 | -1.9125627119808011 | -1.6612663108054171 | -1.358078451067497 | -1.0293013677532521 | -0.68531892058367405 | -0.34431575068507098 | 0 | 0.35447444042494602 | 0.71999609798800102 | 1.0751980280014231 | 1.432755260264579 | 1.8016360325579579 | 2.1344316598044699
Field Data | 0.061829 | 0.073355 | 0.084061 | 0.12374 | 0.12732 | 0.1623 | 0.24176 | 0.30325 | 0.26172 | 0.1619 | 0.094729 | 0.08747 | 0.08549 | 0.08568
FE Model | -0.0072122 | -0.0052303 | 0.0011772 | 0.013739 | 0.035644 | 0.072777 | 0.13569 | 0.24317 | 0.27941 | 0.32084 | 0.36779 | 0.42127 | 0.48143 | 0.54908 | 0.62431 | 0.70654 | 0.79788 | 0.89958 | 0.99099 | 1.0295 | 0.99167 | 0.90101 | 0.80007 | 0.70947 | 0.62796 | 0.55346 | 0.48652 | 0.42708 | 0.37432 | 0.32806 | 0.28732 | 0.25176 | 0.14673 | 0.085562 | 0.048697 | 0.024498 | 0.0054538 | -0.013188 | -0.032917
Geophone
Depths
FE Model
Drum
Pavement
Chart: Geophone Measured Peak Vertical Displacement, mm
| 1.35 | 0.74 | 0.74 | 0.38 | 1.05 | 0.56000000000000005 | 0.63 | 0.32 | 0.67 | 0.33 | 0.28000000000000003 | 0.16 | 0.8 | 0.31 | 0.27 | 0.13 | 0.31 | 0.2 | 0.46 | 0.19 | 0.2 | 0.12 | 0.22 | 0.09 | 0.75 | 0.46 | 0.7 | 0.37 | 0.59 | 0.31 | 0.61 | 0.26 | 0.247 | 0.22 | 0.18 | 0.27 | 0.17399999999999999 | 0.14000000000000001 | 0.34 | 0.24 | 0.14000000000000001 | 0.37 | 0.28000000000000003 | 0.11
 | 3.1494 | 1.6643 | 1.5857 | 0.83506 | 2.4895 | 1.3137 | 1.7454 | 0.91958 | 2.5137 | 1.3266 | 1.6924 | 0.89145 | 1.15 | 0.57 | 1.12 | 0.61 | 0.3 | 0.26 | 0.75 | 0.54 | 0.16 | 0.12 | 0.84 | 0.7 | 2.3842 | 1.3943 | 2.3944 | 1.2693 | 1.4141 | 0.90277 | 2.9827 | 1.6404 | 1.7265 | 1.3973 | 0.90772 | 1.3264 | 1.1055 | 0.7267 | 1.2232 | 0.97442 | 0.63008 | 1.8363 | 1.5181 | 0.99409
Cleburne, TX: Stationary Test, Embankment | 3.1494 | 1.6643 | 1.5857 | 0.83506 | 2.4895 | 1.3137 | 1.7454 | 0.91958 | 2.5137 | 1.3266 | 1.6924 | 0.89145
MnROAD, MN: Moving Test, Subgrade | 2.3842 | 1.3943 | 2.3944 | 1.2693 | 1.4141 | 0.90277 | 2.9827 | 1.6404
Line of Equality | 0 | 8
Calibration

## Slide 14: Development of Artificial Neural Network (ANN)
Number of input parameters | 5
Number of hidden layers | 1
Number of neurons in hidden layer | 20
Inputs pre-processing function | Sigmoid function
Outputs post-processing function | Linear function
Neural network type | Feed-forward
Network training algorithm | Bayesian Regularization Backpropagation
Number of epochs (maximum number of training iterations before training is stopped) | 1000
Training ratio | 70%
Validation ratio | 15%
Testing ratio | 15%
Chart: FE MRBase, MPa
Line of Equality | 0 | 1700
± 20% Error | 0 | 2026.128
± 20% Error | 0 | 1350.752
Chart: Number of Neurons
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50
Training Dataset | 72.0555 | 47.0425 | 43.9545 | 41.2795 | 39.4081 | 39.0128 | 38.8458 | 37.4299 | 36.6333 | 36.1248 | 35.3129 | 35.4824 | 35.3695 | 35.8748 | 35.2136 | 34.7994 | 34.3948 | 34.7851 | 34.8712 | 33.7194 | 34.1614 | 34.5688 | 33.5857 | 33.9706 | 33.8083 | 33.7343 | 33.8378 | 33.0151 | 33.121 | 33.0151 | 33.4813 | 32.5883 | 32.7872 | 32.249 | 33.4215 | 32.3728 | 32.573 | 32.2645 | 32.6956 | 31.6702 | 32.6956 | 31.9061 | 31.8434 | 31.6544 | 32.4808 | 31.9687 | 31.3528 | 31.0966 | 31.4484 | 31.209
Test Dataset | 72.9589 | 48.0104 | 42.2019 | 43.9773 | 40.025 | 37.3363 | 39.3192 | 37.2693 | 36.5513 | 37.3497 | 39.8623 | 36.9594 | 38.3145 | 35.0286 | 37.2424 | 34.6987 | 38.4708 | 36.4005 | 36.2629 | 37.5233 | 34.2491 | 33.8231 | 37.0945 | 35.4683 | 36.2353 | 37.7359 | 34.7707 | 37.7889 | 35.0571 | 35.4683 | 34.7707 | 35.327 | 36.4143 | 38.4318 | 32.078 | 38.2623 | 36.0832 | 38.1182 | 36.756 | 39.0128 | 34.7707 | 33.6006 | 37.7094 | 36.3456 | 33.8231 | 35.1426 | 40.2741 | 37.1887 | 36.3043 | 37.6032
Optimize
Validation
ANN
14

## Slide 15
Chart: Backcalculated ELWD-BASE (MPa)
| 117 | 193 | 138 | 134
 | 140.8547 | 228.5607 | 183.0731 | 169.57
Line of Equality | 0 | 500
+/- 20% Uncertainty Bound | 0 | 738
+/- 20% Uncertainty Bounds | 0 | 492
Chart: Measured Modulus (MPa)
Line of Equality | 0 | 500
+/- 20% Uncertainty Bounds | 0 | 600
+/- 20% Uncertainty Bounds | 0 | 400
Modulus
LWD
Local Calibration
15

## Slide 16: Improve colormaps
Mazari et al. (2017) Impact of Geospatial Classification Method on Interpretation of Intelligent Compaction Data
16

## Slide 17: ICMV Distribution
17

## Slide 18
18
Achieving Real Time Data Analysis & Quality Control

## Slide 19
Too soft
Be Concerned
Our Observations
19

## Slide 20
Proposed Final Protocol
Proof-Map Lot
Cells with high COV
COV > 50%
Rework
Uniformity not achieved
Cells with low COV
COV < 35%
Cells with moderate COV
35%<COV < 50%
Accept with 7 LWD Tests
CMVs ≤ 5
Rework
Too soft to test!
30 > CMV > 5
CMVs > 30
Accept with 3 LWD Tests
CMVs > 5
7 LWD
Tests in Red Areas
20

## Slide 21: What have we learned
TxDOT 0-6903 - 21
Achieving density is necessary but not sufficient
  Density and modulus are not directly related.
  A number of sites that achieved density failed to yield moduli that met design requirements (sometimes by wide margin).
  Areas with low subgrade moduli propagate all the way to the surface.
Earthwork final product is inherently variable, we need to manage it (not ignore it)
  A reasonable amount of variability should be accepted to be practical
  IC can quantify variability in a real time manner
  Use average results of more data points with a faster field tests
    time to run 3-7 LWD = time to perform one NDG
21

## Slide 22: Final Words
IC technology for quality management makes perfect sense to make sure that
  final product is uniform (achievable now)
  design modulus has been met (achievable in near future)
Even though conceptually mature, there are still institutional and technical details to work out
These details can be worked out in a straightforward manner if we work together
22

## Slide 23
23
Happy IC’ing!!

## Slide 24: Thank you!!