## Slide 1: 2019 Pavement Workshop May 21-23, 2019
Cold Central Plant Recycling (CCPR) – Update 2019
Derek Tompkins
Principal Civil Engineer
American Engineering Testing, Inc.

## Slide 2: What is CCPR?
5/22/2019 | NRRA Workshop | 2
CIR methods with stockpiled RAP
Add binder as required
Pave as usual
CCPR vs CIR
Avoids possible concerns about in-place material
Stockpiling with fractionating allows for the development of a consistent material
Additional costs of CCPR for storing, processing, etc

## Slide 3: Survey and Lit Review
5/22/2019 | NRRA Workshop | 3
Recent NCAT/Virginia DOT study is known well
Most states have limited experience with CCPR – initial respondents discuss in terms of CIR
Extensive experience with CCPR on the West Coast dating back to 1970s
  Survey is reaching out to states, municipalities, and contractors out west
Respondents have pointed out difficulties of cost comparison – literature reinforces these difficulties
More to follow as survey completes and tech briefs are produced

## Slide 4: MnROAD field sections
5/22/2019 | NRRA Workshop | 4
Single-source RAP
Constructed Fall 2017
3.5” CCPR lift after compaction
Placed on 12” Class 6, clay/loam subgrade
CELL | SURFACE | SPEC | BINDER | LTC req.
133 | Double chip seal FA-3/FA-2.5 | Emulsion (58S-28) | CIR-EE (H) | -21.4°C
233 | Double chip seal FA-3/FA-2.5 | Foam (58S-28) | 58S-28 | -21.4°C
135 | 1.5” HMA SPWEB340C | Foam (XX-34) | 52-34 | -21.4°C
235 | 1.5” HMA SPWEB340C | Emulsion (XX-34) | CIR-TEC M | -21.4°C

## Slide 5: MnROAD Performance: Cell 233
April 2018
Cell 233
Foamed 58S-28, Double Chip
5/22/2019 | NRRA Pavement Workshop | 5
March 2018

## Slide 6: Rutting, Cells 133 & 233
5/22/2019 | NRRA Pavement Workshop | 6
September 2018
Cells 133, 233
Double Chip (F28, E28)

## Slide 7: Transverse Cracking, Cell 133
5/22/2019 | NRRA Pavement Workshop | 7
May 2018
Cell 133
Emulsion 58S-28, Double Chip

## Slide 8: MnROAD CCPR: Roughness
5/22/2019 | NRRA Pavement Workshop | 8

## Slide 9: Lab Testing
5/23/2019 | NRRA Workshop | 9
Special emphasis on low temperature performance
  DCT and SCB @ -18 C
Indirect tension (IDT) AASHTO T 322
Hamburg wheel tracking AASHTO T 324
Dynamic modulus (E*) using SPT

## Slide 10: Indirect tension (T 322)
5/22/2019 | NRRA Workshop | 10

## Slide 11: Hamburg Wheel Tracking
5/22/2019 | NRRA Workshop | 11
 | Passes to Failure (12.5 mm) | Creep Slope (um/pass) | Stripping Inflection Point (SIP)
Foam 58S-28 | 3520 | -2.97E-03 | 2935*
Foam XX-34 | 2880 | -3.83E-03 | --
EE 58-28 | 7120 | -1.28E-03 | --
EE XX-34 | 5400 | -1.66E-03 | --

## Slide 12: Dynamic modulus
5/22/2019 | NRRA Workshop | 12
F28

## Slide 13: Disk-Shaped Compact Tension
5/22/2019 | NRRA Workshop | 13
DCT specimens remained intact through early loading
Batched specimens from field mix outperformed specimens used for mix design development

## Slide 14: Semi-Circular Bending @ -18°C
5/22/2019 | NRRA Workshop | 14
Low temp SCB procedure by Dr. Eyoab Zegeye Teshale of MnDOT Office of Materials and AET1
Alternative/companion to DCT to estimate fracture energies for reclaimed specimens

## Slide 15: Research products & timeline
5/22/2019 | NRRA Workshop | 15
Surveys
Summaries of
  State of practice
  Performance testing and analysis
  Spec recommendations
Final report

## Slide 16
Principal Investigator | Technical Liaison
David Rettner, AET | Dave Van Deusen, MnDOT

## Slide 17: Mix Designs
5/22/2019 | NRRA Workshop | 17
BINDER TYPE | Emulsion | 
MnROAD CELL | 133 | 135
SURFACING | DCS | 1.5" SP
PG | 58S-28 | XX-34
BINDER ADDED, % | 2.0 | 
Voids @ Opt, % | 11.5 | 11.7
Max Dens @ Opt, pcf | 133.1 | 132.8
Marshall @ Opt, lbs | 1272 | 1365
Ret. Stability @ Opt, % | 72.1 | 71.0
Raveling, % | 1.60 | 1.70
Est Crit Crack Temp, °C | -35 | -36
IDT @ CC Temp, psi | 155 | 158
Developed at AET in Summer 2017
Exceeded low temp req of -21.4°C
Exceeded dry stability of 1250 lb
While no MnDOT requirement for raveling, foamed mixes did not meet target of 2.0%

## Slide 18: Mix Designs
5/22/2019 | NRRA Workshop | 18
BINDER TYPE | Foamed | 
MnROAD CELL | 233 | 235
SURFACING | DCS | 1.5" SP
PG | 58S-28 | XX-34
BINDER ADDED, % | 1.5 | 
Voids @ Opt, % | 12.2 | 10.8
Max Dens @ Opt, pcf | 133.7 | 131.8
Marshall @ Opt, lbs | 1311 | 1272
Ret. Stability @ Opt, % | 70.4 | 73.2
Raveling, % | 3.30 | 2.50
Est Crit Crack Temp, °C | -34 | -34
IDT @ CC Temp, psi | 128 | 132
Developed at AET in Summer 2017
Exceeded low temp req of -21.4°C
Exceeded dry stability of 1250 lb
While no MnDOT requirement for raveling, foamed mixes did not meet target of 2.0%