## Slide 1: Quarter Century of MnROAD Advancements 2019 NRRA Pavement Workshop
Benjamin Worel, P.E. (MnROAD Operations Engineer)
Minnesota Department of Transportation
May 23, 2019

## Slide 2: Gerald Rohrbach Distinguished Speaker
MnDOT for 35 + years
  Director of Office of Materials and Road Research
  MnDOT
  NCHRP committees
  AASHTO Subcommittee of Materials
Gerry created a productive culture…..
Liked and respected by all
Everybody had an important role to contribute
Working together you can be a part of something bigger than yourself

## Slide 3: Presentation Outline
History
(MnROAD 101)
MnROAD
Key
Advancements
(We have come along way)
Future

## Slide 4: MnROAD Early History
AASHO Road Test (1956-58 built – traffic loadings from 1958-60)
Need for Local Calibrations
  MnDOT started Investigation 183 / Flexible Designs (Started 1960’s)
  SHRP/LTPP started for national efforts (8/8/1988)
  Idea of a cold regions testing facility (1980’s)
MnROAD Development
  Development of Support
    Getting 25 million in 1990
  Soil Foundation
  Instrumentation
  1992 and 1993 Construction
  August 2, 1994 Traffic

## Slide 5: MnROAD – why is was really built?

## Slide 6: MnROAD Background
MnROAD Owned and Operated by Minnesota DOT
~25-Years of Long Term Customer Service
HMA and PCC Pavements
New and Rehabilitation
Major Experiments
  Phase I (1994-2006)
  Phase II (2007-2016)
  Phase III (2017-Future)

## Slide 7: MnROAD Operations
Research Development / Partnerships
Coordination of Construction
Traffic Loadings
Performance Monitoring
  Cracking / Rutting / Ride / FWD, …..
Sensors
  Static (Environmental)
  Dynamic (Traffic Loading)
MnROAD Database
Technology Transfer

## Slide 8: Phase-I Key Stakeholders
Construction / Research Funding
  MnDOT
  Local Road Research Board
Research Funding and Major Projects
  FHWA project support
  University of Minnesota
  Cold Regions Research and Engineering Laboratory
MnDOT and LRRB Relationship since 1959

## Slide 9: Phase-II Key Stakeholders
Construction / Research Funding
  MnDOT
  Local Road Research Board
  FHWA / SHRP 2
Research Funding and Major Projects
  Multiple Pooled Fund Efforts
    1:1 - One pooled fund : One project
  University of Minnesota + Other Universities
  Development of TERRA
MnDOT and LRRB Relationship since 1959
PooledFund.org

## Slide 10: Phase-III Stakeholders
MnDOT and LRRB Relationship since 1959
Construction / Research Funding
  MnDOT
  Local Road Research Board
  Industry Partnerships
Research Funding and Major Projects
  Development NRRA
  Bigger Pooled Fund Efforts
    Pooled Fund : Many Projects
    Many Universities / Consultants
  NCAT Partnership
  MnDOT Lead Pooled Funds

## Slide 11: Thermal Cracking ~ 1990
Marshall Mix Designs
  Did not take the environment into account
MnROAD HMA Test Sections
  AC-20 and 120/150 Binders
  5 and 10 year test cells (thin / thick)
  Varying Base Types
Northern Climates Accepted Cracking

## Slide 12: Low Temperature Cracking
Major Findings
  1994 MnROAD Test Sections (PG 64-22, PG 58-28)
  1999 LVR (PG 58-28, 58-34, 58-40)
Cell 19
Cell 1
AC 20 (PG 64-22)
AC 120-150 (PG 58-28)

## Slide 13: National HMA Cracking Performance Test
PG Grading System
2 MnDOT Led Pooled Funds – 4 Universities
NCAT Partnerships
  Utilize both MnROAD / NCAT Test Tracks
    Top Down / Reflection / LTC cracking Efforts
Balanced Mix Design

## Slide 14: MnROAD Partnerships Rejuvenators October 2018 - Cargill and Hardrives
Cargill – 2018 MnROAD Transitions
  Control - 25% RAP Superpave (SPWEB540 / PG 58S-28)
  High RAP - 45% RAP Superpave (SPWEB540 / PG 58S-28 / Anova)
  Lab Testing / Long Term Monitoring
Cargill 2018 MnROAD Transitions
Collaborative Aggregates – 2017 Hennepin Mix
  NB Control - 30% RAP
  SB - 30% RAP / Delta-S
2019 NRRA Rejuvenator Test Sections
  TH-6 (Emily to Outing, Minnesota)
  7-10 Rejuvenators / Industry pays for extra costs / NRRA monitors
    Control – 30% RAP (Project)
    Control – 40% RAP
    Treatments – 40% RAP with Rejuvenators

## Slide 15: Importance of Sealing
PCC Lane / HMA Shoulder Sealing
  Cell 7 Control
  Cell 8 Sealed
Similar results for HMA Pavements
MnDOT: Ruth Roberson
Roger Olson
Chad Millner
Cell 8
Cell 7
  Results
    * 89% reduction between cells
    86% reduction within Cell-8

## Slide 16
Drainage - Effects of Trapped Water
Asphalt
  Deterioration asphalt
  Increased roughness (ride)
Concrete
  ML Observations (high traffic)
    None - PASB used
    Some - Class-5 / well sealed joints / edge drain
    High amount - Class-5 / no edge drains
  LVR Observations (low traffic)
    If sealed class-5 is not as destructive
    If not-sealed class-5 can develop joint damage
Benefits
  Importance of drainable bases / sealing
  Effect on ride

## Slide 17: Class-5 (Minnesota Common Base Material)
3%
7%
Both Class-5 Material
Same Performance?

## Slide 18: Pavement Drainage / Base Improvement s Subsurface Drainage Innovations
HMA and PCC Underlying Base Layers
  Updated specifications Class 5Q in lieu of Class 5
    Tighter Gradations “More drainable and Stable”
  Large Stone Base Materials
    Good performance / ~40% less Frost Depth
    Concrete
      Geocomposite Joint Drain
      Non-Woven Geotextile interlayer
      (PCC overlays of PCC)

## Slide 19: Seasonal Load Limits Spring Restrictions / Winter Overloads
Spring Thaw
MnROAD Models
Thawing Index
Monitoring Sites Installed around the State
MnDOT Website

## Slide 20: MnROAD ME Designs Impacts
Flexible – MnPAVE Flexible
Major Inputs into PavementME (HMA and PCC))
Rigid – MnPAVE Rigid
Concrete Overlay of Asphalt

## Slide 21: Concrete Innovations
PCC Designs
  Very a lot
  Somewhat Conservative
  True for LVR and Mainline Test Sections (Tom Burnham)
Test Cell | MnDOT Method | 1993 AASHTO 95% Rel. | 1993 AASHTO 50% Rel. | 1984 PCA Method
5 | 5.8 | 1.2 | 5.1 | 2.9
6 | 2.6 | 0.8 | 3.3 | 0.7
7 | 4.4 | 2.3 | 9.3 | 2.2
8 | 2.4 | 0.8 | 3.2 | 0.6
9 | 3.9 | 1.8 | 7.2 | 1.6
10 | 12.0 | 5.3 | 19.2 | 76.4
11 | 13.1 | 3.0 | 12.0 | 60.2
12 | 12.0 | 4.3 | 16.1 | 75.9
13 | 12.1 | 4.2 | 16.1 | 69.4

## Slide 22: Whitetopping Design
TPF-5(165) Pooled Fund
  10 state participation
  National design procedure
  19 Test Cells (built: 1997, 2004, 2008)
Observations
  Learned the important factors – accelerated loading
    Thickness
    Panel size
    HMA condition and seasonal behavior
    Importance of bond
    Importance of sealing
Benefits
  Rational (optimized) design procedure
  Provides options for distressed asphalt pavements

## Slide 23: Diamond Grinding Innovations
Evolution from Lab to Specification
  Purdue Study
  Built with industry involvement
    IGGA
    Diamond Surface Inc.
  Tested at MnROAD
    Cell 37 LVR
    Mainline following years
  Developed a specification
  Used in Minnesota and around the country
2007 TRADITIONAL GRIND
2008 INNOVATIVE GRIND
2007 INNOVATIVE GRIND
2010 INNOVATIVE GRIND
NGCS

## Slide 24: Sustainable Technologies
Warm Mix Asphalt
Recycled Pavements
  Asphalt, Shingles, Concrete
  New Pavements, Recycled Base Materials
Surface Treatments
  Chip Seal, Microsurfacing, Fog Seal
Thin Pavements
  - Unbonded Overlays, Novachip
In Place Recycling
  FDR, Stabilized FDR
Lower Construction Costs, Shorter Construction Time, Improved Pavement Performance
Reduce
Reuse
Recycle

## Slide 25: InPlace Recycling
Road Science Partnership
  3 Cells (mainline) / 1 Cell (LVR)
Observations
  2.75” Interstate surface on engineered FDR
  Engineered emulsion  balance stiffness/flexibility
Benefits
  Design for distressed pavements/Full depth repairs

## Slide 26: SPR-5(375) Phase-II PG2 - Pavement Preservation Pooled Fund
  MnDOT Lead State
  Partnership with NCAT
  3 year Study (2019-2021, add 2022-2023)
  24 Partners
  Red States – 5 year commitment
    3 States
    Foundation of Pavement Preservation
  Green States – 3 year commitment
    16 States
    FHWA
  Blue States – Verbal commitment
    3 States
Notes: Through Dec 30, 2023
Auburn Univ (NCAT is a non profit arm of Auburn) is a subcontractor to MnDOT

## Slide 27: Roadway Details
Roadway | LR-159 | US-280 | CSAH-8 | US-169
Traffic volume | Low | High | Low | High
Thickness (inch) | 5.5 | 9.9 | 7.0 | 6.5
Section length (feet) | 100 | 528 | 528 | 528
# Test Sections | 23 | 34 | 22 | 21
Age (Years) @placement | 14 | 9 | 6 | 6
NCAT Offsite Test Sections
Lee Road 159 (2012)
US-280 (2015)
MnROAD Offsite Test Sections
  Mille Lacs County CSAH-8 (2016)
  US-169 (2016)
  70th and 80th Street Recycling

## Slide 28: Northern Layout of US-169/CSAH-8
Northern
High Traffic
Preservation
on US-169
Northern
Low Traffic
Preservation
CSAH-8

## Slide 29: Pavement Preservation Study 70th and 80th Construction Timeline
Project Initial Review (2018)
Mix Designs – (May/June 2019)
Construction
  Partnering with Industry
  June 2019
    Hot Mix Recycling
  August 2019
    Cold In-Place Recycling (foam/emulsion)
    Cold Central Plant Mix Recycling (foam/emulsion)
    Stabilized Full Depth Recycling (foam/emulsion)
    Mill and Fill (Control)
    1” Thinlay Overlay
Notes: Through Dec 30, 2023
Auburn Univ (NCAT is a non profit arm of Auburn) is a subcontractor to MnDOT

## Slide 30: Early Intelligent Construction Tools
Ground Penetrating Radar
Early MnROAD Cell-28 HMA thickness vs cracking and fatigue

## Slide 31: Intelligent Construction Tools
Veta Software TPF-5(334)
HMA Rolling Patterns
Paver Operations / IR Temperature Bar
3D GPR / Rolling Density Meter (pooled fund)

## Slide 32: Current NRRA Initiatives
Construction
  2017 MnROAD
  2018 Missouri CCP
Long Term Projects
  2017 - 8 Projects
  2019 – 12 Projects
Short Term / Technology Transfer Projects
  2017 - 8 Projects
  2019 – 4 Projects
Already Covered already in the workshop
Thanks for everyone's efforts
(Shows the power of what can be done together)

## Slide 33: Other Current Non-Pavement Partnerships
Autonomous Vehicle Testing
  Effects on pavement design
Roadside Vegetation
  University of Minnesota Studies
  Erosion Control Classes 2019
Traffic/WIM Technology
  Kistler, Intercomp, IRD
3M
  Machine Vision
  Pavement Marking

## Slide 34: MnROAD Test Section Benefit Types
Direct
  Savings of materials
Indirect
  Time savings and quality
Avoidance
  Don’t do that on the system
Demonstration
  Confidence to try something new

## Slide 35: MnROAD Benefits (only for Minnesota)
Phase-2
  5:1 B/C Ratio
  Surface Characteristics (HMA/PCC), Pervious Pavements, Implements Husbandry, Stabilized Full Depth Reclaimation, Lightly Surface Roadways, Chip Seal Video, Whitetopping, Thin PCC, Optimal Timing of Preventive Maintenance, Low Temperature Cracking II, Quiet Rumble Strips, Drainable/Stabile Bases
  Phase-3 with NRRA???????
Phase-1
  9:1 B/C Ratio
  Seasonal Load Restrictions; Low Temp Cracking

## Slide 36: MnROAD and LTPP InfoPave FHWA and i-Engineering
Initial Development
TRB 2019
Working on this summer
MnROAD Access
Data
Pictures
Reports/Software
Ties to
LTPP Data
Westrack
C-SHRP

## Slide 37: New Technology of Interest
Google Earth
2008-2019
Google Earth
Opens up the idea of walking a road from your computer
Panorama Camera
Create your own images like a house tour
https://makevt.com/media/tourmaker/iqrcgsaydj/

## Slide 38: Technology Transfer Efforts
Research Pays Off Seminar Series
  Every 3rd Tuesday
  10-11 am
NRRA
  May Workshops
  Technical Visits
  Want your ideas
Newsletters
  Highlight Members
  Highlight NRRA Projects
  Highlight Emerging Technology
MnROAD NCAT Sponsor Meetings
  Early Spring / Late Summer
Pavement Workshop
May 23-24, 2018

## Slide 39: NRRA National Request for Ideas / Innovation
Need New Ideas
  Available Real Estate now
    New Construction
    Rehabilitation
    Maintenance
Processes
  Informal – MnROAD Website
  Formal - Call for Innovation
    Due: August 2, 2019
  Balance Portfolio
    Traditional Research
    Non-Traditional Research
MnROAD Website http://www.dot.state.mn.us/mnroad/newideas.html

## Slide 40: Thank You
Questions?
Benjamin Worel
ben.worel@state.mn.us
NRRA shares Gerald Rohrbach’s vison: Working together you can be a part of something bigger than yourself

## Slide 41: National Test Tracks Past/Present/Future
Wyoming
~Future HMA Mainline
Florida
~2020 Concrete Mainline
Illinois
1960’s
WesTrack
1990’s